Fatigue limit estimation of metals based on the thermographic methods: A comprehensive review

Mohammad Zaeimi1, Rosa De Finis2, Davide Palumbo1 and Umberto Galietti1*

1Polytechnic University of Bari, Department of Mechanics, Mathematics and Management, Via Orabona, 70125 Bari, Italy

2 University of Salento, Department of Engineering for Innovation, Piazza Tancredi, 73100, Lecce, Italy

*Corresponding author: umberto.galietti@poliba.it

Abstract

Infrared Thermography has been under review in the last thirty years due to its versatility and potential in the detection of the thermal signature associated with intrinsic energy phenomena due to dissipative processes, specifically those relying on mechanical fatigue. Nowadays, it is a well-established technique that can support mechanical and structural engineers to implement a damage-tolerant design, assess the residual life, and finally characterize the fatigue behavior of materials.

The aim of this work is to review all thermography-based approaches and procedures for fatigue limit estimation by rapid tests, draw considerations on the role of thermal methods in mechanical design and machine construction, and discuss the pros and cons of each method and open points. This review is intended on one hand, as a warning/guideline to direct new research toward issues that have not been fully resolved or understood yet and on the other hand, to sum up, what has already been done in the field.

Keywords: Thermographic method, Rapid fatigue estimation, Fatigue assessments, Fatigue parameters, Energy-based methods

# NOMMENCLATURE

| A1, A2, a, b | Material constants |
| --- | --- |
| Cp | Specific heat [J/kg K] |
| E | module of elasticity [Pa] |
| Ed | portion of supplied mechanical power that converts in heating [W/m3] |
| Ed2w | second amplitude harmonic of heat dissipated [W/m3] |
| Erev | power of reversible energy variations [W/m3] |
| Es | rate of internal energy that does not convert in heating [W/m3] |
| F | cyclic load in fatigue test [N] |
| f | frequency of loading [Hz] |
| K | thermoelastic constant [m3/J] |
| N | number of cycles |
| Nf | number of cycles to failure |
| Q | heat rate exchanged with the environment [W/m3][W/m3] |
| q | heat flux [W/m2] |
| R | stress ratio |
| Ri, Rθ | slope of temperature at the beginning of temperature trend |
| Rr | relative slope of temperature at the beginning of temperature trend |
| se | entropy flow [W/m3 ℃] |
| T | Temperature [℃] |
| T0 | reference temperature [℃] |
| T1ω, T1 | first amplitude harmonic of temperature [℃] |
| T2w, T2 | second amplitude harmonic of temperature [℃] |
| Ta | amplitude of the temperature [℃] |
| Td | dissipative temperature [℃] |
| TE | thermoelastic temperature [℃] |
| Telastic | temperature due to elastic deformation [℃] |
| Tmax_r | residual temperature [℃] |
| Tplastic | temperature due to elastic deformation [℃] |
| Tstabilized | stabilized temperature rise [℃] |
| Tthe | thermoelastic amplitude of the temperature [℃] |
| tf | time up to the fatigue failure [s] |
| U | internal energy rate [W/m3] |
| W | mechanical energy rate [W/m3] |
| Wp | plastic energy [J] |
| W2w | second amplitude harmonic of mechanical energy [W/m3] |
| α | linear thermal expansion coefficient [1/℃] |
| γf | fatigue fracture entropy [W/m3 ℃] |
| Δs | first invariant change of the stress tensor [Pa] |
| ∆T | temperature rise [℃] |
| ε | strain |
| θ | slope of temperature at the end of temperature trend |
| θE | phase lag due to thermal diffusion |
| θD | phase lag due to thermal diffusion |
| ρ | density [kg/m3] |
| Σ0 | cyclic load in fatigue test [N] |
| σ | stress [Pa] |
| σa | stress amplitude [Pa] |
| σ0, σy | yield stress [Pa] |
| σi | stress level [Pa] |
| σc | fatigue limit [Pa] |
| φ | phase angle between temperature and loading signal |
| φ1 | Phase of the first Fourier component of temperature |
| φ2 | phase of the second Fourier component of temperature |
| Ψ | damping capacity |
| ω | angular frequency [Hz] |

# INTRODUCTION

Infrared thermography, a contactless, non-destructive and full-field experimental technique has demonstrated in these years its versatility in the field of experimental mechanics and mechanical design owing to the possibility of carrying out structural integrity investigations [1-14], stress analysis (thermoelastic stress analysis-TSA) evaluations [15-22] and energy-based assessments to study fatigue processes [23-26]. In effect, it has been thirty years since the tests assisted by an infrared (IR) camera were developed to obtain reliable parameters capable of describing, from an energetic point of view, the fatigue processes [27-31].

Thermography-based methods have evolved a lot due to more performant equipment and robust tools for data analysis. Nowadays, some considerations can be drawn upon the robustness and reliability of such methods to support fatigue investigations in terms of damage analysis and assessment, residual life predictions, and above all, fatigue limit estimations [32-40].

Basically, the motivation for the development of alternative and innovative procedures to estimate the fatigue limit, relying on the use of an experimental technique during fatigue tests, lies on two points:

- the rapidity of the testing procedures with respect to classic protocols

- the possibility to obtain more information about the material state during the loading.

Referring to the first point, while classic well-established fatigue characterization methods [41, 42] (i.e. constant amplitude tests to obtain the Wöhler curve) represent a standard, they are time and cost-consuming due to the number of samples being tested to obtain a statistical significant fatigue limit estimation, and due to the test duration involving high energy, operability, and maintenance costs. In general, a classic fatigue test involves a pristine material tested until its failure at a specific stress level, stress ratio and mechanical frequency.

To reduce testing time and costs, rapid fatigue testing was developed according to the approach of La Rosa and Risitano [42] based on a sequence of constant amplitude loading blocks applied in a stepwise manner; where the stress amplitude and the mean stress are increasing while both the frequency and stress ratio are fixed for a specific number of cycles in each block, until material failure. During such a test program, the material experiences different damage regimes [43, 44], as discussed later. The switch from one regime to another determines discontinuities in the behavior that can be associated with critical stages of fatigue life, hence leading to the fatigue limit estimation. In other words, the main concept behind the so-called ‘stepwise’ tests, is that the value of the fatigue limit coincides with the first increase of the temperature, so that by using a specific loading procedure, significant temperature variations associated with the damage can be assessed [42-45].

As per the second point, a key role in the development of such a thermography-based technique was played by the possibility to obtain more complementary information about the fatigue behavior, from a simple classic test: estimation of energy dissipated due to fatigue processes, identification of the damage onset and locations [36]. The processing of thermal signal ensures somehow the just said outputs.

In recent years, the aforementioned technique has gained improvements in the pioneering procedure and many developments, especially in the evaluation of the heat sources related to intrinsic dissipations [27-46]. The approaches presented in the literature, relying on the estimation of heat sources accompanying damage phenomena [27-46], are based on the assessment of specific energy-based indices/parameters: (a) Mean temperature increase (usually the mean value of the steady state temperature) [39, 47-55], (b) Initial slope of the temperature [39, 56, 57], (c) Energy loss per cycle [23] (d) Temperature harmonic components [33, 36, 58, 59], (e) Loss of the adiabaticity which the approach relies on the study of the thermoelastic signal and the thermoelastic phase shift [15, 36, 60, 61] and (f) Fracture fatigue entropy [62].

In Fig. 1, an overview of the main idea of the well-established methods based on the above parameters is presented. Once the parameters have been assessed, well-established procedures [41, 42, 63-65] can be applied to estimate the fatigue limit.

The present review is organized as follows: In section 2 the heat dissipations induced by fatigue damage are discussed, in section 3 the approaches relying on well-established methods to obtain thermal indices and recent advances are presented while in section 4 the basics of fatigue under stress-controlled tests and the typical experimental setups for fatigue tests assisted by an IR-camera are presented. Section 5 is focused on the procedures to obtain the fatigue limit using stepwise and static tensile tests while section 6 deals with a general discussion on methods (pros, cons, achieved milestones) and open points to be resolved to further enhance the methods. Finally, the paper is concluded in Section 7.

FIGURE 1 Thermal parameters to study fatigue and procedures for estimating fatigue limit [41, 42, 63-65]

# THEORY: HEAT SOURCES RELATED TO FATIGUE DAMAGE

As already demonstrated by pioneer researches [66], it is well-established that fatigue is a dissipative process [67-86] starting at the microscopic level [67, 71, 83] and culminating in fatigue cracks. As explained in the work of Schijve [87] where the crack onset occurs at stress amplitudes below the yield limit.

Bauschinger [83] showed that during cyclic loading, very small inelastic, i.e., plastic, micro-strains occurred [77]. However, the microscopic reasons that cause fatigue failure remained obscure and were not studied further until the beginning of the twentieth century when Ewing and Humfrey [85] observed the slip bands and microcracks developed on the surface of a fatigued steel. Following, the damage mechanics explained that the appearance of cyclic slips, a not non-recoverable phenomenon due to strain hardening [87], determined the slips accumulation and a microcrack is then formed which may continue to grow under further cyclic loading, Fig. 2a.

| (a) | (b) |
| --- | --- |

FIGURE 2 (a) Fatigue crack initiation mechanism [81], b) schematic illustration of slip band extrusions during a cyclic straining [88]

From a macroscopic point of view, the slip bands produced during cyclic loading result in the formation of extrusion-intrusion pairs that in turn produce surface roughness which could be a direct cause of crack initiation Fig. 2.

According to Murakami [77], the fatigue limit can be defined as: ‘the threshold stress for crack propagation and not the critical stress for crack initiation’ and the main conclusion, still valid, from the work of Bauschinger [83] and Ewing & Humfrey [85] is that the fatigue damage results from the accumulation of many very small irreversible plastic cyclic micro-strains.

Under an energetic point of view, during a fatigue test, by neglecting the possible phase transformations in material (i.e., shape memory alloys or crystallizable rubbers), two inner heat sources are generated due to mechanical loading: dissipative and thermoelastic sources [84]. The former produces the temperature increase of specimen while the latter are reversible and related to thermomechanical coupling phenomena. In Boulanger’s work [38], the authors analytically separate both thermal contributions from each other in order to analyze separately the influence of fatigue damage on each one. Referring to dissipative heat component, it is related to fatigue damage mechanisms due to the inelastic/anelastic behavior of the material [67, 68]. As discussed before, irreversible plastic deformations are responsible for crack nucleation/growth and propagation and in the presence of macroscopic strains in the material during fatigue tests, the mechanical energy is dissipated in all loading cycles. Graphically, this energy consumption can be represented by a hysteresis loop in the stress-strain curve [69, 74, 82] and the area is the measure of the dissipated energy. An amount of this energy converts into heating, another one remains stored internally to produce irreversible deformations [24, 68, 70].

By observing Fig. 3a, the total power balance according to the first principle of thermodynamics applied to a body subjected to a mechanical load, is as follows:

| W+Q=U=Erev+Ed+Es | (1) |
| --- | --- |

where W is the rate of total work energy supplied to the material, Q is the rate of the heat exchanged with the environment and U is the internal energy variation from the initial to the end of the test. Erev is the power of reversible energy variations, while Ed is the portion of supplied mechanical power that converts in heating and Es is the rate of internal energy that does not convert in heating. The sum of Ed+Es corresponds to the rate of irreversible energy variations that are related to the fatigue damage. Different techniques derived it indirectly by considering the difference between the mechanical energy (W) and the energy released as heat (Q ) [70].

Stress-strain hysteresis behavior in metals is dependent on the micro-mechanisms which dissipate energy during cyclic deformation. These processes determine a lag in the response of the material (strain) to an applied force (or stress) during cyclic deformation [82] and then the appearance of the hysteresis loop is explained. The ability of materials to dispel energy by internal adjustments is referred to as damping [69].

A sketch of the specimen in Fig. 3a shows the dissipative powers involved in fatigue processes. As the temperature is a sentinel of inner heat sources produced by cyclic loading, different authors dealt with the study of thermal signature associated with reversible and irreversible heat sources [15-18, 20-27, 29, 31, 32, 34-46, 49, 59], Fig. 3b (the quantities ∆θE,∆θD are respectively the phase lags due to thermal diffusion, of first harmonic and second harmonic and ∆θ the difference between the two) [33].

The reversible energy variations produced by small volume changes inducing ‘thermoelastic effect’ [36] are represented in Fig. 4. In the case of uniaxial sinusoidal loading, the thermoelastic coupling related temperature variations can be expressed as follows:

| T=Tthe sin⁡(2πft+π+φ) | (2) |
| --- | --- |

where T is the temperature variations at the mechanical exciting frequency f, Tthe is the peak-to-peak signal amplitude and φ (is the phase angle between temperature and loading signal) [89]. The symbol ‘π’ has been included according to the classic theory of thermoelastic stress analysis, where the temperature and first stress invariant have opposite signs [18]. Fig. 4 depicts the relations between T and φ in two opposite cases [36, 60].

| (a) | (b) |  |
| --- | --- | --- |

FIGURE 3 Energy balance during cyclic loading [24] and heat converted energy and detected thermographic signal, (b) Schematic illustration of temperature variations due to reversible (thermoelastic) and irreversible (dissipated energy) phenomena [33].

| (a) | (b) |
| --- | --- |

FIGURE 4 Thermoelastic phase shift φ: temperature and stress relation (a) under adiabatic condition, (b) under non-adiabatic conditions [36]

A phase shift depending on several factors can occur in the presence of phenomena leading to the loss of adiabatic conditions (dissipative process). The loss of adiabaticity is associated with a thermal dissipative process.

In general, intrinsic dissipations produce heating in the form of two distinct contributions:

- heat produced under the hysteresis conditions (anelastic regime) [67],

- heat produced under visco-plastic deformations regime [73, 80],

These heat contributions, clearly affect the adiabaticity of the processes and then determine the variation in φ values. It is necessary to remark that in the case of a purely elastic cyclic response, the adiabaticity level (and the value of φ) depends on the loading frequency. The higher the loading frequency, the higher the adiabaticity level.

By focusing on the irreversible energy variations during fatigue tests (Fig. 3a), the irreversible work energy supplied to the material depends on the adopted stress ratio. When the stored energy Es is negligible, heat converted energy (Ed) can be obtained directly from thermodynamic balance. Ed, however, can be assessed by analyzing the surface temperature of the sample [9, 49] and can be expressed as:

| Ed=ρCp∆Td | (3) |
| --- | --- |

where ∆Td are the dissipative temperature variations, ρ is the density while Cp is the heat capacity at constant pressure. In previous research, Jordan [30] found a direct relationship between the mechanical energy variation (area under the hysteresis loop) and heat converted energy during fatigue. Fig. 5a shows the variation of the hysteresis loop within the fatigue regimes during classic constant amplitude tests to build Wholer’s curve [68].

During rapid fatigue tests [90], a self-heating effect [46, 78] is produced in the material involving two mechanisms. According to Mareau [78], the first one is associated with a reversible movement of the dislocations (mechanically reversible but thermally irreversible) and the second one is with plastic activity. The latter is associated with the progressive appearance of microplasticity [86], while some open points still exist about the mechanisms occurring during the primary regime.

In Fig. 5b, according to Munier’s study [46], a model was proposed to link the self-heating measurements and high cycle fatigue properties of metals in terms of temperature variations. In particular, in Fig. 5c, a Representative Elementary Volume (REV) is defined as an elasto-plastic matrix containing several lattice discontinuities e.g., inclusions.

| (a) | (b) |
| --- | --- |

FIGURE 5 (a) fatigue life and dissipated energy [68] (b) modeling of men temperature variations and micromechanical damage processes [46]

Under low stress amplitudes, inclusions were considered behaving in the same way as the matrix while the dissipation was mainly due to the elasto-plastic behavior of the matrix. Further, above a given stress value, plastic hardening within the inclusions was activated. In these conditions, the dissipation associated with the matrix corresponds to the primary regime and that associated with the set of inclusions to the secondary regime. The latter, according to the Munier’s approach [46] governed the physical process of fatigue damage initiation.

Besides the cyclic loading, the tensile test was reported to be an efficient way to estimate the fatigue limit. Risitano and Risitano [65] proposed that, during tensile tests, fatigue failures happen at points in the material’s stress–strain curve where the local stress is able to produce plastic deformation. These stresses will be intensified in comparison to the average applied stress (load/area) and fatigue failure occurs due to local plastic conditions. Therefore, the specimen will fail when it is loaded at the above-mentioned average value [65]. This specific value can be found when the linear trend, thermoelastic behavior in Fig. 6, of the maximum temperature of the surface is lost [65].

FIGURE 6 Qualitative stress–strain and temperature - strain curves [65]

This happens due to the fact that the local intensified stress causes irreversible micro-plastic deformations (zone II in Fig. 6) and consequently heat dissipation. As mentioned by Risitano and Risitano [65] and according to Fig. 6, except for some crystals which are deformed plastically, most of them are stressed in an elastic field. In contrast, the plastic deformation increases in zone III and it completely involves every crystal in zone IV. In the following sections the well-established and recent advanced approaches to obtain thermal parameters to study fatigue behavior will be presented together with the procedures to estimate the fatigue limit.

# DIFFERENT METHODS TO INVESTIGATE THE THERMAL BEHAVIOR FOR FATIGUE PREDICTION

## Direct Temperature Assessment

### Mean temperature increase

The self-heating phenomenon dates to the work of Stromeyer [91] in 1914 and then it has been used for a rapid fatigue limit prediction. In 1983, the pioneer researcher, Risitano [43], and in 1986 Curti et al. [34], explored the ability of thermography as a non-contact sensing technique for determining the fatigue limit based on the surface temperature [42].

It is worth noting that the variation of the surface temperature is mainly due to a macroscopic result of the energy transfer. The advent of the heat dissipation and self-heating regime during the cyclic loading can be mainly tracked by internal mechanisms of the fatigue damage, or simply microplasticity. Furthermore, external factors, for example thermal convection and radiation, can significantly affect the temperature change [35, 55, 92].

La Rosa and Risitano [42] studied the behavior of the surface temperature of specimens under cyclic loading. As proposed in Fig. 7, (Na and Nf are correspondingly, the number of cycles to reach the stabilized temperature and the failure), for loads higher than the fatigue limit, the temperature exhibits a typical behavior: an increase from the beginning of the test (phase 1) followed by a “stabilization” (phase 2) until a short time before failure, and finally a sharp increase before failure (phase 3).

They noted that the greater the stress with respect to the fatigue limit, the higher the rate of temperature in phase 1 and the “stabilization” temperature in phase 2 [42, 44]. By using the temperature of the steady state (∆Tsteady) acquired during a stepped loading procedure, it is possible to investigate the fatigue behavior of material and components [36, 45].

FIGURE 7 Surface temperature behavior and phases (thermal increments vs number of cycles)

In another pioneer study [41], the intrinsic dissipation was introduced by Luong as an accurate indicator of damage initiation. Using the coupled thermomechanical equation and subtracting the thermal image at different reference time, the intrinsic dissipation can be estimated by acquiring the mean temperature. It should be noted that the quantification of the intrinsic dissipation for engineering materials is difficult (e.g., measurements of surface thermal signature can be affected by heat exchanges hence the resulting measurement is just an estimation of internal heat energy dissipated [45]). The quantification of intrinsic dissipation becomes more complex in the case of brittle or high diffusive materials due to small temperature changes [45] requiring the development of specific smoothing procedures. De Finis et al. [45], developed a new procedure of thermal data analysis. They filtered out the superficial temperatures including the environmental temperature and the one produced by the heating from the hot servo-hydraulic fixture of the loading machine. The ambient temperature effect was removed by subtracting the surface temperature of a dummy specimen. On the other hand, the loading machine contribution was eliminated by assuming a linear temperature increase and using a specific data fitting procedure of longitudinal thermal profiles lying in the gage length and affected by such disturbing heating. These recent advances in image processing, make infrared thermography capable of detecting the fatigue limit for different types of materials (in particular, automotive components) and stress paths (reversed tension, rotating bending, cyclic torsion, etc.)  [49].

Crupi found a relationship between the stabilized temperature increment ∆Tstabilized and the square of the applied stress (σa) amplitude [37] based on damping in materials. Damping is a material or system property to dissipate energy under cyclic loading, which can be obtained either from the exponential free decay curve or the half-power bandwidth method in time or frequency domain, correspondingly [37]. As shown in Fig. 8, the onset or the evolution of damage and defects leads to a change in the dynamic characteristics, for example the specific damping capacity Ψ, and particularly, the natural frequency of the materials which are related to damping parameters (e.g., the loss factor and damping ratio) [37]. Crupi proposed a model as follows [37]:

| ∆Tstabilized=0, σa<σc∆Tstabilized=a σa2+b,σc≤σa≤σy | (4) |
| --- | --- |

where a and b denote material constants depending on the specific damping capacity Ψ and σc and σy are the fatigue limit and the stress amplitude, respectively.

FIGURE 8 Specific damping Ψ versus the stress range ∆σ, relative to AISI304 specimens at a load ratio R = 1 and a frequency f = 100 Hz [37]

The specific damping capacity is related to the stable hysteresis loop, which is a fatigue parameter, and consequently to the ∆Tstabilized. A higher a value means a higher ∆Tstabilized under the same σa which implies that the fatigue damage accumulation is accelerated. Briefly, ∆Tstabilized related to different loading levels can be found using only one specimen through the stepwise loading and acquired thermography sequences [37].

Based on the same parameter, the stabilized temperature, Wang et al. [93] developed the Quantitative Thermographic Methodology (QTM). By taking advantage of the shakedown theory and multiscale concept, they provided theoretical support for the relevant energy analysis and an intrinsic correlation between stress amplitude (σa), ∆Tstabilised and Nf was considered. Recently, Feng et al. [94] proposed a modified version of QTM by including the heat exchange with the help of the heat diffusion equation [26, 38, 95] and considering the variable amplitude loading by assuming that the damage can be equivalently transformed from one loading block to the another [96].

### Initial slope of the temperature curve

Through the fatigue tests, it was shown that there exists a close connection between the temperature rise during the first stage and the material degradation under cyclic load. The evolution of the temperature slope as a function of normalized number of cycles, with respect to the number of cycles to failure, for Aluminum 6061-T6 is presented in Fig. 9. It increases at the beginning of the test, then falls quickly and remains relatively flat in the stabilization phase for about 90% of the life, and finally rises sharply [90].

FIGURE 9 The evolution of the temperature slope in bending fatigue of Aluminum 6061-T6 [90]

On the right hand of the temperature curve (phase III, in Fig. 7), Huang et al. [97] revealed experimentally, for some stainless steel and superalloys, a sharp increase of temperature just after a steady-state condition and very close to the final failure. This rise, as shown in Fig. 10, was reported to be associated with the initiation and propagation of macrocrack [50] and forthcoming fracture.

FIGURE 10 Temperature slope just after a steady-state condition

However, it seems not to be an effective index since it is determined after a huge damage accumulation and through a time-consuming process.

On the left hand of the temperature curve, phase I, the temperature rise angle before stabilized phase, is considered to be a possible index as already mentioned in pioneer works by Curti et al. [34] and Botny and Kaleta [98]. Boulanger et al. [38], showed that the initial slope of the temperature rise is an effective index for studying the fatigue behavior and specifically for estimating the dissipated energy. Mehdizadeh and Khonsari [62] proposed that the fatigue limit estimation capability of this slope (see Fig. 11a), depends on the sharp slope change in Rθ-σ curve (shown in Fig. 11b as an example for SS 304 [62] with fatigue limit around 230 MPa). In addition, a relation for determining the fatigue life as a function of the temperature slope in the first phase of the temperature trend was reported by Amiri and Khonsari [56, 57].

As shown in Fig. 11a, since the slope of the temperature evolution, R=∆T/N, is measured in the early stages of the test, it offers a very rapid technique to predict the fatigue life, preserving testing time and avoiding catastrophic failure. The drawback is that the relation pertains to the fatigue tests of fresh specimens with no prior damage, in other words, there is no parameter to consider the specimen’s history. Later, Khonsari and colleagues modified the aforementioned relationship by considering the accumulated damage for a non-pristine sample [39] that is similar to the case of stepwise tests. Meyendorf et al. [47] demonstrated that when the specimen has already experienced fatigue, its microstructure has been changed and thus its thermal response differs from the pristine specimen. Through a series of fatigue tests on cylindrical dog-bone samples machined from forged titanium, they reported a gradual change in the rate of temperature as the number of cycles accumulates [47].

| FIGURE 11 (a) Temperature Slope at the beginning of the test and (b) fatigue limit predicted by initial slope of temperature for SS 304 (Redrawn based on [56]) |  |
| --- | --- |

As the sample experiences cyclic fatigue, the temperature rise after each stop considerably increases. According to this observation, Amiri and Khonsari [39] presented that this slope as a function of time can also be useful for determining of remaining fatigue life; in this way, the level of prior fatigue damage can be quantified. It is worth pointing out that all of these works were accomplished during an excitation loading which is a short-time mechanical loading [47].

In another work by Liakat and Khonsari [99], another indicator called relative slope (Rr) was shown to be utilized for prediction of the remaining fatigue life. It was defined as the difference between the slope of the temperature rise (R) and the intercept of the slope and number of load cycles (R-N) curve. By defining the relative slope Rr, Liakat and Khonsari [99] showed that it is a linear function of N and was considered a promising index in both constant and variable amplitude cyclic loadings for damage accumulation in cases without stress concentration and simple dog-bone geometry. Furthermore, the slope of temperature can be utilized to predict the fatigue limit by estimating the entropy accumulation and plastic energy generation [100] which are discussed later.

## Thermoelastic Stress Analysis

The thermoelastic effect was observed by Gough [48] while the first experiments were performed by Weber [101], and then the theoretical foundations were defined by Thomson (later known as Lord Kelvin) [102]. Briefly, the concept of Thermoelastic Stress Analysis (TSA) is based on the reversible temperature changes during the elastic deformation of homogenous solids under adiabatic conditions. Under these assumptions, a linear dependence between surface temperature variations and the first stress invariant can be provided [18, 20, 22, 103, 104]; called the classic TSA equation [104]:

| ρCpΔTT0=-αΔs | (5) |
| --- | --- |

where ρ is the density, Cp is the specific heat under constant strain, ΔT is temperature change, T0 is the reference temperature, α is the coefficient of linear thermal expansion and Δs is the first invariant change of the stress tensor [103]. This linearity is violated when non-adiabatic phenomena like heat diffusion due to intrinsic damage sources occur. A comprehensive review can be found in the works by Wong et al. [103, 105, 106]. For the classic TSA equation, by considering a uniaxial stress with sinusoidal loading, the temperature variations can be described as follows:

| T=αρCTasinωt+π+φ | (6) |
| --- | --- |

Eq. 6 presents a phase angle between temperature and loading signal which depends on different factors such as the thickness of the painting or the gripers. In the presence of high stress gradient and viscoelastic–plastic behavior, there are considerable phase signal alterations due to the loss of adiabatic conditions and fatigue damage [60].

As mentioned before, the capability of TSA is not limited to the sample or component in presence of the adiabatic condition. Thermoelastic temperature amplitude (T1ω) and thermoelastic phase can be used as a sentinel of non-adiabaticity, and then they indirectly lead to study the damage behavior of material and to estimate the fatigue limit during a stepwise loading test [30, 58, 59, 107, 108], as presented below.

### Loss of adiabaticity (thermoelastic phase analysis)

Palumbo and Galietti [60] proposed a novel empirical method, called Thermoelastic Phase Analysis (TPA), based on the phase of the thermoelastic signal to study fatigue behavior of stainless steel. The feature is also useful to estimate the fatigue limit. In effect, phase can change due to the presence of either visco-plastic behavior of material [63, 89] or high stress gradient which leads to heat conduction and loss of adiabatic conditions [18, 20, 109, 110]. This of course leads to a loss of adibaticity and then changes in thermoelastic phase trend.

For a better explanation, Fig. 12a shows the change in phase signal with four stress amplitudes, the first two below the fatigue limit and the other two beyond the fatigue limit around 170 MPa of ASTM A182. As can be seen, a significant rise of the phase was observed for stress amplitudes more than the fatigue limit; which means the loss of adiabatic conditions and indicates the damage occurrence [60].

In TPA, the thermoelastic data were extracted during the second phase of the temperature trend (in Loung’s method) when the average surface temperature remains constant [60]. For each loading step, the maximum phase change (Δφmax) was calculated by subtracting the max and min phase values during a certain thermographic sequence. Then from the variation of Δφmax with stress amplitude, a point in the curve with a sharp shift in the slope can be found (see Fig. 12b), which corresponds to the fatigue limit [60].

| (a) | (b) |
| --- | --- |

FIGURE 12 (a) Thermoelastic phase map for four different loading steps of ASTM A182 and (b) the maximum phase change curve [60]

A similar variation, ϕEI in Fig. 13, was also reported by Cappello et al. for C45 [21]. Comparing with the classical thermographic method (ΔTmax) in Loung’s method, TPA data (Δφmax) showed superior performance for some material or components that experience not significant temperature values. It is reported that TPA shows better performance in comparison with the fatigue prediction method based on only the stabilized temperature in materials with higher ductility [60]. In Fig. 13, The green and blue cross marks show the minimum value (5th percentile) and the maximum value (95th percentile) which were changed with the loading amplitude [21].

In another study, De Finis et al. [36] showed the reliability of the fatigue limit prediction by using the phase shift data after proper data analysis. Furthermore, its sensitive behavior with increasing the stress amplitude [36] makes it a proper index to monitor the transition between the plastic and viscous phenomena and for describing dissipative phenomena related to the plastic stress regime.

| (a) | (b) |
| --- | --- |

FIGURE 13 (a) Thermoelastic phase map for four different loading steps and (b) its variation for C45, R=0.1 [21]

### Loss of linearity of FAH (first amplitude harmonic)

Krapez et al. [30, 59], and later De Finis et al. [36, 51], proposed similar temperature models to take advantage of using the first amplitude harmonic. By comparing the first temperature amplitude with its linear trend evaluated at the beginning of the test, a significant difference was reported when the stress amplitude is higher than the fatigue limit. In other words, in presence of damage, microplastic phenomena occur within the material and the TSA equation is no longer valid. In these conditions, for a given stress value, the loss of linearity of the first harmonic can be observed and the stress value can be associated with the fatigue limit. The full field maps of the first harmonic amplitude of temperature for C45 with a fatigue limit of around 200 MPa and its variation (EI in [21]) are shown in Fig. 14 a and b, respectively.

It can be seen in Fig. 14 b, the nonlinearity occurred around 220 MPa very close to its fatigue limit [30]. Noted that green and blue crosses in Fig. 14 indicate minimum and maximum related values [21]. It is worth to note that the intensity of the slope change of the curve depends on both the material and the stress ratio [30, 36].

| (a) | (b) |
| --- | --- |

FIGURE 14 (a) First harmonic amplitude map for four different loading steps and (b) its variation for C45, R=0.1 [21]

## Energetic approaches

Works on the relation between fatigue (or failure) and energy can be tracked from the 1920s [111]. Nevertheless, just the beginning of the 1940s and 1950s several researchers considered a correlation between the fatigue life of a material and the strain energy dissipation during the fatigue process [25, 74]. A promising suggestion was that the strain energy needed for failure of a material subjected to a static test is similar to the strain energy dissipated during a fatigue process [30].

FIGURE 15 Normalized strain energy variation during the fatigue test for Al 6061-T6 [74]

As shown in Fig. 15, the strain energy (or the normalized strain energy which is the strain energy density per cycle per the strain energy density in the steady-state strain region) rises with the number of cycles as plastic deformation or damage accumulated [74].

### Second amplitude harmonics (SAH)

Enke and Sandor [58] showed how the evaluation of dissipative heat sources allows the assessment of the damage of material. By assuming no large mean strain (fully reversed cyclic loading), they presented a general form of thermo-elastic-plastic response. Applying the Fourier sine series on the thermal signal obtained from an infrared camera, they mentioned that the amplitudes at the frequency and twice the frequency of the mechanical loading are proportional to the elastic and plastic strains (or deformation), respectively. A schematic description of the hysteresis loop with the variations of stress, strain and temperatures is shown in Fig. 16 for a single sinusoidal loading. From a to b, the elastic strain is increasing while the temperature is falling, both in sinusoidal form. In elastic unloading, from b to c, the temperature is due to only elastic deformation (Telastic). This behavior is repeated for c-d and d-e but with opposite sign for elastic temperature contribution. As reported clearly by Enke and Sandor [58], Fig. 16, for each cycle of elastic temperature response, two cycles of plastic temperature response occur, therefore, the frequency, 2f, is fundamental for Tplastic. Note that at the beginning of the test, this temperature contribution is zero and it increases with plastic deformation and damage. As an example, the full field maps of the second harmonic amplitude of temperature (DI in [21]) for C45 with fatigue limit of around 200 MPa is shown in Fig. 17.

FIGURE 16  A schematic representation of hysteresis loop and temperature variations during a single cycle under a sinusoidal stress (Redrawn based on [58])

| (a) | (b) |
| --- | --- |

FIGURE 17 (a) Second harmonic amplitude map for four different loading steps and (b) its variation for C45, R=0.1 [21]

In addition, Krapez et al. [30, 59], showed that the energy variations produced by irreversible processes determine a second harmonic temperature component, which was first suggested by Bremont and Potet [31], as a fatigue indicator. They studied the thermal signal in the frequency domain to separate both the dissipative and thermoelastic sources.

For improving the accuracy of the measurement of the dissipated energy, Shiozawa et al. [33, 112] proposed a technique that benefits from the phase 2f lock-in infrared method. It works with a double frequency component of temperature change which includes the influence of both energy dissipation and thermoelastic source (see Fig. 3b). The technique can remove the superficial portion of dissipated energy (or generally the noise components) related to thermoelastic temperature, ∆TE, caused by harmonic vibration of the loading machine. The aim was finding the real temperature rise due to the energy dissipated, ∆Td, and consequently the energy dissipated rate, q, which were calculated as follows:

| ∆TE=-KT∆σ | (7) |
| --- | --- |
| q=ρCp∆Td | (8) |

where K is thermoelastic constant, T is the absolute temperature and ∆σ is the sum of principal stresses from IRT.

De Finis et al. [24], investigated the capability of the second amplitude harmonic (SAH) of temperature (ΔT2w) signal as an indicator to predict the heat dissipated energy. Additionally, they studied the relationship between SAH of heat dissipated rate ∆Ed2w and mechanical energy rate ∆W2w for C45 steel under two stress ratios, R= 0.1 and -1, as follows:

| ∆W2w=A1 ∆Ed2w+A2 | (9) |
| --- | --- |

where the coefficients A1, A2 depend on the material. While the first one was reported to be dimensionless, the second dimension has the same of either ∆W2w or ∆Ed2w.

The endurance limit can be estimated from the latter one [113] by ∆Ed2w and then the area under the hysteresis loop. However, the accuracy of this approach depends on the following assumptions, (i) the full conversion of the mechanical energy into heat, (ii) considering only a portion of ∆Ed and (iii) determining of ∆Ed2w from ΔT2w on the surface which is smaller than the value related to the actual heat source. Furthermore, a framework was analytically developed and validated experimentally by Meneghetti and Ricotta [70, 114] to provide a correlation between intrinsic dissipation and the second amplitude harmonic.

### Specific Heat loss

Meneghetti [23] presented another promising parameter for fatigue characterization based on the energy per cycle in a unit volume rather than the surface temperature. Using the energy balance equation, a relationship between thermal power dissipated per unit volume (including conduction, convection and radiation) and the cooling rate (∂T∂t) was found from temperature evolution curves after a sudden interruption of the fatigue test, see Fig. 18.

FIGURE 18 Slope of the cooling rate

After finding the rate from experimental measurements, the heat dissipated was calculated [23, 92]:

| Q=-ρCf∂T∂tt=t* | (10) |
| --- | --- |

where ρ and C represent respectively the mass density and the specific heat, f is the frequency. This heat loss only depends on the applied cyclic loading characteristics, mean, amplitude and stress state. Applicability of this method can be observed for different steels and fracture mechanics approach [115-117]. As an example, the fatigue limit predicted with thermal energy dissipated, or the cooling gradient, for AISI 304L stainless steel is shown in Fig. 19.

FIGURE 19 fatigue limit prediction with thermal energy dissipated or the cooling gradient for AISI 304L stainless steel [118]

For a given material, loading and mechanical boundary conditions, the surface temperature depends on the geometry of the sample, loading frequency and heat exchange from the material to the surroundings. However, the dissipated energy is only dependent on applied stress amplitude and load ratio. Therefore, surface temperature cannot be adopted for geometries and testing conditions different from the reference ones [23].

Rigon et al. [119] showed that the cooling gradient just after t* is at least one order of magnitude higher than the heating gradient at the same time. Therefore, of the total heat production, the dissipated fraction is by far greater than the self-heating fraction. Furthermore, in a more recent study, Rigon et al. [40] proposed the successful application of the method in fatigue test under in-phase and out-of-phase axial/torsional multiaxial loadings. It is worth mentioning that the thermographic technique is mainly carried out for uniaxial fatigue tests where the occurrence of a steady‐state temperature period in the temperature curve is feasible. However, this assumption cannot be always made in case of multiaxial loadings that is not the focus of this paper, and the reader can refer to an interesting work by Skibicki et al. [120] who investigated the applicability of thermography in fatigue life prediction under multiaxial and non‐proportional fatigue loadings.

### Entropy based methods

Based on the thermodynamic theory of irreversible process, Naderi et al. [121], proposed that the entropy generation during the fatigue test can be regarded as a degradation index. According to this work, entropy accumulates until reaches a value called fatigue fracture entropy (FFE) and defined as follows:

| γf=0tfWpT-q. grad TT2 | (11) |
| --- | --- |

where γf is the fatigue fracture entropy (FFE), tf is the time up to the fatigue failure and q is the heat flux across the boundary; infrared thermography was used to record the temperature evolution, T, during the entire test; and the plastic energy, Wp, determined by Morrow’s cyclic plastic energy dissipation formula [122]. The evolution of rate of entropy flow of aluminum 6061 up to failure occurs is shown in Fig. 20.

In low-cycle fatigue where the entropy generation is dominantly due to the plastic deformation, the second term in the integral can be negligible [100]. They verified that γf is a material constant, independent on the geometry as well as load and frequency [100].  As can be seen from the temperature trend, after the steady state phase, entropy increases sharply around 90% of the fatigue life, like what mentioned about the temperature slope at the beginning of the test (see Fig. 11). From this observation, Naderi and Konsari [123] stated that the operation should be continued until  γ≤0.9 γf.

| (a) | (b) |
| --- | --- |

FIGURE 20 Evolution of rate of entropy flow of aluminum until failure occurs: (a) variation with temperature; (b) variation with time  [90]

In other studies, they showed that the cyclic energy dissipation in the form of thermodynamic entropy can be effectively used to calculate the evolution of the fatigue damage [90] and remaining life prediction [62]. Through an experimentally-verified analytical approach, Jang and Khonsari [124] showed that the energy dissipation due to irreversible microplastic deformation and recoverable internal friction is required to be assessed for FFE calculation [124-127], see Fig. 21.

FIGURE 21 The schematic diagram of energy generation as a function of stress or strain showing the contribution of
microplastic and internal friction [128]

## Thermoelastic point inversion assessment

A different approach has been adopted by Risitano and Risitano [65]. They estimated the fatigue limit by assessing the end of the thermoelastic effect during a static test (Static Thermographic Method). Generally, the thermal behavior of metals or crystalline solids under tensile test can be distinguished by two distinct zones, the elastic zone with linear stress–strain relationship and the plastic zone in which not all crystals are deformed in an elastic field.

As Risitano and Risitano mentioned, a static tensile test can be considered as a part of the initial cycle of a fatigue test under fully reversed loading, thus it is possible to find the stress amplitude related to the fatigue limit by monitoring the surface temperature changes during the static test [65]. It is worth pointing out that this method is inspired by the work by Bottani and Caglioti [129] in some way, and it is mostly based on the work by Plekhov and Naimark [52] and Risitano et al. [130].

In another work, Risitano et al. [53] showed that the method is dependent on the stress rate applied during the tensile test. However, this dependency does not affect the results achieved in terms of fatigue limit. The method can be performed even with a limited number of specimens and in a short amount of time [32, 131-133]. Of course, in order to make robust the estimation of the fatigue limit, it is advisable to test at least five samples.

# PROCEDURE, TYPICAL SETUP AND EQUIPMENT USED FOR RAPID FATIGUE TESTS

## Experimental setup

The experimental setup involves generally an infrared camera and a few controls managed by a computer, Fig. 22. Tests are carried out with a mechanical excitation source provided by a servo-hydraulic testing machine with a suitable load cell capacity, in a room with controlled temperature. Samples should be sized based on the available standards [134] and typically have a dog-bone or hourglass shapes.

The testing procedure includes a sequence of loading blocks of equal duration in terms of loading cycles and with fixed values for loading frequency and stress ratio [45], up to the material failure. The sequence of loading blocks is characterized by an increased mean stress, so that the procedure is called stepwise loading, Fig. 23.

FIGURE 22 Experimental setup for the rapid fatigue test

FIGURE 23 A schematic of stepwise loading

As just said, all blocks contain a specific number of cycles and at the end of each block the stress is increased until the material fails. For the first block, it is suggested that the maximum stress should be 20-30% of the ultimate tensile strength of the material to ensure enough data below the fatigue limit [135]. The stress amplitude increment between each block can be variable and should be set such that the total test time is reasonable and the number of points around the fatigue limit is sufficient [113].

During each block, thermographic acquisitions are performed for a predefined time period and sampling frequency. Of course, first and foremost, the quality of the thermal acquisition depends on the camera specifications and settings (i.e., cooled or uncooled, the frame rate, the integration time and the temperature range).

Generally, the Thermographic method [45], requires a continuous thermal sequence acquisition that can be carried out using an uncooled micro-bolometer camera. A cooled camera is, on the other hand, needed if the purpose of the tests is extracting harmonic components of the temperature where high performances (frame rate) are required in order to properly reconstruct the thermal signal. In this latter case, thermal sequences can be acquired at fixed period of the tests. Of course, if the two types of IR detectors are used in combination [41, 42, 45], all the presented approaches can be performed. The interested reader can refer to an interesting study by Deane et al. [136] for a comprehensive comparison between cooled and uncooled cameras.

As can be seen in Fig. 22, a computer collects both the load cell signal as the reference signal that can be used later for the noise rejection process, and the thermographic signal. Next, a software calculates temperature from the infrared signal and shows it in the form of colorful temperature maps.

Key factors which can make big differences in measurement accuracy are classified into three groups [137]. The first group is operational factors which are related to the available information and experiences about the test conditions and samples. The use of skilled thermographers can help to minimize it and provides better thermal images from the region of interest. Technical factors are in the second group, including the emissivity of the object under investigation and the distance between camera and object. The emissivity is considered an effective parameter in measurement. For this issue, samples are usually covered by a layer of black paint with an appropriate thickness to increase their emissivity and to avoid reflections caused by heat sources located near the samples during the test. The final group contains environmental factors like ambient air temperature, humidity, and convention. To minimize these effects, samples can be also enclosed in an insulating chamber if it is possible [45]. Furthermore, putting a dummy-unloaded specimen made of the same tested material as a black body inside the insulated chamber provides a temperature reference [60].

Table 1 outlines the necessary experimental conditions to obtain various thermal indices. It is worth noting that the experimental setup required for obtaining the thermal indices is similar to what was previously explained, and only specific requirements for each index are presented below.

Table 1 Experimental requirements for the acquisition of different thermal indices

| Requirements |  |  | Thermal indices |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | 1 | 2 | 3 | 4 | 5 | 6 |
|  |  |  | Mean temperature increase | Initial slope of the temperature | Thermoelastic phase | First amplitude harmonic | Second amplitude harmonic | Specific heat loss |
| 1 | IR Camera | Uncooled camera | X | X |  |  |  | X |
|  |  | Cooled camera |  |  | X | X | X |  |
| 2 | High frame rate |  |  |  | X | X | X |  |
| 3 | High loading frequency |  |  |  |  | X |  |  |
| 4 | Dummy specimen |  | X | X |  |  |  |  |
| 5 | Insulating chamber |  | X | X | X | X | X | X |
| 6 | Thermal acquisition type | Continuous | X |  |  |  |  |  |
|  |  | Discrete |  | X | X | X | X | X |

As can be seen, the first consideration refers to the use of an appropriate IR camera to acquire the data suitable for obtaining the specific thermal index. In contrast to the mean temperature related indices (i.e., indices 1, 2 and 6 or mean temperature increase, the initial slope of the temperature and specific heat loss, respectively) which require a typical low-cost uncooled camera, acquisition of harmonic components (indices 3, 4 and 5 or thermoelastic phase, first amplitude harmonic and second amplitude harmonic, correspondingly) need a high-performance uncooled camera [23, 24, 57, 60, 137].

The second row of Table 1 regards the sample rate used for acquiring the thermal sequence. For thermal indices 3 to 5, on contrary to indices 1, 2 and 6, a higher frame rate is necessary because the temperature signal should be reconstructed appropriately, which is crucial for accurately obtaining the aforementioned indices [30, 36, 51].

In addition, for the first harmonic amplitude acquisition, the test should be performed with a high loading frequency, to guarantee the adiabatic condition in the first steps of loading and then observe the loss of linearity due to the damage [20, 138, 139].

From the fourth row of Table 1, a dummy pristine sample should be included when the first two indices are chosen to eliminate the environmental temperature effect from the mean surface temperature of the sample [60]. For all indices, the use of an insulating chamber is recommended to reduce the influence of environmental factors mentioned before [140, 141].

Moreover, the last consideration is the way each index should be captured. As shown in the last row of Table 1, except the mean temperature index which needs to be acquired for the whole of the temperature trend, the other indices can be captured in discrete ways considering suitable time windows during the test [21, 27, 36, 42, 49].

## Thermal signal processing

La Rosa and Risitano [42] and Luong [41] were the first ones who performed signal processing on the mean temperature acquired from the surface of the specimen by the thermography technique. The process was subtracting the environmental temperature from the mean temperature.

Another approach involves the assessment of harmonic components of a thermal signal in terms of amplitudes and phases, as proposed by Krapez et al. [30]. In effect, Krapez was the first one who investigated the thermal signal deeply by examining the harmonic components of the temperature signal. A particular signal demodulation procedure was used to extract the first two Fourier components and the mean temperature rise of some stainless steel and aluminum. They found experimentally that for stress amplitude roughly close to the fatigue limit, three phenomena occur: (i) the mean temperature rises considerably; (ii) the slope of the thermoelastic curve (i.e., the curve of the temperature component at the frequency of loading (f) – stress amplitude) changes sharply; and (iii) a temperature component at 2f appears. Because this procedure needs a reference signal (load or strain) for processing the temperature field via the Fast Fourier Transform (FFT), it is called Lock-in [92]. With lock-in thermography, all of them can be acquired [50]. Therefore, they modeled the temperature as follows:

| Tt=T0+∆Tft+T1sinωt+φ1+T2sinωt+φ2 | (12) |
| --- | --- |

where f is the loading frequency, T0 is the temperature level at the beginning, ∆T is the mean rise of the temperature per cycle, T1, φ1, T2, φ2 are the amplitudes and phases of the first and second Fourier components, respectively. A schematic presentation of thermal signal processing is shown in Fig. 24. Noted that the above model can also be implemented in the least square method for thermal signal reconstruction [30]. To improve the signal to noise ratio, the temperature maps in the central part of the sample or a region with a particular thermal behavior were averaged. It should be noted that in contrast to Risitano’s method which is based on the mean temperature, analyzing the first order and higher order harmonics of the temperature signal are based on the amplitude and phase. Therefore, thermal cameras with higher frame rates are necessary [55, 92].

As explained by De Finis et al. [36, 51], T1 shows the stress field on the surface of the sample which corresponds to the signal variation or thermoelastic effect, while T2 is proportional to the energy of intrinsic dissipation. ϕ can be related to various factors like losing the adiabatic condition, plastic deformation, damage and surface treatment. The change of these parameters with respect to the stress amplitude was used to probe into the thermoelastic and plastic behavior of the material, to estimate the fatigue limit [36, 51], the fatigue behavior of materials [142] especially with high diffusive behavior like aluminum [135].

FIGURE 24 From the thermographic signal to temperature components acquisition

# METHODS FOR RAPID ESTIMATING OF THE FATIGUE LIMIT

In the present section, the focus is on the well-established methods used for estimating the fatigue limit in a rapid way. By starting from the pioneer method, a roundup of recent advances in the field is presented. In fact, there are only a few methods for fatigue limit estimation as follows: Thermographic Method by Luong-Risitano’s or referred also so as Luong’s method” [42, 49], “Iterative method” by Cura` et al. [54], “Threshold method” by De Finis et al. [45] and “Thermoelastic point inversion” by Risitano and Risitano [65].

## Luong-Risitano’s method

As mentioned before, the stabilization temperature is monitored during the fatigue test. By plotting the curves of the stabilized temperature or the initial thermal gradient against the stress magnitude (see Fig. 7), La Rosa and Risitano [42] expressed that the fatigue limit might be estimated as the intercept of the curve on the x-axis. An interesting point about this method is that since the initial temperature increase lasts few cycles on the stabilization temperature, the process is done in a very small number of cycles (generally 10% of the entire lifespan) thus it is possible to use the same specimen for different levels of loading. With this limited number of cycles, the cumulative damage to the specimen is considered negligible [27, 29].

FIGURE 25 Graphical determination of the fatigue limit of a steel by Luong [49]

Furthermore, as La Rosa and Risitano mentioned [42], only three specimens are sufficient because the data show very limited scattering. As shown in Fig. 25, through plotting the temperature related to high dissipation (observing from the surface of the sample) with stress level, Loung noticed a breakpoint (i.e. a point with sharp slope change) which can be used for fatigue life prediction [41, 49].

## Iterative method

Cura`et al. [54], proposed another rapid method based on the stabilization temperature for determination of the fatigue limit of materials (mild steel Fe 510 in their study) and components based on the Luong approach [41, 49]. As shown in Fig. 26, first, the method considered a trial stress magnitude to separate the thermal data into two groups, below and above the stress value, respectively. Next, two straight lines interpolating each group of data were fitted in temperature difference and stress amplitude space, and the intersection of these two lines was recorded as a trial fatigue limit. If the difference between trial stress and estimated fatigue limit is positive, the next trial stress must be selected lower than the first one, and vice versa. The process of imposing a trial stress and finding the trial fatigue limit was continued via an iteration method until the difference between them was below a predefined value, in this condition the trial stress was shown to be a good estimation of the fatigue limit. On the contrary, in Luong’s method, there is not any trial-and-error procedure; after finding the first intersection point, its corresponding stress value was reported as the fatigue limit. Therefore, the accuracy of the method is highly dependent on the chosen trial stress.

FIGURE 26 Schematic representation of Cura` et al. method

As mentioned before, Crupi [37] proposed a non-linear relationship between stabilized temperature increment (∆Tstabilized) and stress amplitude (σa). To predict the fatigue limit, a fitting was applied on all data pairs (∆Tstabilized, σa2) using least-squared and by extrapolating the regression line down to zero at the σa2 - axis. It is worth noting that other relations as the same as the above power function can also be found in the literature but with different exponents [42, 143-146].

## Threshold method

By removing the effects of the environment and loading machine on temperature from measured surface temperature, De Finis et al. [45] approximated the temperature change due to the damage through a linear function of stress amplitude with two constants which could be identified in the first loading steps, by fitting a line to the experimental data, and used as known values for the next steps. As shown in Fig. 27 b, they showed that when the “residual” or ∆Tmax_r, the difference between the maximum temperature change (or steady state temperature) acquired from the surface by IR camera and the linear function, exceeds a threshold value, fatigue failure is likely to happen. The threshold value was defined as six times the standard deviation of residuals for the first five experimental data (∆Th_6σ). Moreover, as shown in Fig. 27b, in contrast to Luong’s method [49] in Fig. 27a, it is not necessary to continue the test up to the failure to evaluate the fatigue limit [45]. The Threshold method determines the transition that occurs in the behavior of the material.

(a)

(b)

FIGURE 27 Comparison between (a) Luong’s method and (b) Threshold method for ASTM A 182 grade F6NM [45]

## Thermoelastic point inversion in tensile test

According to the work by Risitano and Risitano [65], if the temperature curve is added to the typical stress–strain curve (see Fig. 28), it will be feasible to find a limit temperature that shows the beginning of the nonlinearity of the temperature curve and the corresponding stress value can be regarded as a good estimation of the fatigue limit. From Fig. 28, the temperature evolution is characterized by three zones: (I) an approximately linear decrease at the beginning because of the thermoelastic effect, (II) the advent of the non-linearity due to the conversion of mechanical energy to heat (i.e., micro-plastic deformation initiation) and reaching a minimum temperature value; and (III) rising to the material failure.

FIGURE 28 Fatigue limit prediction from tensile test

# DISSCUSSION AND OPEN POINTS

In the present section, a discussion on the methods and still open points is presented. In Table 2, to resume all the parameters adopted in the literature for estimating fatigue limit are proposed. Referring to each parameter, pioneer and relevant works have been indicated in addition to the procedures of each parameter. It is worth mentioning that either temperature or energy-based parameters are suitable to be implemented in the procedures presented in the previous section to estimate the fatigue limit.

Table 2 A summary of fatigue indicators and specific implementation

| Method | Index | Author(s) | Year | Procedures | Fatigue limit estimation procedure |
| --- | --- | --- | --- | --- | --- |
| Direct temperature assessment | Mean temperature increase | La Rosa & Risitano [42, 43] | 1983& 2000 | The first usage of thermography on the fatigue using stabilization temperature for fatigue limit estimation; slope of Tstabilized-σa curve that could be associated with the fatigue limit. | Luong-Risitano’s method |
|  |  | Luong [41] | 1995 | Estimating the intrinsic dissipation from the mean temperature; a sharp change in the dissipation-stress amplitude curve can be related to the fatigue limit. |  |
|  |  | Cura` et al. [54] | 2005 | The method is also used as a basic procedure for other methods based on other indices; using the mean temperature; Considering a trial fatigue limit and applying stress below and above it to find thermal data; finding the intersection of two fitted lines on the thermal data and comparing it with trial one, continuing the process until the trial value and the one from intersection of thermal data are almost the same; at the end, updated trial value shows the fatigue limit. | Iterative method |
|  |  | De Finis et al. [45] | 2015 | Filtering out the superficial temperatures; modeling a linear relation between ∆Tstabilized and σa; evaluating the residual of ∆Tstabilized. The first statistically significant value of temperature residuals was used to estimate the fatigue limit. | Threshold method |
|  | Initial slope of the temperature | Khonsari and colleagues [56, 57, 62] | 2012 | Using the slope of the mean temperature evolution; a sharp change of the temperature rise at the beginning and stress amplitude (Rθ-σa) curve is used for fatigue limit estimation. | Luong-Risitano’s method |
| Loss of adiabaticity within the Thermoelastic Stress Analysis framework | Thermoelastic phase analysis | Palumbo & Galietti [60] | 2017 | Observing the phase change of the temperature signal; a sharp point in the ∆φ-σa curve shows the fatigue limit. | Luong-Risitano’s method |
|  | First amplitude harmonic | Krapez et al. [30] | 2000 | Using the loss of linearity of the trend of the first harmonic of thermoelastic signal with stress amplitude used to estimate the fatigue limit. | / |
|  |  | De Finis et al. [36] | 2019 | Using the first amplitude and phase shift of the thermal signal; the sharp change in the slope of either of them with stress amplitude is used for fatigue limit estimation. | Threshold-like method |
| Energetic approaches | Second amplitude harmonics (SAH) | Shiozawa et al. [33] | 2016 | Assessing the dissipated energy q=ρC(∆Td) using temperature change (∆Td); finding a sharp change in q-σa curve as a fatigue limit. | Luong-Risitano’s method |
|  |  | De Finis et al. [24] | 2021 | Using the SAH of temperature to find the relationship between the heat dissipated rate and mechanical energy rate; estimating the fatigue limit with the trend SAH and plastic work. | / |
|  | Specific Heat loss | Meneghetti [23] | 2007 | Finding the heat dissipation based on the cooling rate; drawing dissipated energy per cycle – σa curve to estimate the fatigue limit. | Luong-Risitano’s method |
| Thermoelastic point inversion or minimum temperature in a tensile test |  | Risitano and Risitano [65] | 2013 | Inspiring from temperature gradient due to the advent of the plastic zone in a tensile test; adding a temperature curve to the typical stress–strain curve; finding a point in the curve shows the beginning of the nonlinearity of the temperature and the corresponding stress value was reported as the fatigue limit. | Thermoelastic point inversion method |

## Capabilities of the fatigue indices

In the present section, the capability of the different indexes is also compared with different factors that could compromise the measurement and/or the analysis. Thus, in Table 2 for the sake of simplicity and ease of reading, they are reported in separate columns and numbered as follows:

- Mean temperature increase

- Initial slope of the temperature

- Thermoelastic Phase

- First amplitude harmonic of temperature

- Second amplitude harmonic of temperature

- Specific heat loss

while each factor is reported in different rows.

Referring to the sensitivity to the heat diffusion effect (first row in Table 3), the methods based on the direct measurement of the temperature such as the mean temperature, have problems with materials with high diffusivity. Indeed, the temperature variations intended as the mean temperature variations can be very little and difficult to measure also with high performance equipment (IR cooled cameras), [42, 45, 49, 54]. Indices 6, 3 and 4 based on either the harmonic amplitudes [24, 30, 33, 36, 59] or the phase information [60] can be most accurate for fatigue limit estimation because they involve a post-processing analysis of the thermal data. As explained below, in different studies, this superior performance can be found in comparison with the mean temperature. Kawai et al. [147] studied the performance of the mean temperature and the second amplitude harmonic and clearly claimed that, in contrast to the latter one, the first one should not be used to high stress concentrated part. The reason is the formation of a significant temperature gradient between the region with stress concentration and the surrounding regions. By increasing the load level, this gradient will be larger and consequently, the correlation between load amplitude and the mean temperature will be distorted that affects fatigue limit evaluation [147]. In another work, De Finis et al. [142], showed the effectiveness of the second harmonic amplitude and thermoelastic phase in martensitic stainless steels where the martensitic microstructure leads to stress concentrations during the cyclic load. In addition, in a more recent work by Lepitre et al. [148], a reliable performance of the first amplitude harmonic in fatigue crack detection of steel was shown.

As can be found in the second row of the table, the brittleness of the material is another limitation for fatigue limit prediction by certain indices. The index 6 is the only one with almost insensitive behavior to this problem [60]. As explained by Palumbo and Galietti [60], this sensitivity can be due to the fact that the heat generation and the maximum temperature that can be reached during the test are much lower in the case of brittle materials. In this case, accurate data processing is required to extract the signal from the noise.

Concerning the effect of the environmental conditions as placed in the third row of Table 3, all indices which are based on mean temperature are sensitive to them, but the harmonic components were reported to be less sensitive than the others since they are analyzed in the frequency domain and the environmental factors are almost filtered out [33, 36].

Of course, other factors can influence the above parameters but it will be the same for all considered indices, for example, first and foremost, the inaccuracy associated with the assumption that the temperature of the surface is a representative of what happens through the thickness, the material geometry, loading frequency, loading ratio and the heat conduction produced by the hot oil of the loading machine gripper [118, 149].

Table 3 Sensitivity of different indices to different factors

| Item /factors # | Description of item | Parameters/Indices* |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | 1 | 2 | 3 | 4 | 5 | 6 |
| 1 | Sensitivity to the heat diffusion effect | x | x |  |  | x |  |
| 2 | Sensitivity to the microstructures, i.e., ductility or brittleness | x | x | x | x | x |  |
| 3 | Sensitivity to the environmental condition | x | x | x |  |  | x |

* Indices:

- Mean temperature increase

- Initial slope of the temperature

- Thermoelastic Phase

- First amplitude harmonic of temperature

- Second amplitude harmonic of temperture

- Specific heat loss

In light of the investigation resumed by Table 3, it can be concluded that the presented parameters can be also used in synergy to obtain complementary information for fatigue characterization.

## Uncertainty in the assessment of the thermal fatigue limit

One point that requires careful attention is the uncertainty in the assessment of the fatigue limit, that depends mainly on both the loading table settings and the number of specimens being tested. The only statistical value that is often used to give an idea about the dispersion on the fatigue limit estimation is the standard deviation. Theoretically, with only one specimen being tested, the standard deviation in the evaluation of the fatigue limit would be zero. It is not reasonable and comparable with the statistic (standard deviation) provided by standard test methods e.g., Staircase.

The present section analyses the differences among the methods in terms of precision in the fatigue limit estimation. Four rapid methods for fatigue limit estimation, including (I) Loung-Risitano’s method [42], (II) Iterative method [54] (III) Threshold method [45] and (IV) Thermoelastic point inversion in tensile test [65], are compared to investigate their effectiveness.

Beginning with the accuracy, as can be seen in Table 4, methods (I)-(III) can estimate the fatigue limit very close to the one determined by the Staircase method [42, 45, 54]. It should be noted that the results in this table are taken from the papers in which each method was proposed for the first time. Moreover, as recently proposed by Risitano et al. [53], the estimated fatigue limit using method (IV) is considerably below the traditional Staircase procedure; in other words, it gives a conservative estimation of the fatigue limit [53].

Table 4 Comparison between the fatigue limit obtained from each method with the traditional one

| Material | Method for fatigue limit prediction | Fatigue limit (Mean value) | Difference (%) |
| --- | --- | --- | --- |
| XC55 steel [42] | Staircase | 399 |  |
|  | Luong - Risitano | 375 | 6 |
| Fe 510 steel [54] | Staircase | 203 |  |
|  | Iterative method | 199 | 1.97 |
| 17-4 PH Steel [45] | Staircase | 212.1 |  |
|  | Threshold method | 201.7 | 4.9 |
| Fe360 steel [65] | Staircase | 43.5 |  |
|  | Thermoelastic point inversion | 44 | 1.15 |

Moreover, a summary of different features playing a key role in the effectiveness and applicability of each method is proposed in Table 5.

The first considered feature is related to the accuracy of the fatigue limit prediction. On one hand, the definition of loading blocks is a very influential factor for which inappropriate settings could lead to underestimation/overestimation of the fatigue limit.  As shown in Table 5, the step dimension (load increment from one step to another one and the number of cycles for each block, see Fig. 23) is one of the main parts of the loading blocks definition that should be considered for methods (I) to (III). Furthermore, the number of loading blocks is another part of the above procedure. In this regard and according to the literature [42, 45, 54], method (III) can make predictions using less than 10 loading blocks, unlike methods (I) and (II) which require more; thus, it can be said that it is more time-saving in comparison to methods (I) and (II). Finally, the last part of the definition is the stress level for the first block. Unlike methods (I) and (II), the load of the initial block is clearly mentioned for method (III) [45] which is approximately 30% of the ultimate tensile stress (in terms of maximum stress).

Table 5 Summary of different features of the fatigue limit prediction methods

| Features |  |  |  | Fatigue limit estimation procedure |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | (I) Luong-Risitano | (II) Iterative method | (III) Threshold method | (IV) Thermoelastic point inversion |
| 1 | Factors affecting the accuracy of fatigue limit estimations | Loading block definition | ‘Step dimension’ between two loading blocks | YES | YES | YES | - |
|  |  |  | Minimum number of loading blocks | More than 10 [42] | More than 10 [54] | Below 10 [45] | - |
|  |  |  | Stress of the first loading block | Not specified | Not specified | σmax =30% UTS | - |
|  |  | Number of specimens required |  | Dependence on the definition of loading blocks | Dependence on the definition of loading blocks | Dependence on the definitions of loading blocks | Dependence on the loading rate in the tensile test |
| 2 | Possibility to be done automatically |  |  | NO | YES | NO | NO |
| 3 | Applicability to more than one thermal indices |  |  | YES | - | YES | NO |
| 4 | Analytical expression to evaluate the uncertainty |  |  | NO | NO | NO | NO |

On the other hand, the number of samples that each method needs to estimate the fatigue limit with the desired accuracy is another factor mentioned in Table 5. As can be seen from Table 5, this factor is basically dependent on the mechanical loading blocks definition. In a different way, the method (IV) also relies on the loading rate during the tensile test.

Of course, the least number of samples required for each method affects completely the time and cost of the test. In methods (I)-(III), samples should be under the cyclic loading up to the stabilized temperature for each load block, so only one sample is theoretically needed to find the fatigue limit, since loading is removed before any damage in the sample [42, 45, 118]. However, there are some uncertainties related to the environmental conditions, material microstructure, geometry, etc., which cause statistical scatter in the results from one sample to another [118]. Accounting for this scatter while keeping the test fast, needs at least three samples [42, 118]. So, the estimation of the fatigue limit, theoretically with only one specimen, is useful only for exploratory purposes. In method (II), it can be expected that if the number of points in T-σa is not enough, it will be difficult to fit straight lines to the thermal data [54]. Thus, it can be said that more thermal data seems to be needed in this method than in (I) and (III). Consequently, for more thermal data, more testing time and of course more samples (the more the thermal points, the higher the possibility of damage initiation) might be required. In method (III), the identification of the relation between the temperature increase and stress amplitude and finding the threshold value can be done in the very first loading steps, and the fatigue limit can be estimated as soon as the residual exceeds the threshold value. When this criterion is satisfied, the fatigue limit can be estimated, and no additional loading is required. Theoretically, this method could lead to a new generation of fatigue tests: non-destructive ones. Therefore, it seems that method (III) presents the potentials to be faster than methods (I) and (II) for the fatigue limit prediction.

According to Risitano & Risitano [65], the thermoelastic point inversion method is faster than the methods with cyclic loading, methods (I)-(III). However, due to the dependency on the loading rate of the tensile test as proposed in Table 5, it is necessary to perform the test for some trial stress rates to observe a sharp and clear slope change in the temperature, then continue with more tests and the selected loading rate from the previous step to consider the possible scatter as explained by Foti et al. [32].

- Additionally, according to the second featured in Table 5, among the four mentioned methods, only Method II can predict the fatigue limit automatically. From the third feature, in contrast to methods I and III, method IV can be only applicable with the mean temperature. It should be noted that the Iterative method (method II) has not been applied with indices different from the mean temperature, theoretically, it can be applied also to the other indices (at least on indices 5 and 6, section 6.1).

Finally, as shown in the last row of Table 5, it is important to highlight that the considered methods have a common issue: none of them provide an analytical expression of the uncertainty of the assessed fatigue limit. This means that a correct comparison with traditional methods cannot be performed.

## Fatigue limit prediction in components

Another open point that limits the development of the presented methods and procedures, regards their application to out-of-laboratory case studies such as the in-situ inspections on components undergoing operating loads.

From an operational point of view, the in-situ inspection requires the availability of sufficient space to set up the equipment with good spatial resolution and the possibility to apply a matt black to increase the emissivity on the component. Of course, critical regions of the components must be known as a priori and loading stresses too. In effect, the physical space should be enough to put the equipment (infrared camera and tripod and etc.) in the right places and connect to a computer for the data processing. In addition, the surface thermal emissivity of the area being inspected must be ensured by coating a proper matt black.

A further set of issues arising from the exportation of laboratory techniques to real applications is related to the geometry of components. In fact, in thicker components, the possible presence of the inner heat sources produces a small surface thermal footprint which cannot be easily detected unless a specific post-processing analysis is carried out to separate the weak signal of the heat source from the noise. Otherwise, the determination of the most critical area in components with complex geometry will be an arduous task due to the presence of the heat dissipation in different locations. In this case, however, the finite element models could be supportive to understand the most stressed areas.

In addition to the above problematic situations, the stress history and the actual stress state are unknown a priori, especially for components under operational loads. Therefore, it is not straightforward to relate directly measured thermal data with the stress state and then residual life. Overall, another important consideration, in sight of the analyses made in previous sections, is that before applying a certain method on a specific component with a specific material, all the procedures must be tuned with the base material specimens in the laboratory.

In effect, accounting for the above considerations, the fatigue limit determination of metals at the component level is a big challenge, that is why only two studies were proposed in contrast to tremendous works on flat and cylindrical samples. To date, the first attempt to export experimental procedure on components was proposed by Luong [28, 49] on XC55 steel connecting rods under tension–compression fatigue tests. He showed that the fatigue limit can be found in a few hours instead of several months when using the standard staircase method [28, 49]. In the most recent study by Faria et al. [150], the thermographic method was used for fast prediction of a relatively more complex component, a cast iron crankshaft. The results showed a good correlation between thermographic results and Staircase method data for dog-bone samples taken from the crankshaft counterweights.

# CONCLUSIONS

A comparative review of the methods and procedures based on thermography for the fatigue limit estimation has been performed, identifying their main advantages and drawbacks in each of the steps of the fatigue behavior assessment: from the experimental campaign to data processing and analysis of thermal indices both on laboratory case studies and on in-situ applications.  It can be concluded that:

- the thermal indices related to the specific physical process being analyzed (thermoelastic effect, intrinsic dissipation, non-adiabatic effects...) are effective parameters for studying the damage to the material both from a qualitative and quantitative point of view;

- the link between these processes and the microstructural phenomena related to damage should be further investigated to better understand the meaning of the ‘thermal fatigue limit’;

- an analysis in the frequency domain to study the harmonics of the thermal signal allows obtaining parameters more robust with respect to the damage than the mean temperature;

- all the presented procedures to estimate the thermal fatigue limit are actually rapid and promising however, more efforts must be paid to define a procedure to calculate the uncertainty in the estimation of fatigue limit even from few samples to be comparable with those of standard test methods;

- the application of the presented methods and procedures to in-situ industrial applications is an ongoing topic that requires more efforts.

# ACKNOWLEDGEMENTS

No sources of funding were involved in the completion of this work.

# CONFLICT OF INTERESTS

The authors declare no conflict of interest.

# AUTHOR CONTRIBUTION

Each person who meets the established criteria for authorship is acknowledged as an author, and all authors have adequately engaged in this study to accept public accountability for its content. This encompassing involvement includes active participation in the conceptions, planning, writing, and revision of the manuscript.

# REFERENCES

[1] Heydari A A, Salerno A, Bagherifard S, Carlone P, Parmar H, Astarita A, et al. Thermographic analysis of composite metallization through cold spray. Metals. 2021; 11: 1860.

[2] Shepard S M. Advances in Pulsed Thermography. Proc. SPIE - The International Society for Optical Engineering, Thermosense XXVIII, Orlando, Florida. 2001.

[3] Rajic N. Principal component thermography. Airframes and Engines Division Aeronautical and Maritime Research Laboratory, DSTO-TR-1298. 2002.

[4] Ibarra-Castanedo C, Avdelidis N P, Maldague X P. Thermosense XXVII, International Society for Optics and Photonics. 2005.

[5] Balageas D L, Roche J-M, Leroy F-H, Liu W-M, Gorbach A M. The thermographic signal reconstruction method: A powerful tool for the enhancement of transient thermographic images. Biocybernetics and Biomedical Engineering. 2015; 35: 1-9.

[6] Angioni S L, Ciampa F, Pinto F, Scarselli G, Almond D P, Meo M. An analytical model for defect depth estimation using pulsed thermography. Experimental Mechanics. 2016; 56: 1111-1122.

[7] Maierhofer C, Röllig M, Krankenhagen R, Myrach P. Comparison of quantitative defect characterization using pulse-phase and lock-in thermography. Applied Optics. 2016; 55: D76-D86.

[8] D’Accardi E, Krankenhagen R, Ulbricht A, Pelkner M, Pohl R, Palumbo D, et al. Capability to detect and localize typical defects of laser powder bed fusion (L-PBF) process: an experimental investigation with different non-destructive techniques. Progress in Additive Manufacturing. 2022; 7: 1239-1256.

[9] D’Accardi E, Palumbo D, Galietti U. Experimental procedure to assess depth and size of defects with pulsed thermography. Journal of Nondestructive Evaluation. 2022; 41: 41.

[10] Dell'Avvocato G, Gohlke D, Palumbo D, Krankenhagen R, Galietti U. Quantitative evaluation of the welded area in resistance projection welded (RPW) thin joints by pulsed laser thermography. SPIE; 2022.

[11] Rani A, Sharma A, Mulaveesala R. In: Mandayam S, Sagar S P. eds, Advances in Non Destructive Evaluation. Singapore: Springer Nature; 2022: 73-82.

[12] Dell’Avvocato G, Palumbo D, Galietti U. A non-destructive thermographic procedure for the evaluation of heat treatment in Usibor®1500 through the thermal diffusivity measurement. NDT & E International. 2023; 133: 102748.

[13] Montinaro N, Cerniglia D, Pitarresi G. Evaluation of vertical fatigue cracks by means of flying laser thermography. Journal of Nondestructive Evaluation. 2019; 38: 48.

[14] Pitarresi G, Cappello R, Capraro A, Pinto V, Badagliacco D, Valenza A. In: Rizzo P, Milazzo A, eds. European Workshop on Structural Health Monitoring. Germany: Springer International Publishing; 2023: 610-618.

[15] Pitarresi G, Cappello R. Evaluation of crack-closure by second harmonic thermoelastic stress analysis. International Journal of Fatigue. 2022; 164: 107116.

[16] Jiménez-Fortunato I, Bull D J, Thomsen O T, Dulieu-Barton J M. Quantitative microbolometer-based thermoelastic stress analysis. Optics and Lasers in Engineering. 2023; 160: 107276.

[17] Dulieu-Barton J. Thermoelastic stress analysis. Optical Methods For Solid Mechanics, John Wiley & Sons. 2012; 345-366.

[18] Harwood N, Cummings W M. Thermoelastic stress analysis. USA: National Engineering Laboratory, Adam Hilger; 1991.

[19] Palumbo D, De Finis R, Galietti U. Thermoelastic stress analysis as a method for the quantitative non-destructive evaluation of bonded CFRP T-joints. NDT & E International. 2021; 124: 102526.

[20] Wang W J, Dulieu-Barton J M, Li Q. Assessment of non-adiabatic behaviour in thermoelastic stress analysis of small scale components. Experimental Mechanics. 2010; 50: 449-461.

[21] Cappello R, Meneghetti G, Ricotta M, Pitarresi G. On the correlation of temperature harmonic content with energy dissipation in C45 steel samples under fatigue loading. Mechanics of Materials. 2022; 168: 104271.

[22] Stanley P. Beginnings and early development of thermoelastic stress analysis. Strain. 2008; 44: 285-297.

[23] Meneghetti G. Analysis of the fatigue strength of a stainless steel based on the energy dissipation. International Journal of Fatigue. 2007; 29: 81-94.

[24] De Finis R, Palumbo D, Galietti U. On the relationship between mechanical energy rate and heat dissipated rate during fatigue for a C45 steel depending on stress ratio. Fatigue & Fracture of Engineering Materials & Structures. 2021; 44: 2781-2799.

[25] Feltner C E, Morrow J D. Microplastic strain hysteresis energy as a criterion for fatigue fracture. Journal of Basic Engineering. 1961; 83: 15-22.

[26] Chrysochoos A, Louche H. An infrared image processing to analyse the calorific effects accompanying strain localisation. International Journal of Engineering Science. 2000; 38: 1759-1788.

[27] Rosa G L, Risitano A. Application of a new methodology to determine the fatigue limit using thermal infrared techniques. 17th Symposium on Experimental Mechanics. 1996; 498–503.

[28] Luong M P. Infrared thermography of fatigue in metals. SPIE; 1992.

[29] Geraci A, Rosa G L, Risitano A. Influence of frequency and cumulative damage on the determination of fatigue limit of materials using the thermal infrared methodology. 15th Symposium on Experimental Mechanics of Solids. 1992; 63–65.

[30] Krapez J C, Pacou D, Gardette G. Lock-in thermography and fatigue limit of metals. Quantitative InfraRed Thermography. 2000.

[31] Bremont P, Potet P D. Démodulation synchrone des images thermiques. Application à l’analyse expérimentale des structures. Journée de la Société Française des Thermiciens, Thermographie Quantitative. 1994.

[32] Foti P, Santonocito D, Ferro P, Risitano G, Berto F. Determination of fatigue limit by static thermographic method and classic thermographic method on notched specimens. Procedia Structural Integrity. 2020; 26: 166-174.

[33] Shiozawa D, Inagawa T, Washio T, Sakagami T. Fatigue limit estimation of stainless steels with new dissipated energy data analysis. Procedia Structural Integrity. 2016; 2: 2091-2096.

[34] Curti G, Rosa G L, Orlando M, Risitano A. Analisi tramite infrarosso termico della temperatura limite in prove di fatica. XIV Convegno Nazionale AIAS. 1986.

[35] Colombo C, Fumagalli G, Bolzoni F, Gobbi G, Vergani L. Fatigue behavior of hydrogen pre-charged low alloy Cr–Mo steel. International Journal of Fatigue. 2016; 83: 2-9.

[36] De Finis R, Palumbo D, Galietti U. A multianalysis thermography-based approach for fatigue and damage investigations of ASTM A182 F6NM steel at two stress ratios. Fatigue & Fracture of Engineering Materials & Structures. 2019; 42: 267-283.

[37] Crupi V. An unifying approach to assess the structural strength. International Journal of Fatigue. 2008; 30: 1150-1159.

[38] Boulanger T, Chrysochoos A, Mabru C, Galtier A. Calorimetric analysis of dissipative and thermoelastic effects associated with the fatigue behavior of steels. International Journal of Fatigue. 2004; 26: 221-229.

[39] Amiri M, Khonsari M M. Nondestructive estimation of remaining fatigue life: thermography technique. Journal of Failure Analysis and Prevention. 2012; 12: 683-688.

[40] Rigon D, Berto F, Meneghetti G. Estimating the multiaxial fatigue behaviour of C45 steel specimens by using the energy dissipation. International Journal of Fatigue. 2021; 151: 106381.

[41] Luong M P. Infrared thermographic scanning of fatigue in metals. Nuclear Engineering and Design. 1995; 158: 363-376.

[42] La Rosa G, Risitano A. Thermographic methodology for rapid determination of the fatigue limit of materials and mechanical components. International Journal of Fatigue. 2000; 22: 65-73.

[43] Geraci A, Rosa G L, Risitano A. L’infrarosso termico nelle applicazioni meccaniche. CRES Symposium. 1983.

[44] Catalbiano T, Geraci A, Orlando M. Analisi tramite infrarosso termico di provini sollecitati a fatica. Il progettista industriale. 1984.

[45] De Finis R, Palumbo D, Ancona F, Galietti U. Fatigue limit evaluation of various martensitic stainless steels with new robust thermographic data analysis. International Journal of Fatigue. 2015; 74: 88-96.

[46] Munier R, Doudard C, Calloch S, Weber B. Determination of high cycle fatigue properties of a wide range of steel sheet grades from self-heating measurements. International Journal of Fatigue. 2014; 63: 46-61.

[47] Meyendorf N G, Rösner H, Kramb V, Sathish S. Thermo-acoustic fatigue characterization. Ultrasonics. 2002; 40: 427-434.

[48] Gough J. A description of a property of Caoutchouc, or India rubber with some reflections on the cause of the elasticity of this substance. Memoirs of the Literary and Philosophical Society of Manchester. 1805; 1: 288–295.

[49] Luong M P. Fatigue limit evaluation of metals using an infrared thermographic technique. Mechanics of Materials. 1998; 28: 155-163.

[50] Ranc N, Wagner D, Paris P C. Study of thermal effects associated with crack propagation during very high cycle fatigue tests. Acta Materialia. 2008; 56: 4012-4021.

[51] De Finis R, Palumbo D, Galietti U. Mechanical behaviour of stainless steels under dynamic loading: an investigation with thermal methods. Journal of Imaging. 2016; 2.

[52] Plekhov O A, Naimark O B. Theoretical and experimental study of energy dissipation in the course of strain localization in iron. Journal of Applied Mechanics and Technical Physics. 2009; 50: 127-136.

[53] Risitano G, Guglielmino E, Santonocito D. Rapid energetic approaches for the fatigue limit assessment in a medium carbon steel. Procedia Structural Integrity. 2021; 33: 748-756.

[54] Curà F, Curti G, Sesana R. A new iteration method for the thermographic determination of fatigue limit in steels. International Journal of Fatigue. 2005; 27: 453-459.

[55] Colombo C, Vergani L. Thermographic applications for the rapid estimation of fatigue limit. Procedia Structural Integrity. 2019; 24: 658-666.

[56] Amiri M, Khonsari M M. Life prediction of metals undergoing fatigue load based on temperature evolution. Materials Science and Engineering: A. 2010; 527: 1555-1559.

[57] Amiri M, Khonsari M M. Rapid determination of fatigue failure based on temperature evolution: Fully reversed bending load. International Journal of Fatigue. 2010; 32: 382-389.

[58] Enke N F, Sandor B I. Cyclic plasticity analysis by differential infrared thermography. Proceedings of the VII International Congress on Experimental Mechanics. 1988; 830–835.

[59] Krapez J-C, Pacou D, Bertin C. Application of lock-in thermography to rapid evaluation of fatigue limit in metals. Workshop on Advanced Infrared Technology and Applications. 1999.

[60] Palumbo D, Galietti U. Thermoelastic Phase Analysis (TPA): a new method for fatigue behaviour analysis of steels. Fatigue & Fracture of Engineering Materials & Structures. 2017; 40: 523-534.

[61] De Finis R. Application of thermal methods based on infrared thermography for the mechanical characterisation of materials, PhD thesis. Italy: Polytechnic University of Bari; 2017.

[62] Mehdizadeh M, Khonsari M M. On the application of fracture fatigue entropy to variable frequency and loading amplitude. Theoretical and Applied Fracture Mechanics. 2018; 98: 30-37.

[63] Galietti U, Palumbo D, Finis R D, Ancona F. Fatigue limit evaluation of martensitic steels with thermal methods. Conference QIRT 2014. 2014.

[64] Risitano A, Fargione G, Guglielmino E. Definition of the linearity loss of the surface temperature in static tensile tests. Frattura ed Integrità Strutturale. 2014; 8: pages 201-210.

[65] Risitano A, Risitano G. Determining fatigue limits with thermal analysis of static traction tests. Fatigue & Fracture of Engineering Materials & Structures. 2013; 36: 631-639.

[66] Rosner H, Sathish S, Meyendorf N. Thermographic characterisation of fatigue. In: Thompson D, Chimenti D, eds. Review of progress in QNDE. USA: Springer; 2001.

[67] Audenino A L, Zanetti E M, Calderale P M. Assessment of internal damping in uniaxially stressed metals: exponential and autoregressive methods. Journal of Dynamic Systems, Measurement, and Control. 1998; 120: 177-184.

[68] Mughrabi H. Dislocations in Fatigue. UK: Institute of Metals; 1985.

[69] Lazan B J. Effect of damping constants and stress distribution on the resonance response of members. Journal of Applied Mechanics. 1953; 20: 201-209.

[70] Meneghetti G, Ricotta M. Estimating the intrinsic dissipation using the second harmonic of the temperature signal in tension-compression fatigue. Part II: Experiments. Fatigue & Fracture of Engineering Materials & Structures. 2021; 44: 2153-2167.

[71] Ewing J A, Rosenhain W. Experiments in micro-metallurgy:- effects of strain. Preliminary notice. Proceedings of the Royal Society of London. 1900; 65: 85-90.

[72] Suresh S. Fatigue of materials. UK: Cambridge solid state science series; 1992.

[73] Maquin F, Pierron F. Heat dissipation measurements in low stress cyclic loading of metallic materials: From internal friction to micro-plasticity. Mechanics of Materials. 2009; 41: 928-942.

[74] Scott-Emuakpor O, George T, Cross C, Shen M-H H. Hysteresis-loop representation for strain energy calculation and fatigue assessment. The Journal of Strain Analysis for Engineering Design. 2010; 45: 275-282.

[75] Pedersen M M. Introduction to metal fatigue. Denmark: Aarhus University; 2018.

[76] Stephens R I, Fatemi A, Stephens R R, Fuchs H O. Metal fatigue in engineering. USA: Wiley; 2000.

[77] Murakami Y. Metal fatigue: effects of small defects and nonmetallic inclusions. Japan: Academic Press; 2019.

[78] Mareau C. Micromechanical modeling of self-heating and microplasticity in steels under cyclic loading, PhD thesis. France: Arts et Métiers Paris Tech; 2007.

[79] Jordan E H. Notch-root plastic response by temperature measurement. Experimental Mechanics. 1985; 25: 24-31.

[80] Nourian-Avval A, Khonsari M M. Rapid prediction of fatigue life based on thermodynamic entropy generation. International Journal of Fatigue. 2021; 145: 106105.

[81] Sakai T, Nakagawa A, Oguma N, Nakamura Y, Ueno A, Kikuchi S, et al. A review on fatigue fracture modes of structural metallic materials in very high cycle regime. International Journal of Fatigue. 2016; 93: 339-351.

[82] Fancher D R. Stress-strain hysteresis loops and rheological epicycles, PhD thesis. USA: The University of Arizona; 1943.

[83] Bauschinger J. Ueber die veranderungen der elastizitatsgrenze und der festigkeit des eisens und stahls durch strecken, quetschen, erwarmen abkiihlen und durch oftmals wiederholte belastung. Mitt: Mech-Tech Lab., XIII Miinchen. 1986;

[84] Chrysochoos A, Huon V, Jourdan F, Muracciole J-M, Peyroux R, Wattrisse B. Use of full-field digital image correlation and infrared thermography measurements for the thermomechanical analysis of material behaviour. Strain. 2010; 46: 117-130.

[85] Ewing J A, Humfrey J C W. VI. The fracture of metals under repeated alternations of stress. Philosophical Transactions of the Royal Society of London. Series A, Containing Papers of a Mathematical or Physical Character. 1903; 200: 241-250.

[86] Doudard C, Calloch S, Cugy P, Galtier A, Hild F. A probabilistic two-scale model for high-cycle fatigue life predictions. Fatigue & Fracture of Engineering Materials & Structures. 2005; 28: 279-288.

[87] Schijve J. Fatigue of Structures and Materials. Netherlands: Springer Dordrecht; 2009.

[88] Srivatsan S, Sudarshan T S. Mechanisms of fatigue crack initiation in metals: role of aqueous environments. Journal of Materials Science. 1988; 23: 1521-1533.

[89] Connesson N, Maquin F, Pierron F. Experimental energy balance during the first cycles of cyclically loaded specimens under the conventional yield stress. Experimental Mechanics. 2011; 51: 23-44.

[90] Naderi M, Khonsari M M. An experimental approach to low-cycle fatigue damage based on thermodynamic entropy. International Journal of Solids and Structures. 2010; 47: 875-880.

[91] Stromeyer C E, Dalby W E. The determination of fatigue limits under alternating stress conditions. Proceedings of the Royal Society of London. Series A, Containing Papers of a Mathematical and Physical Character. 1914; 90: 411-425.

[92] Colombo C, Sansone M, Patriarca L, Vergani L. Rapid estimation of fatigue limit for C45 steel by thermography and digital image correlation. The Journal of Strain Analysis for Engineering Design. 2021; 56: 478-491.

[93] Wang X G, Crupi V, Jiang C, Guglielmino E. Quantitative Thermographic Methodology for fatigue life assessment in a multiscale energy dissipation framework. International Journal of Fatigue. 2015; 81: 249-256.

[94] Feng E, Wang X, Jiang C, Crupi V. Quantitative thermographic method for fatigue life prediction under variable amplitude loading. Fatigue & Fracture of Engineering Materials & Structures. 2022; 45: 1199-1212.

[95] Louche H, Chrysochoos A. An infrared image processing to analyse the calorific effects accompanying strain localisation. International Journal of Engineering Science. 2000; 38: 1759-1788.

[96] Aeran A, Vantadori S, Carpinteri A, Siriwardane S C, Scorza D. Novel non-linear relationship to evaluate the critical plane orientation. International Journal of Fatigue. 2019; 124: 537-543.

[97] Huang Y, Li S X, Lin S E, Shih C N. Using the method of infrared sensing for monitoring fatigue process of metals. Materials Evaluation. 1984; 42: 1020-1024.

[98] Botny R, Kaleta J. A method for determining the heat energy of the fatigue process in metals under uniaxial stress: Part 1. Determination of the amount of heat liberated from a fatigue-tested specimen. International Journal of Fatigue. 1986; 8: 29-33.

[99] Liakat M, Khonsari M M. An experimental approach to estimate damage and remaining life of metals under uniaxial fatigue loading. Materials & Design. 2014; 57: 289-297.

[100] Liakat M, Khonsari M M. Rapid estimation of fatigue entropy and toughness in metals. Materials & Design. 2014; 62: 149-157.

[101] Weber W. Ueber die specifische wärme fester körper, insbesondere der metalle. Annalen der Physik. 1830; 96: 177-213.

[102] Thomson W. II. On the dynamical theory of heat, with numerical results deduced from Mr. Joule's equivalent of a thermal unit, and M. Regnault's observations on steam. The London, Edinburgh, and Dublin Philosophical Magazine and Journal of Science. 1852; 4: 8-21.

[103] Wong A K, Sparrow J G, Dunn S A. On the revised theory of the thermoelastic effect. Journal of Physics and Chemistry of Solids. 1988; 49: 395-400.

[104] Pitarresi G, Patterson E A. A review of the general theory of thermoelastic stress analysis. The Journal of Strain Analysis for Engineering Design. 2003; 38.

[105] Wong A K, Jones R, Sparrow J G. Thermoelastic constant or thermoelastic parameter? Journal of Physics and Chemistry of Solids. 1987; 48: 749-753.

[106] Wong A K, Dunn S A, Sparrow J G. Residual stress measurement by means of the thermoelastic effect. Nature. 1988; 332: 613-615.

[107] Sakagami T, Kubo S, Tamura E, Nishimura T. Identification of plastic‐zone based on double frequency lock‐in thermographic temperature measurement. Italian Group of Fracture.  2013.

[108] Galietti U, Palumbo D, Finis R D, Ancona F. Fatigue damage evaluation with new thermal methods. 3rd International Workshop on Advanced Infrared Technology and Applications, 2013.

[109] Dulieu-Barton J M. Introduction to thermoelastic stress analysis. Strain. 1999; 35: 35-39.

[110] Offermann S, Beaudoin J L, Bissieux C, Frick H. Thermoelastic stress analysis under nonadiabatic conditions. Experimental Mechanics. 1997; 37: 409-413.

[111] Jasper T M. LXVII. The value of the energy relation in the testing of ferrous metals at varying ranges of stress and at intermediate and high temperatures. The London, Edinburgh, and Dublin Philosophical Magazine and Journal of Science. 1923; 46: 609-627.

[112] Shiozawa D, Inagawa T, Washio T, Sakagami T. Accuracy improvement in dissipated energy measurement by using phase information. Measurement Science and Technology. 2017; 28: 044004.

[113] Finis R D, Palumbo D, Pirinu A, Saponaro A, Panella F W, Nobile R, et al. Fatigue behaviour assessment of C45 steel by means of energy-based methods. IOP Conference Series: Materials Science and Engineering. 2021.

[114] Meneghetti G, Ricotta M. Estimating the intrinsic dissipation using the second harmonic of the temperature signal in tension-compression fatigue: Part I. Theory. Fatigue & Fracture of Engineering Materials & Structures. 2021; 44: 2168-2185.

[115] Meneghetti G, Ricotta M. Evaluating the heat energy dissipated in a small volume surrounding the tip of a fatigue crack. International Journal of Fatigue. 2016; 92: 605-615.

[116] Meneghetti G, Ricotta M. The heat energy dissipated in the material structural volume to correlate the fatigue crack growth rate in stainless steel specimens. International Journal of Fatigue. 2018; 115: 107-119.

[117] Meneghetti G, Ricotta M. The use of the specific heat loss to analyse the low- and high-cycle fatigue behaviour of plain and notched specimens made of a stainless steel. Engineering Fracture Mechanics. 2012; 81: 2-16.

[118] Ricotta M, Meneghetti G, Atzori B, Risitano G, Risitano A. Comparison of experimental thermal methods for the fatigue limit evaluation of a stainless steel. Metals. 2019; 9: 677.

[119] Rigon D, Ricotta M, Meneghetti G. An analysis of the specific heat loss at the tip of severely notched stainless steel specimens to correlate the fatigue strength. Theoretical and Applied Fracture Mechanics. 2017; 92: 240-251.

[120] Skibicki D, Lipski A, Pejkowski Ł. Evaluation of plastic strain work and multiaxial fatigue life in CuZn37 alloy by means of thermography method and energy-based approaches of Ellyin and Garud. Fatigue & Fracture of Engineering Materials & Structures. 2018; 41: 2541-2556.

[121] Naderi M, Amiri M, Khonsari M M. On the thermodynamic entropy of fatigue fracture. Proceedings of the Royal Society A: Mathematical, Physical and Engineering Sciences. 2010; 466: 423-438.

[122] Marrow J D. Cyclic plastic strain energy and fatigue of metals. STM STP 378. 1995; 45-84.

[123] Naderi M, Khonsari M. Real-time fatigue life monitoring based on thermodynamic entropy. Structural Health Monitoring. 2011; 10: 189-197.

[124] Jang J Y, Khonsari M M. On the evaluation of fracture fatigue entropy. Theoretical and Applied Fracture Mechanics. 2018; 96: 351-361.

[125] Liakat M, Khonsari M M. On the anelasticity and fatigue fracture entropy in high-cycle metal fatigue. Materials & Design. 2015; 82: 18-27.

[126] Haghshenas A, Jang J Y, Khonsari M M. On the intrinsic dissipation and fracture fatigue entropy of metals. Mechanics of Materials. 2021; 155: 103734.

[127] Guo Q, Guo X, Fan J, Syed R, Wu C. An energy method for rapid evaluation of high-cycle fatigue parameters based on intrinsic dissipation. International Journal of Fatigue. 2015; 80: 136-144.

[128] Mehdizadeh M, Khonsari M M. On the role of internal friction in low-and high-cycle fatigue. International Journal of Fatigue. 2018; 114: 159-166.

[129] Bottani C E, Caglioti G. Thermoelastic instabilities in metals. Physica Scripta. 1982; T1: 65-70.

[130] Risitano A, Corallo D, Risitano G, Sirugo A. Determinazione del limite di fatica mediante prove quasistatiche. Proceedings XXXIX AIAS National Conference. 2010.

[131] Foti P, Risitano G, Berto F, Santonocito D. Evaluation of the energetic release during tensile tests in notched specimens by means of experimental and numerical techniques. IOP Conference Series: Materials Science and Engineering. 2021; 1038: 012038.

[132] Risitano G, Santonocito D. Experimental and numerical assessment of the end of the thermoelastic effect during static traction test. Procedia Structural Integrity. 2020; 28: 1449-1457.

[133] Corigliano P, Cucinotta F, Guglielmino E, Risitano G, Santonocito D. Fatigue assessment of a marine structural steel and comparison with thermographic method and static thermographic method. Fatigue & Fracture of Engineering Materials & Structures. 2020; 43: 734-743.

[134] ASTM E 466, Standard practice for conducting force controlled constant amplitude axial fatigue tests of metallic materials. ASM International. 1996.

[135] De Finis R, Palumbo D, Serio L M, De Filippis L A C, Galietti U. Correlation between thermal behaviour of AA5754-H111 during fatigue loading and fatigue strength at fixed number of cycles. Materials. 2018; 11: 719.

[136] Deane S, Avdelidis N P, Ibarra-Castanedo C, Zhang H, Yazdani Nezhad H, Williamson A A, et al. Comparison of Cooled and Uncooled IR Sensors by Means of Signal-to-Noise Ratio for NDT Diagnostics of Aerospace Grade Composites. Sensors. 2020; 20.

[137] Bagavathiappan S, Lahiri B B, Saravanan T, Philip J, Jayakumar T. Infrared thermography for condition monitoring – A review. Infrared Physics & Technology. 2013; 60: 35-55.

[138] Chrysochoos A, Berthel B, Latourte F, Pagano S, Wattrisse B, Weber B. Local energy approach to steel fatigue. Strain. 2008; 44: 327-334.

[139] Morabito A E, Chrysochoos A, Dattoma V, Galietti U. Analysis of heat sources accompanying the fatigue of 2024 T3 aluminium alloys. International Journal of Fatigue. 2007; 29: 977-984.

[140] De Finis R, Palumbo D, da Silva M M, Galietti U. Is the temperature plateau of a self-heating test a robust parameter to investigate the fatigue limit of steels with thermography?. Fatigue & Fracture of Engineering Materials & Structures. 2018; 41: 917-934.

[141] Finis R D, Palumbo D, Pirinu A, Saponaro A, Panella F W, Nobile R, et al. Fatigue behaviour assessment of C45 steel by means of energy-based methods. IOP Conference Series: Materials Science and Engineering. 2021; 1038: 012015.

[142] De Finis R, Palumbo D, Ancona F, Galietti U. In: Quinn S, Balandraud X, eds. Residual Stress, Thermomechanics & Infrared Imaging, Hybrid Techniques and Inverse Problems. Germany: Springer International Publishing. 2017; 1-8.

[143] Crupi V, Guglielmino E, Maestro M, Marinò A. Fatigue analysis of butt welded AH36 steel joints: thermographic method and design S–N curve. Marine Structures. 2009; 22: 373-386.

[144] Wang X G, Crupi V, Guo X L, Zhao Y G. Quantitative Thermographic Methodology for fatigue assessment and stress measurement. International Journal of Fatigue. 2010; 32: 1970-1976.

[145] Fargione G, Geraci A, La Rosa G, Risitano A. Rapid determination of the fatigue curve by the thermographic method. International Journal of Fatigue. 2002; 24: 11-19.

[146] Wang X G, Crupi V, Guo X L, Guglielmino E. A thermography-based approach for structural analysis and fatigue evaluation. Proceedings of the Institution of Mechanical Engineers, Part C: Journal of Mechanical Engineering Science. 2011; 226: 1173-1185.

[147] Kawai R, Yoshikawa T, Kurokawa Y, Irie Y, Inoue H. Rapid evaluation of fatigue limit using infrared thermography: comparison between two methods for quantifying temperature evolution. Mechanical Engineering Journal. 2017; 4: 17-00009-00017-00009.

[148] Lepitre P, Calloch S, Dhondt M, Surand M, Doudard C. Identification of the damage scenarios under cyclic loading of a coated 300M steel by infrared thermography measurements. Physical Sciences Forum. 2022; 4: 30.

[149] Fernández-Canteli A, Castillo E, Argüelles A, Fernández P, Canales M. Checking the fatigue limit from thermographic techniques by means of a probabilistic model of the epsilon–N field. International Journal of Fatigue. 2012; 39: 109-115.

[150] Faria J J R, Fonseca L G A, de Faria A R, Cantisano A, Cunha T N, Jahed H, et al. Determination of the fatigue behavior of mechanical components through infrared thermography. Engineering Failure Analysis. 2022; 134: 106018.