INFLUENCE OF HOT ISOSTATIC PRESSING AND SURFACE FINISH ON THE MECHANICAL BEHAVIOUR OF TI6AL4V PROCESSED BY ELECTRON BEAM MELTING

S. Franchitti1, C. Pirozzi1, R. Borrelli1

1CIRA, Italian Aerospace Research Centre, Structural and Material Department,

Via Maiorise, 81043 Capua, Italy

*Corresponding author: Rosario Borrelli email: r.borrelli@cira.it

Abstract

Electron Beam Melting (EBM) is one of a few additive manufacturing technologies capable of making full-density functional metallic parts realized from raw materials in the form of powders. The ability of direct fabrications of metallic parts can accelerate product designs and developments in a wide range of metallic-part applications, especially for complex components, which are difficult to make by conventional manufacturing means. To capitalize on these benefits, it must be shown that the mechanical performances of parts produced by EBM can meet design requirements. In this research an intensive mechanical characterization aimed at determining static and fatigue performance of the alloy Ti6Al4V processed by EBM has been performed. The effect of both postprocessing treatments (HIP and surface finish) on the mechanical behavior was evaluated by mechanical testing, microstructural study, computed tomography analysis and fracture surface investigation.

Keywords: Additive Materials, Electron-Beam, Ti-6Al-4V, Heat Treatment, Fatigue, Mechanical Properties

1. Introduction

As defined by the American Society for Testing and Materials (ASTM), additive manufacturing (AM) refers to “a process of joining materials to make objects from 3D model data, usually layer upon layer, as opposed to subtractive manufacturing methodologies.” Its synonyms include additive fabrication, additive processes, additive techniques, additive layer manufacturing, layer manufacturing, direct manufacturing and freeform fabrication [1], and it is also known as 3D printing and rapid prototyping (RP) in industry.

A comprehensive review of all major Additive Manufacturing (AM) processes for metallic materials which have been developed along the past 30 years is provided in [2]. Among these, the AM processes based on the Powder Bed Fusion (PBF) technique are the most mature and widely used metal additive manufacturing processes. Powder bed fusion (PBF) uses a high-energy power source to selectively melt or sinter a metallic powder bed. Depending on the type of power source, PBF can be further divided into two major techniques: selective laser melting (SLM) which uses a high-intensity laser, and electron beam melting (EBM), which uses an electron beam. Both processes need a building platform to hold the powder.

The present study is on the mechanical characterization of Ti6Al4V alloy processed by EBM. The EBM technology was ready for commercialization in 2002 when the company Arcam AB Inc. (Sweden) launched its first EBM system [4]. In a vacuum chamber, the electron beam is emitted by heating a tungsten filament and accelerated towards the powder on the powder bed using an accelerating voltage in the order of 60 kV in such a way to generate the energy needed for high melting capacity and high productivity (energy density is in excess of 100 kW/cm2). The electron beam is managed by electromagnetic coils providing extremely fast and accurate beam control that allows several melt pools to be maintained simultaneously. Comprehensive review on the EBM process can be found in [5] and [6].

While the AM processes present many advantages to the aerospace industry in comparison with traditional manufacturing processes, airworthiness and air transport safety must be guaranteed. For these reasons, specific technical challenges of AM still need to be addressed. One of the most compelling challenge is to develop an understanding of how to achieve better mechanical properties and surface finish by using post treatment processes [7].

Unlike more abundant tensile data, published values on the fatigue characteristics of specimens manufactured using SLM or EBM are limited [8]. The evaluation of fatigue properties is critical to understand the failure cause of metal AM parts under cyclic loading [9-13].

Several researchers have investigated the effect of the Hot Isostatic Pressure (HIP) process on the mechanical behavior of material processed by EBM. The HIP process is a thermo-mechanical process used to reduce the porosity of the material which is subjected to both elevated temperature and isostatic gas pressure in a high pressure containment vessel. It is well known in literature that HIP produces a significant α-lath coarsening that results in a reduction of static strength [14]-[15]. Nevertheless, it is also highlighted that the effect of the HIP on the fatigue performance is not well understood. This uncertainty is evident by analyzing various research works reported in literature: in some works the HIP process improves the material fatigue behavior [16] - [17] - [18] while other recent studies [19]-[20] shows that HIP has no enhancing effect on fatigue strength for EBM materials.

In this work, in order to assess the HIP effect on the alloy Ti6Al4V processed by EBM, an intensive mechanical characterization aimed at determining static and fatigue performance of the material was performed.

A second objective of the present work is to investigate on the influence of the surface roughness on the mechanical behavior of the alloy Ti6Al4V processed by EBM. Indeed, one of the main advantages of ALM is the geometric freedom involved in fabricating components. One common way to use EBM is to produce near-net shaped structures which are finished machined to tight tolerances for demanding applications. Although this machining can achieve the required dimensional accuracy, the differing surface conditions between machined and unmachined regions of a part may impair the mechanical behavior. Therefore, it is important to investigate the mechanical behavior of EBM built parts with respect to the surface condition. An investigation on the influence of surface finish on the tensile properties of EBM Ti6Al4V samples was performed in [21] and [22]. The main finding was the identification of a true cross section, inscribed into the measured cross section, which really withstands the applied load. A quantitative study [23] has been made on the influence of as-built surface conditions on the tensile and fatigue properties of Ti6Al4V produced by EBM as compared to acid-etched and machined conditions. The experimental results show that chemical etching can double tensile elongation and noticeably improve tensile strengths due to improved surface finish. However, the fatigue strength of  Ti6Al4V chemical etched specimens is still much lower to that of mill-annealed Ti6Al4V due to residual surface defects. In [24], it has been reported that the fatigue strength of machined EBM Ti6Al4V specimens was significantly better than that of as-built ones. Moreover, it was found that the fatigue strength of EBM built samples was less than that of standard annealed Ti6Al4V materials.

In this paper, a mechanical test campaign on Ti6AlV processed by EBM was performed in order to evaluate the influence of both HIP process and surface condition on the material mechanical behaviour. Microstructural investigation, computed tomographic and fracture surface analysis were also performed to support theoretical explanations of the mechanical test results.

2. Material and testing

The samples used in this study have been manufactured by using Ti6Al4V grade 5 alloy atomized powder with spherical morphology [1]. The spherical shape may contribute to improve flowability and may ensure high build rates and accuracy. The powder flow rate measured according to ASTM B213 [25] was found as 25 s/50 g. The apparent density according to ASTM B212 [26] was 2.57 g/cm3. As regards the particle size distribution, the percentage by mass of particle size in the range 45-106 m was found to be equal to 93.7% as even shown in Figure 1. The powder nominal chemical composition is summarized in Table 1.

Figure 1: Ti6Al4V particle size distribution

Table 1 Nominal chemical composition (wt.% ) of the Ti6Al4V pre-alloyed powder used in EBM

The EBM machine used for this study was an ARCAM A2X, and the software installed was the EBM Control version 3.2. The specimens manufactured in this study have been built by using standard Ti6Al4V build themes for a layer thickness of 50 m. This build theme varies electron beam parameters in a controlled sequence throughout the build according to algorithms developed by the manufacturer in an effort to achieve fully dense as-built parts with consistent microstructure and properties. Since the algorithm is covered by copyright, beam current and beam speed time-dependent diagrams are hided to the users. A line offset of 0.1 mm has been set; the EBM process has been carried out in a vacuum.

## Tensile Tests

# The tensile tests have been performed on round tensile samples produced by EBM technology, with final geometry and dimensions compliant to the standard ASTM E08 [27], as shown in Figure 2.

Figure 2: Geometry of the tensile specimens (dimensions in mm)

In order to limit the number of variables that can affect the mechanical response of the specimens, in this work a single grow orientation and the same set of parameters for all specimens has been considered.

In particular the samples were tested in the z-direction growth orientations, i.e. perpendicular to the layers, in order to get tensile properties with the same samples configuration (same growth orientation) of the fatigue ones which will be presented in the next section.

Three sets of specimens have been manufactured with 90° grow orientation with respect to the start plate (x-y plane) and tensile tested:

-	N. 5 specimens “As built”

-	N. 5 specimens “Machined”

-	N. 5 specimens “Machined HIP”

# The first set of specimens has been directly EBM manufactured in the dogbone shape and they have been tested in “As built” condition, the second ones obtained by machining cylindrical bars EBMed and tested without performing any other postprocessing treatment and the third ones obtained by machining cylindrical bars EBMed then treated by HIP (Hot Isostatic Pressing). The HIP is a thermo-mechanical treatment aimed at reducing the size and radius of curvature of the porosity defects. The HIPing treatment was performed with the parameters recommended in ASTM F2924-14 [28]. The coupons were subjected to an argon inert atmosphere at 100 MPa pressure and at 920 °C for 120 minutes. An example of “As built” and “Machined” specimens is shown in Figure 3.

Figure 3: a) Tensile tested “as built” specimens b) Tensile tested “machined” specimens

The tensile tests have been performed by using an Instron 4505 machine with load cell of 100 kN.

## Fatigue Tests

Experimental tests were performed using dog bone round specimens, with final geometry and dimensions compliant to the standard ASTM E466 [29] shown in Figure 4.

Figure 4: Geometry of the fatigue specimens (dimensions in mm)

To limit the number of variables that can affect the mechanical response of the specimens, in this work a single grow orientation and the same set of parameters for all specimens has been considered.

In particular, according to [13] and [18], the samples were tested in the “weak” z-direction, i.e. perpendicular to the layers, to get minimum fatigue properties.

Three batches of specimens were produced with 90° grow orientation with respect to the start plate (x-y plane) and tested by fatigue:

-	N. 25 specimens “As built”

-	N. 25 specimens “Machined”

-	N. 25 specimens “Machined HIP”

The “As built” specimens have been produced by EBM process and tested in “As built” condition.

The “Machined”specimens have been produced by machining cylindrical bars manufactured by EBM process (Figure 5b), no heat treatment has been performed before to be tested.

The “Machined HIP”specimens have been produced by machining cylindrical bars produced by EBM process, then treated by HIP. HIP treatment on the fatigue specimens was performed with the parameters recommended in ASTM F2924-14 [28], as well as for the tensile specimens. Hence, the coupons were subjected to an argon inert atmosphere at 100 MPa pressure and at 920 °C for 120 minutes. The specimens are shown in Figure 5.

| a) | b) | c) |
| --- | --- | --- |

Figure 5: a) Fatigue tested “As built” specimens  b) Cylindrical bars manufactured by EBM process to obtain               c) “Machined” and “Machined HIP” specimens fatigue tested.

Fatigue tests have been carried out compliant to the standard ASTM E466 [29]. The S-N curves, according to the ASTM E466 [29], have been calculated for each set of specimens.

The fatigue tests have been performed by using a Zwick/Roel AMSLER100 machine with load cell of 100 KN and test execution parameters are R = 0.1, Kt = 1 and load frequency=20 Hz.

## Microstructural analysis

Microscope optical observations have been carried out on cylindrical samples (height of 1cm) obtained by cutting the upper part of all the fatigue specimens heads, in order to investigate microstructure of  specimens and in particular to show evidence of microstructural changes due to the effect of HIP treatment on  phases segregation and on  lath aspect ratio

Then cylindrical surfaces of samples have been subjected to metallographic preparation consisting in grinding with abrasive papers, polishing with diamond pastes of several granulometry sizes, and etching with Kroll’s reagent.

The optical observations have been carried out with the metallographic microscope LEICA DM RXE and with the camera LEICA MC 190 HD at several magnifications in order to evidence macrostructure and microstructure of the investigated samples.

## Computed tomographic analysis

A tomographic analysis has been carried out on samples obtained by machining cylindrical bars EBM manufactured before and after HIP treatment in order to evaluate its effect on macrostructure particularly on pores and voids closure. At this aim tomographic investigations have been carried out by YXLON FF35 Computer Tomography with settings suitable to detect voids of about 78m (voxel size).

## Fracture surface analysis

Microscope optical observation have been carried out, at low level of magnification, on all tested tensile and fatigue samples in order to investigate the surfaces of fracture and to locate the cracks origin. The optical observations were taken by means of a Leica MZ12 stereo-graphic microscope and a Leica MC190 HD camera.

3. Results

## Tensile Tests

In Figure 6 tensile test results for all the types of specimens tested have been reported in terms of Young Modulus (E), elongation at fracture (at fracture), Tensile strength (TS) and Yield strength (Y0,2).

| a) |  |
| --- | --- |
| b) | c) |

Figure 6: Tensile tests results: a) Yield Strength (Y0,2) and Tensile Strength (TS); b) Young Modulus (E);                     c) Elongation at fracture ( at fracture)

## Fatigue Tests

In Figure 7, the S-N curves have been reported on the same graph for all the types of specimens tested, in addition to the S-N curve of standard Ti6Al4V in annealed condition [30].

Figure 7: Plot of S-N Curves

## Microstructural Analysis

A microstructural investigation aimed at finding out possible explanations of the mechanical  behavior of Ti6Al4V processed by EBM has been carried out.

The microstructure of the “Machined” specimens vs. “Machined HIP” specimens are shown in Figure 8.

Figure 8: Microstructure of Ti6Al4V in perpendicular planes for non-treated (a) (c) and (e) and HIP-treated (b) (d) and (f) specimens

## Computed Tomographic Analysis

A computed tomographic investigation aimed at evaluating the effect of the HIP process was performed.  Figure 9 shows a tomographic image of a specimen before and after the HIP treatment.

Figure 9: Microporosity healing as effect of the HIP process

## Fracture Surface Analysis

An analysis of the fracture surfaces has been carried out on tensile and fatigue specimens in order to understand where crack originates.

Typical macrographs showing the fracture surfaces after the tensile tests for the “Machined” samples, “Machined HIP” samples and “As built” samples are shown in Figure 10, Figure 11 and Figure 12.

Figure 10: Macrograph of surface fractures of tensile tested “Machined” samples  a) 7.0 X, b) fracture zone at 100 X.

Figure 11: Macrograph of surface fractures of tensile tested “Machined HIP” samples  a) 7.0 X, b) fracture zone at 100 X.

Figure 12: Macrograph of surface fractures of tensile tested “As built” samples  a) 7.0 X, b) fracture zone at 100 X.

Typical macrographs showing the fracture surfaces after fatigue testing for the “Machined” samples, “Machined HIP” samples and “As built” samples are shown in Figure 13, Figure 14 and Figure 15, respectively.

Figure 13: Macrograph of surface fractures of fatigue “Machined” samples

Figure 14: Macrograph of surface fractures of fatigue “Machined HIP” samples

Figure 15: Macrograph of surface fractures of fatigue “As built” samples

4. Discussion

In this section, the results of the tensile and fatigue testing presented in the previous section will be deeply commented.

The effect of the HIP process on the static mechanical properties is shown in Figure 6. Hipped and machined specimens show lower tensile strength with respect to the no-hipped and machined specimens. Such results, confirming findings in [14] and [15], are due to the fact that one of the hipping effect is a significant α-lath coarsening that results in a reduction of static strengths. The significant microstructural coarsening due to the HIP, resulting from self-diffusion, can be clearly seen in Figure 8. The Figure show a comparison between the microstructure of non-treated and HIP-treated specimens and reveals an  lath growth by almost one order of magnitude after HIP, according to the results obtained in [31].

The effect of the surface finish on the static mechanical properties is also shown in Figure 6. “As built” specimens show lower tensile properties with respect to the “Machined” ones because of the significant reduction of the actual cross section due to high irregular external circular surfaces, confirming literature data on this topic [21]-[22]. Such irregular circular surfaces is related to the high    surface roughness which for “As built” specimens may be very high [32]. Therefore, when EBM parts are used in-service in their “As built” state, it is necessary that designer use appropriate values of the mechanical properties which take into account the effective resistance of the component, especially for parts having thin dimensions since in this case the reduction of the cross-section (in percentage) due to the irregular surface, is higher.

The fracture surface analysis on tensile specimens reveals that tensile tests failures always take origins from defects, which consist in metallurgical incoherences due to the presence of unmelted grains of Ti6Al4V powder inside the bulk metal, as it is possible to note looking at Figure 10, Figure 11 and Figure 12, which refer to “Machined HIP”, “Machined” and “As built” specimens, respectively.

The effect of the HIP process on the fatigue behavior of Ti6Al4V EBMed is shown in the S-N Curve of Figure 7 where the cyclic stresses () have been plotted against the number of cycles to failure (N) on a log-log diagram. By comparing the results obtained by the machined specimens, and in particular, by comparing “Machined HIP” specimens (circles) with “Machined” specimens (triangles), the following observations can be drawn:

- At low number of cycles (oligocyclic fatigue) there is no significant difference in the fatigue behaviour of the two families of specimens.

- The Wohler curve of “Machine” specimens drops continuously while the Wohler curve of “Machined HIP” specimens becomes a horizontal line with decreasing stress amplitude.

- At very high number of cycles, “Machined HIP” specimens tends to have a slight higher fatigue strength with respect to the “Machined” specimens.

In order to explain such behaviour it should be highlighted that in Ti6Al4V, as shown in [33] and [34], when there are not too many bulk defects as in the case of EBM process, the phenomenon of crack initiation plays the dominant role in controlling the total life in high-cycle fatigue. On the contrary, in low-cycle fatigue, the phenomenon of crack propagation turns dominant.

One of the main effect of the HIP process is shown in the CT images of Figure 9 which reveals a significant decrease of the number and dimensions of defects in the treated specimens compared to those ones observed in the non-treated specimens. Such successful defects closure is related to self-diffusion occurred at the applied heat treatment under the isostatic pressure. HIP process effectively reduces the defects consisting in sharpened voids or circular porosity spread inside the bulk metal and which represent a cause of a quick crack initiation. Anyway, the crack initiation does not play the dominant role at low-cycle level. On the other hands, a second effect of the HIP process is the above mentioned microstructural coarsening due to the heat treatment to which the material is subjected. The  lath coarsening is a factor easing the crack propagation, since the phaseboundaries coarsening can represent a preferential path for it [35] reflecting a decrease in fatigue resistance especially in low cycle fatigue when crack propagation is dominant. This behavior is typical of lamellar microstructure. In fact lamellar microstructures are characterized by parallel  lamellae with intergranular phase. The so arranged  and  phases, under a cyclic tensile load, deform in coherent way because the slip system of the two phases is parallel, i.e. the parallel lamellae with intergranular behaves as an homogeneous body. On the contrary a discontinuity in the slip mode occurs at the boundary between lamellae and  layer and here the fracture begins and propagates [36]. In other words,  in low-cycle fatigue, HIP process produce two contrasting effects on the material (densification and microstructural coarsening) that compensate one each other and ensure that the behaviour of “Machined HIP” specimens is substantially similar to that of “Machined” ones.

At high cycle level, since the crack initiation has the dominant role, the HIP densification effect begins to predominate over the microstructural coarsening effect. As a consequence, “Machined HIP”  specimens tends to have better fatigue behaviour than the “Machined” ones. As it is well known the effect of the HIP is even to make more homogeneous the microstructure which improves the resistance to crack initiation [37]. Voids closures and microstructural homogenization have the effect of increasing the fatigue life at high number of cycles. This phenomena can explain the better behaviour of hipped specimens at high-cycle level than the not hipped ones.

An analysis of the fracture surfaces has been carried out in order to understand where fatigue crack originates. All the “Machined HIP” specimens have one or several crack initiations at the surface as shown in the macrograph of Figure 14. For these specimens, the failures have been originated in all the cases from the edge of the surface, at a surface defect. A different behavior was observed in the “Machined” specimens. In this case, indeed, at low-cycle fatigue, failures originates from the surface edge (similarly to what observed in the “Machined HIP” specimens) but the crack initiation sites abruptly shift from surface to interior of the specimen (at about 1 mm from the surface) with decreasing the stress amplitude as observed in the fracture surface macrograph of Figure 13 which is related to a “Machined” specimen failed at 107 cycles.  Such behavior was observed also in [34].

The effect of the surface finish on the fatigue behavior of Ti6Al4V EBMed  is also shown in Figure 7. As expected, “As built” specimens show very low fatigue performance with respect to the “Machined” ones because of the high surface roughness which plays a major role in fatigue failures mechanisms. Hence, as highlighted for tensile properties, also from a fatigue point of view it is necessary that designers will take into account the considerations above exposed if will design EBM parts with some regions which will be used in-service in their “As built” condition.

All the “As built” specimens failures have been originated from the edge of the surface. Such failure mode is mainly due to the high roughness which is a predominant failure cause even respect to the internal porosity.

4. Conclusions

In this study the influence of both the HIP process and the surface finish on the mechanical behavior of Ti6Al4V produced via EBM has been carried out by testing this alloys in three different conditions: “As built”, “Machined” and “Machined HIP”.

According with the state of the art it has been found that the HIP process causes an effective reduction of porosities but also a significant α-lath coarsening in the material that results in a reduction of static strengths. Moreover, “As built” specimens show a reduction of tensile strength of about 10% with respect to the “Machined” ones due to the high irregular external surface which drastically reduce the true cross-section.

The influence of the HIP process on the fatigue behavior of Ti6Al4V produced via EBM was found function of the cycles level. At low number of cycles (oligocyclic fatigue) there is no significant difference in the fatigue behavior of “Machined HIP” and “Machined” specimens. At very high number of cycles, “Machined HIP” specimens tends to have a slight higher fatigue strength with respect to the “Machined” specimens. In fact, at lower loads, when the crack initiation plays the dominant role in the fatigue failure, the presence of defects (voids/lack of fusions and porosity) inside the “Machined” specimens can promote a faster nucleation of the crack causing a slight worse fatigue behavior than the “Machined HIP” ones. Finally, the Ti6Al4V in “As built” condition shows very bad fatigue performance, which may be not compliant with the standards and the requirements of the aerospace applications. The reason of low Ti6Al4V fatigue performance at “As built” condition is mainly due to the presence of very high surface roughness from which originate all the cracks leading to failure. On the contrary “Machined HIP” and “Machined” specimens have shown both a high fatigue strength almost comparable with Ti6Al4V standard (annealed condition).

Acknowledgements

Authors acknowledge Dr. Andrea Vigliotti and Dr. Angela Ferrigno for their support during the microscopic analysis of samples.

References

- ASTM, F2792-12a, Standard Terminology for Additive Manufacturing Technologies.

- Zhang, Y., Wu, L., Guo, X. et al., Additive Manufacturing of Metallic Materials: A Review, J. of Materi Eng and Perform (2018) 27: 1. https://doi.org/10.1007/s11665-017-2747-y

- J. Dawes, R. Bowerman, and R. Trepleton, Introduction to the Additive Manufacturing Powder Metallurgy Supply Chain Technol, Johnson Matthey Technol. Rev., 2015, 59(3), p 243–256

- www.arcam.com

- X. Gong, T. Anderson, K. Chou, Review on powder-based electron beam additive manufacturing technology, Manuf. Rev. 1 (2014) 1-10.

- C. Koerner, Additive manufacturing of metallic components by selective electron beam melting — a review, Int. Mater. Rev. 61 (2016) 361-377.

- A. Uriondo, M. Esperon-Miguez and S. Perinpanayagam, The present and future of additive manufacturing in the aerospace sector: A review of important aspects, Proc IMechE Part G: J Aerospace Engineering, 0(0) 1–16

- M. Koike, K. Martinez, L. Guo, G. Chahine, R. Kovacevic, T. Okabe, Evaluation of titanium alloy fabricated using electron beam melting system for dental applications, Journal of Materials Processing Technology 211 (2011) 1400–1408

- Fatemi, A, Molaei, R, Simsiriwong, J, et al. Fatigue behaviour of additive manufactured materials: An overview of some recent experimental studies on Ti‐6Al‐4V considering various processing and loading direction effects. Fatigue Fract Eng Mater Struct. 2019; 42: 991– 1009. https://doi.org/10.1111/ffe.13000

- Yates, JR, Efthymiadis, P, Antonysamy, A, Pinna, C, Tong, J. Do additive manufactured parts deserve better? Fatigue Fract Eng Mater Struct. 2019; 42: 2146– 2154. https://doi.org/10.1111/ffe.13092

- Yadollahi, A, Mahmoudi, M, Elwany, A, Doude, H, Bian, L, Newman, JC. Fatigue‐life prediction of additively manufactured material: Effects of heat treatment and build orientation. Fatigue Fract Eng Mater Struct. 2020; 43: 831– 844. https://doi.org/10.1111/ffe.13200

- Zhang, X., Martina, F., Ding, J., Wang, X., and Williams, S. W. ( 2017) Fracture toughness and fatigue crack growth rate properties in wire + arc additive manufactured Ti‐6Al‐4V. Fatigue Fract Engng Mater Struct, 40: 790– 803. doi: 10.1111/ffe.12547.

- Y. Kok, X.P. Tan, P. Wang, M.L.S. Nai, N.H. Loh, E. Liu, S.B. Tor, Anisotropy and heterogeneity of microstructure and mechanical properties in metal additive manufacturing: A critical review, Materials & Design, Volume 139, 2018, Pages 565-586, ISSN 0264-1275, https://doi.org/10.1016/j.matdes.2017.11.021.

- Ming-WeiWu, Pang-HsinLai, The positive effect of hot isostatic pressing on improving the anisotropies of bending and impact properties ins elective laser melted Ti-6Al-4V alloy, Materials Science & Engineering A658 (2016) 429–438

- A.M. Vilardell, G. Fredriksson, I. Yadroitsev, P. Krakhmalev, Fracture mechanisms in the as-built and stress-relieved laser powder bed fusion Ti6Al4V ELI alloy, Optics and Laser Technology 109 (2019) 608–615

- L. Facchini, E. Magalini, P. Robotti, A. Molinari, (2009), Microstructure and mechanical properties of Ti-6Al-4V produced by electron beam melting of pre-alloyed powders, Rapid Prototyping Journal, Vol. 15 Iss 3 pp. 171 – 178

- V. Popov, A. Katz-Demyanetz, A. Garkun, G. Muller, E. Strokin, H. Rosenson, Effect of Hot Isostatic Pressure treatment on the Electron-Beam Melted Ti-6Al-4V specimens, Procedia Manufacturing, Volume 21, 2018, Pages 125-132, ISSN 2351-9789, https://doi.org/10.1016/j.promfg.2018.02.102.

- E. Brandl, C. Leyens, F. Palm, Mechanical properties of additive manufactured Ti-6Al-4V using wire and powder based processes, IOP Conf. Series: Materials Science and Engineering 26 (2011) 012004 doi:10.1088/1757-899X/26/1/012004

- G. Nicoletto, R. Konečná, M. Frkáň, E. Riva, Surface roughness and directional fatigue behavior of as-built EBM and DMLS Ti6Al4V, International Journal of Fatigue 116 (2018) 140–148

- M. Kahlin, H. Ansell, J.J. Moverare, Fatigue behaviour of notched additive manufactured Ti6Al4V with as-built surfaces, International Journal of Fatigue 101 (2017) 51–60

- C. Pirozzi, R. Borrelli, S. Franchitti, F. Caiazzo, V. Alfieri, P. Argenio, Study on the Factors Affecting the Mechanical Behavior of Electron Beam Melted Ti6Al4V, Journal of Materials Engineering and Performance 2017, DOI 10.1007/s11665-017-2894-1

- R. Sepe, S. Franchitti, R. Borrelli, F. Di Caprio, E. Armentani, F. Caputo, Correlation between real geometry and tensile mechanical behaviour for Ti6Al4V Electron Beam Melted thin specimens, Theoretical and Applied Fracture Mechanics, 2020, 102519, ISSN 0167-8442, https://doi.org/10.1016/j.tafmec.2020.102519.

- Sun, Y 2016, Powder manipulation, microstructure, mechanical properties and bio-corrosion performance of titanium and titanium alloys additively manufactured by selective electron beam melting, Doctor of Philosophy (PhD), Aerospace, Mechanical and Manufacturing Engineering, RMIT University. http://researchbank.rmit.edu.au/view/rmit:161976

- Rafi, K., Starr, T.L., & Stucker, B.E., Mechanical property evaluation of Ti-6Al-4V parts made using Electron Beam Melting, Solid Freeform Fabrication Symposium Proceedings, 2012, Austin, TX, August 2012

- Standard Test Methods for Flow Rate of Metal Powders Using the Hall Flowmeter Funnel, 2013, B213, ASTM

- Standard Test Method for Apparent Density of Free-Flowing Metal Powders Using the Hall Flowmeter Funnel, 2013, B212, ASTM

- Standard Test Methods for Tension Testing of Metallic Materials, E8, ASTM, 2016

- Standard Specification for Additive Manufacturing Titanium-6 Aluminum-4 Vanadium with Powder Bed Fusion, F2924, ASTM (2014)

- Standard Practice for Conducting Force Controlled Constant Amplitude Axial Fatigue Tests of Metallic Materials, E466, ASTM (2015)

- http://www.matweb.com/

- A. Mohammodhosseimi et al, Microstructure and mechanical properties of Ti6Al4V manufactured by electron beam melting process, Material research Innovation, December 2013

- R. Borrelli, S. Franchitti, C. Pirozzi, L. Carrino, L. Nele, W. Polini, L. Sorrentino, A. Corrado, Ti6Al4V Parts Produced by Electron Beam Melting: Analysis of Dimensional Accuracy and Surface Roughness, Journal of Advanced Manufacturing Systems, Vol. 19, No. 1 (2020) 1–24,  https://doi.org/10.1142/S0219686720500067

- F. J. Gil, M. P. Ginebra, J. M. Manero, and J. A. Planell, “Formation of α-Widmanstätten structure: effects of grain size and cooling rate on the Widmanstätten morphologies and on the mechanical properties in Ti6Al4V alloy,” Journal of Alloys and Compounds, vol. 329, no. 1-2, pp. 142–152, 2001.

- J. H. Zuo, Z. G. Wang, and E. H. Han, “Effect of microstructure on ultra-high cycle fatigue behavior of Ti-6Al-4V,” Materials Science and Engineering: A, vol. 473, no. 1-2, pp. 147–152, 2008.

- Mohsesen Seifi et al, Effect of Hot Isostatic Pressure treatment on the Electron-Beam Melted specimen, International Journal of Fatigue, 2017 p. 263-287

- F. Scherillo et al, Microstructural and micromechanical study of a Ti6Al4V component made by Electron Beam Melting, ESAFORM2016 conf., Nantes, 27-29 Aprile 2016

- Y. Fan, W.  Tian, Y. Guo, Z. Sun, J. Xu, Relationships among the Microstructure, Mechanical Properties, and Fatigue Behavior in Thin Ti6Al4V, Advances in Materials Science and Engineering, 2016, https://doi.org/10.1155/2016/7278267