Table 1 Summary of producing BaSO4 nanoparticles using microreactors

| Phase system | Microreactor | Size of nanoparticles (nm) | Range of total flow rates (mL/min) | Ref. |
| --- | --- | --- | --- | --- |
| Na2SO4 and BaCl2·2H2O | Chaotic flow microreactor | 23–109 | 10–160 | This paper |
| Na2SO4 and BaCl2 | Laminar flow microreactor | 200–10 000 | 3.69–27.3 | [22] |
| Na2SO4 and BaCl2·2H2O | Laminar flow microreactor | 12–30 | 10–40 | [4] |
| H2SO4 and BaCl2 | Laminar flow microreactor | 91.2–252 | 4.44–13.3 | [8] |
| H2SO4, BaCl2, and butyl alcohol | Segment flow microreactor | 10–30 | 0.75–0.85 | [6] |
| Na2SO4, BaCl2, and fluorinated oil | Segment flow microreactor | 30–160 | 0.0002–0.001 | [10] |
| H2SO4, BaCl2, and butyl alcohol | Segment flow microreactor | 10–40 | 0.02–0.2 | [9] |
| H2SO4, BaCl2·2H2O, and dodecane | Segment flow microreactor | 65–505 | 2.321–9.946 | [25] |
| [NH4]2SO4, BaCl2, and corn oil | Segment flow microreactor | 15–100 | 0.8 | [26] |
| Na2SO4, BaCl2, and nitrogen | Segment flow microreactor | 200–1100 | 2.75–6.5 | [27] |