A High-Throughput Chaotic Advection Microreactor for Preparation of Uniform and Aggregated BaSO4 Nanoparticles

Hua Yang1, Shi-Xiao Wei1, Han Chen1, Lang Chen1, Chak-Tong Au2, Ting-Liang Xie1*, Shuang-Feng Yin1*

1College of Chemistry and Chemical Engineering, Advanced Catalytic Engineering Research Center of the Ministry of Education, State Key Laboratory of Chemo/Biosensing and Chemometrics, Provincial Hunan Key Laboratory for Cost-effective Utilization of Fossil Fuel Aimed at Reducing Carbon-dioxide Emissions, Hunan University, Changsha 410082, P. R. China.

2College of Chemical Engineering, Fuzhou University, Fuzhou 350002, P. R. China.

*Corresponding authors:

E-mail: xtl2020041@hnu.edu.cn (Ting-Liang Xie)

E-mail: sf_yin@hnu.edu.cn (Shuang-Feng Yin)

Abstract

A high-throughput (105.5 g/h) passive four-stage asymmetric oscillating feedback microreactor using chaotic mixing mechanism was developed to prepare aggregated BaSO4 particles of high primary nanoparticle size uniformity. Three-dimensional unsteady simulations showed that chaotic mixing could be induced by three unique secondary flows (i.e., vortex, recirculation, and oscillation), and the fluid oscillation mechanism was examined in detail. Simulations and Villermaux-Dushman experiments indicate that almost complete mixing down to molecular level can be achieved and the prepared BaSO4 nanoparticles were with narrow primary particle size distribution (PSD) having geometric standard deviation, σg, less than 1.43 when the total volumetric flow rate Qtotal was larger than 10 mL/min. By selecting Qtotal and reactant concentrations, average primary particle size can be controlled from 23 to 109 nm as determined by microscopy. An average size of 26 nm with narrow primary PSD (σg = 1.22) could be achieved at Qtotal of 160 mL/min.

Keywords: Passive oscillating feedback microreactor, high-throughput, chaotic convection, fluid oscillation, BaSO4 nanoparticles

Introduction

Barium sulfate (BaSO4) is an important inorganic material widely used in industries such as ceramic, plastic, paint, pigment, paper-making and medical 1. Compared with ordinary micro-sized BaSO4 particles, BaSO4 nanoparticles with small size and narrow PSD have larger surface-to-volume ratio and better dispersion properties. The latter is essential for the manufacture of high-class resins and rubbers with high thermal stability and mechanical strength 2. At present, BaSO4 nanoparticles are prepared by co-precipitation, ball milling and anion exchange methods, with co-precipitation being the major one for industrial production 3. Traditional batch reactors (e.g., stirred tanks) are often used in industry. However, due to inadequate mixing and poor mass transfer, it is difficult to achieve homogeneity in terms of concentration and temperature in a batch reactor, and hence hard to produce high quality nanoparticles with a narrow PSD 4.

In recent years, with the development of micro manufacturing and micro machining technology, microreactors have been adopted to overcome the problems due to their efficient heat and mass transfer 5. Consequently, high quality BaSO4 nanoparticles with narrow PSD could be achieved 6. However, all the studies were performed in microreactors of ordered flows, including those of lamination flow and segment flow.

With respect to lamination flow (Figure 1A), the two liquids flow side by side in low throughput, and with diffusion induced mainly by molecular thermal motion, mass transfer efficiency is extremely poor 7. Therefore, homogeneous mixing on molecular scale prior to the fast nucleation and growth of BaSO4 is hard to achieve 8. In addition, the laminar flow can cause a typically parabolic velocity profiles in the microchannel, which can induce a relatively broad residence-time distribution, thereby making it difficult to guarantee a narrow PSD 4. As for segment flow (Figure 1B and Figure 1C), an inert gas phase or insoluble liquid phase is added as separation medium to induce a two-phase flow. The recirculation flow inside the discrete droplets (Figure 1B) or slugs (Figure 1C) can enhance mass transfer, which can help provide a uniform reaction environment for nucleation and growth of nanoparticles 9. Nonetheless, the throughput must be scrupulously low to keep the frail stability of such a special flow pattern 10.

To sum up, due to poor mixing efficiency or low throughput, it is difficult to meet the high demand of industrial production using the ordered microreactors. Although the throughput of ordered microreactors can be improved through the numbering-up approach, it remains a challenge to maintain even distribution of feed flow in each of the branch microreactors 11. Therefore, it is of significance to develop a method to increase the throughput of microreactors to produce high quality small-sized BaSO4 nanoparticles in large amount.

Lately, chaotic advection microreactors (Figure 1D) have attracted much attention 12. Unlike ordered flow microreactors, chaotic advection microreactors usually operate in disordered flow mode at Reynolds numbers of 102–103, which is much larger than those of ordered flow microreactors (10-1–102) 13. In addition, the transverse flow perpendicular to the bulk flow direction in chaotic advection microreactors can cause the fluid to stretch, fold and compress, which distinctly reduce molecule diffusion distance and enhance fluid mixing and mass/heat transfer 14. It is envisaged that a field homogeneous in both concentration and temperature could be achieved in chaotic advection microreactors for the preparation of high quality BaSO4 nanoparticles with narrow PSD at high throughput. However, there are few reports on the synthesis of nanoparticles using chaotic advection microreactors 15. To the best of our knowledge, chaotic advection microreactors have not been used to produce BaSO4 nanoparticles.

Based on the concept of passive chaotic advection microreactors, we designed a four-stage asymmetric oscillating feedback microreactor (FOFM) of high throughput to prepare uniform and aggregated BaSO4 nanoparticles. The mixing mechanism and flow characteristics of FOFM were investigated by computational fluid dynamics (CFD) simulation. The mixing performance of FOFM was determined by Villermaux-Dushman experiments. The effect of operation parameters on the average size and PSD of BaSO4 nanoparticles was determined. High quality small-sized nanoparticles with narrow PSD could be produced at a high throughput of 160 mL/min.

Experiments and methods

Chemicals

Barium chloride dihydrate (BaCl2·2H2O, AR), sodium sulfate (Na2SO4, AR), boric acid (H3BO3, AR), potassium iodide (KI, AR), potassium iodate (KIO3, AR) and sodium hydroxide (NaOH, AR) were purchased from Sinopharm Chemical Reagent Co., Ltd (Shanghai, China). All chemicals were used as received without any further purification. Deionized water (DI, 18 MΩ cm) was used in all experiments.

Four-stage asymmetric oscillating feedback microreactor

The FOFM of “T-type inlet” (Figure 2A) and “Y-type inlet” (Figure 2B) structures were designed based on our previous work 16. As indicated in the figures, every stage of FOFM includes a diverging chamber, two feedback channels, and a splitter. The splitter could effectively promote internal flow recirculation through the feedback channels, thereby enhancing the fluid lateral perturbance. The chaotic advection characteristics and the three unique flow patterns (viz. vortex, recirculation and oscillating) in a single-stage symmetrical oscillating feedback microreactor have been illustrated elsewhere 16, and the results indicated that the enhancement of mixing and mass transfer performance could be attributed to the flow patterns. To increase the residence time at high throughput, the single stage microreactor was expanded to four stages. In addition, the T-type inlet (Figure 2A) was designed to enhance premixing effect in the inlet section, and asymmetric feedback channels (2 and 3 in Figure 2) were designed to induce unbalanced transverse forces through the two feedback channels. With enhanced internal recirculation and oscillation, there was better mixing and mass transfer performance of FOFM 17. It is worth mentioning that the FOFM operating in passive mode without any moving parts or external energy input is easy to control and cost saving. The stage dimensions are shown in Figure 2C, the inlet width was 0.2 mm, and all channels had the same depth of 1 mm.

FOFM was fabricated by two poly(methyl methacrylate) (PMMA) sample plates (supplied by Guanghe Acrylic Sheet Co., Ltd., Shenzhen, China) using micromachining technology. The two PMMA plates were sealed by hot-pressing sealing techniques.

CFD simulation method

The three-dimensional (3D) flow field and mixing performance in the FOFM were simulated using finite volume method by ANSYS Fluent 2021 software. The continuity, momentum and species convection-diffusion equations can be written as follows 15:

Continuity equation:                                          (1)

Momentum equation:                    (2)

Species convection-diffusion equation:                  (3)

where  is the velocity vector, ρ is the density, t is the time, P is the pressure, and µ is the dynamic viscosity. C and D is the concentration and diffusion coefficient of the species, respectively. Unsteady and incompressible Newtonian liquid conditions were assumed to solve the above equations.

For the 3D flow field and mixing performance simulation, water without dye went into the FOFM through the left inlet passage (mass fraction of water in the left inlet passage was marked as 0), while water with dye went through the right inlet passage (mass fraction of dye in the right inlet passage was marked as 1). Since the concentration of dye was extremely low, the density and dynamic viscosity of both fluids were set as 998.2 kg·m-3 and 1.003×10-3 kg·m−1·s−1, respectively. The diffusion coefficient of dye in water was set as 2.2×10-9 m2·s-1 18.

Constant velocity and constant pressure (P = 0) were imposed for the inlet and outlet boundary conditions, respectively. No-slip boundary conditions were set for all the walls. The time step was set from 1×10-6 to 1×10-4 s according to fluid velocity. Considering the largest Reynolds number explored in this study was smaller than 2300, a laminar flow model was adopted for all the simulations. Pressure-velocity coupling was solved by the Coupled scheme. The PRESTO! scheme was adopted for pressure spatial discretization. The second-order upwind scheme was selected for the spatial discretization of momentum. Simulations were typically considered to converge until the residual fell below 1×10-6.

A commercial software ICEM was used to construct the mesh with hexahedral cells for discretizing the computational domain, and 3D cells with number ranging from 519 640 to 5 059 890 were carefully built. As showed in Figure 3, after mesh-independent check, a mesh consisting of 3 354 450 cells was adopted.

Villermaux-Dushman method

Micromixing is the ultimate stage of mixing to achieve molecular-scale homogeneity. Nevertheless, CFD simulation mainly reflects the mixing process at mesoscale and macroscale. Therefore, to obtain more details at microscale in FOFM, Villermaux-Dushman experiment was adopted to quantify the micromixing quality, which included the following parallel competing reactions 19.

(quasi-instantaneous)             (4)

(fast)                  (5)

(instantaneous equilibrium reaction)           (6)

The Dushman reaction 5 is fast, in the same characteristic time scale of micromixing process, but much slower than the neutralization reaction 4. For perfect mixing conditions, H+ is instantaneously dispersed in the reactive medium and instantaneously consumed by H2BO3− according to reaction 4. Under imperfect mixing conditions, there is local stoichiometric excess of H+ (namely, the H+ amount is larger than that required for H2BO3− neutralization), which reacts with I− and IO3− to yield I2 according to the Dushman reaction 5. The produced I2 further reacts with I− to yield I3− according to reaction 6. The concentration of produced I3− can be easily monitored using a UV-vis spectrophotometer (Cary-100, Agilent) at a characteristic wavelength of 353 nm.

Segregation index Xs was adopted to quantify the micromixing performance of FOFM, and Xs is defined as follows:

(7)

(8)

(9)

where n denotes the number of moles, square brackets “[]” represents the concentration of the species, and the subscript “0” denotes initial state. Qtotal is the total volumetric flow rate of the left inlet (H2SO4 solution) and that of the right inlet (the mixed solution), and Qacid = 0.5Qtotal. Y is the ratio of n(H+) consumed in reaction 5 to the total n(H+). Yst represents the value Y upon complete segregation (i.e., when the mixing process is infinitely slow). Xs = 0 and Xs = 1 indicates that the two fluids are completely mixed and completely segregation, respectively. When the value of Xs is between 0 and 1, there is a partial mix.

Preparation of BaSO4 nanoparticles

Figure 4 displays the schematic of experimental setup for continuous generation of BaSO4 nanoparticles. The experiment was carried out at 301.15–303.15 K. Two precursors (aqueous BaCl2 and Na2SO4 solutions) were pumped into the microreactor using two precise syringes (LSP01-1BH, stroke resolution 0.156 μm, Baoding Longer Precision Pump Co., Ltd., Baoding, China), and Qtotal was set between 10 mL/min and 160 mL/min, and the flow rate ratio was constantly kept at 1. The product was collected in a beaker when the flow approached the steady state conditions. After stirred for another minute, the product was collected by centrifugation and washed twice with water and ethanol. Finally, the produced BaSO4 power was harvested after drying in air at 333.15 K for 24 h. After each experiment, FOFM was immediately and repeatedly rinsed with deionized water to remove residual reactants and prevent clogging.

Characterization

The crystal structure of BaSO4 nanoparticles was characterized by a Bruker D8 Advance X-ray diffractometer with Cu-Kα monochromatized radiation (λ = 0.154 06 nm) at a scan rate of 5°/min. The average size (d) and PSD were observed using a transmission electron microscope (TEM, JEOL JEM-2100Plus).

Results and discussion

CFD simulation

The nucleation and growth steps for the formation of nanoparticles are strongly dependent on supersaturation and have an influence on average particle size and PSD. In a fast reaction, supersaturation is determined by molecular mixing (i.e., micromixing), which is controlled by fluid flow. Therefore, an in-depth knowledge of flow characteristics and mixing behavior in FOFM is essential for robust and controllable synthesis of BaSO4 nanoparticles. In the following sections, the general pressure field is discussed, the fluid oscillating mechanism explained, and the mixing performance quantitatively characterized. It should be noted that the volumetric flow rates of the left inlet were equal to those of the right inlet for all the simulations.

Internal dynamics

A proper knowledge of FOFM internal dynamics can serve as guideline for the design and optimization of FOFM structure targeted for a specific requirement and application. Therefore, the pressure field and flow field (fluid oscillation characteristics) were investigated in this section. Figure 5 depicts the pressure signals and mass flow rates in FOFM feedback channels. As illustrated in Figure 5a, the pressure signals were measured in the middle of left feedback channel of stage I, and the pressure increased with the increase of Qtotal. This is because the mass flow rate in the left channel of stage I increased with the increase of Qtotal, resulting in a larger amount of fluid flowing through the left feedback channels of stage I at a higher flow rate (as showed in Figure 5c). Therefore, the pressure increased with the increase of Qtotal. In addition, the pressure signals (Figure 5a) and mass flow rates (Figure 5c) in the left feedback channel of stage I presented obvious periodical oscillation as Qtotal was larger than 5 mL/min, and the time of one oscillation cycle decreased with the increase of Qtotal. It should be noted that no periodical oscillation was observed as Qtotal was 5 mL/min. This is because almost no fluid could be driven into the left feedback channel, and the mass flow rate was 2.5 × 10-6 kg/s (Figure 5c). Figure 5b describes the change of pressure signals in the middle of left and right feedback channels of different stages. The results reveal that the pressure decreased with the increase of stages, and the pressure in the left channel and right channel presented an alternate change. In addition, based on the results of pressure signals, the oscillation frequency (Figure S1a) and Strouhal number (Figure S1b) were calculated to further characterize the oscillating performance of FOFM, and the details are presented in the Supporting Information.

As discussed in the part related to pressure field, obvious periodic oscillations could be achieved in FOFM as Qtotal was larger than 5 mL/min. To further describe the mixing process, velocity contours (Figure S2a) and streamline map (Figure S2b) within a single oscillation cycle at the condition of Qtotal = 15 mL/min was used to reveal the fluid oscillation mechanism in FOFM, and one can conclude that the recirculation flow through the feedback channels could facilitate the growth of vortex in the mixing chamber, which could increase the flow resistance on the corresponding side, and with pushing of inlet fluid tending to the other side, a similar phenomenon happened. As a result, there was the occurrence of fluid oscillation, and the details of the fluid oscillation process were described in the Supporting Information.

Concentration field

To reveal the relationship between flow field and concentration (mass fraction) field in FOFM, we investigated the concentration field. The mass fraction contours of middle cross section of FOFM at different total volumetric flow rates are displayed in Figure 6. The mass fraction of the left inlet is marked as 0 (blue fluid), while that of the right 1 (red fluid). In other words, a mass fraction of 0.5 means perfect (homogenous) mixing of the two fluids, while 0 and 1 mean no mixing. Generally, the mass fraction of the mixed fluid is between 0 and 1 during a mixing process. Figure 6 shows that more homogenous mixing could be achieved with the increase of stages (e.g., from stage I to stage IV) at the same Qtotal, especially for stage II where homogenous mixing is larger than that of stage I. In addition, at a Qtotal of 7.5 mL/min, despite good mixing from stage II to stage IV, small KAM (Kolmogorov-Arnold-Moser) toris 20 (marked by red circles) was observed in the lower part of the mixing chamber. It is well known that KAM tori can prevent inside mix of materials, resulting in a lowering of mixing efficiency 16. In addition, the area of KAM toris decreased with the increase of Qtotal, and completely disappeared as Qtotal was larger than 10 mL/min (Figure 6d and Figure 6e).

Figure 7 describes the mass fraction contours of different longitudinal sections (S0–S4 showed in Figure 7a) of FOFM at different total volumetric flow rates. The results reveal that better homogenous mixing could be achieved in S1 than in S0 across the total volumetric flow rates investigated. In other words, the mixing mainly took place in the stage sections, unlike that of the T-type inlet system. This is because the generated vortex, recirculation, and oscillating flow could induce chaotic advection mixing in stage I, and the fluid could be stretched, folded, and compressed, resulting in reduction of mass transfer distance and increase of area available for diffusion. Consequently, a better mixing was achieved in S1 than in S0. In addition, when Qtotal was larger than 5 mL/min, good mixing could be achieved from S1 to S4 (Figure 7c to Figure 7f), and Qtotal had little effect on the mass fraction distribution. It should be noted that much better mixing could be achieved in S1–S4 at Qtotal ≥ 7.5 mL/min than at Qtotal = 5 mL/min. For example, much more uniform mass fraction distribution in S1 was achieved at Qtotal = 15 mL/min (Figure 7e) than at Qtotal = 5 mL/min (Figure 7b). This is because much more intense chaotic advection mixing could be induced owing to the stronger unique secondary flows (i.e., vortex, recirculation, and oscillation) in stage I at Qtotal = 15 mL/min than at Qtotal = 5 mL/min. Therefore, a better mixing could be achieved in S1 at Qtotal = 15 mL/min than at Qtotal = 5 mL/min.

Figure S3 describes the mass fraction contours within a single oscillation cycle in stage I at Qtotal = 15 mL/min, and they were like to the velocity contours in Figure S2a, where obvious fluid oscillation could be detected. In addition, we adopted a mixing index (m) to quantitatively characterize the mixing performance in FOFM (Figure S4 and Supporting Information), the results show that m increased with the increase of stages at same Qtotal and increased with the increase of Qtotal. Moreover, almost complete mixing could be achieved at the outlet (S4) as Qtotal was larger than 5 mL/min.

Microscale mixing performance

According to the Villermaux-Dushman method, H2SO4 was diluted to 0.03 mol/L, and the mixed solution was with 0.1818 mol/L H3BO3, 0.0909 mol/L NaOH, 0.0116 mol/L KI and 0.00233 mol/L KIO3. The effects of Qtotal and inlet structure on micromixing performance were investigated with the volumetric flow rates for both inlets kept the same in all experiments. As depicted in Figure 8a, the segregation index (Xs) of the T-type FOFM was smaller than that of the Y-type FOFM at same Qtotal. This is because the two fluids at the T junction collided head-on, achieving better premixing than that at the Y junction. In addition, micromixing quality became better with the increase of Qtotal, because the mixing could be obviously enhanced owing to the vortex, recirculation, and oscillating flow at a higher flow rate 16. It is worth noting that when Qtotal was 80 mL/min, the Xs value of T-type and Y-type FOFM was 1.27×10-4 and 1.81×10-4, respectively, suggesting almost perfect micromixing.

We estimated the mixing time by the incorporation model 21, where the limit fluid was dilute sulfuric acid. In the experiment, the limit fluid was divided into aggregates which were constantly invaded by the surrounding alkaline fluid containing iodide and iodate. The characteristic time of incorporation, tm, was assumed to be equal to the micromixing time 21, and the volume of the aggregate grows according to Equation 10：

(10)

where V2 is the volume of acid aggregate, V20 is the initial volume of acid aggregate, and g(t) is the incorporation function as follows:

or                 (11)

where τm is the characteristic micromixing time. The concentration of j species can be calculated through Equation 12:

(12)

where subscript 10 represents the surrounding fluid and Rj is the net production rate of j species (j = H2BO3-, H+, I-, IO3-, I2 or I3-) for reaction 4, 5 and 6. As  (showed in Equation 11), Equation 12 can be transformed to Equation 13.

(13)

The initial concentrations of the species j are constant, and Equation 13 can be solved through MATLAB using Runge-Kutta method. The value of time step was fixed at 1×10-9 s, and the iteration ended when H+ was completely consumed. Figure 8b shows the MATLAB simulation results of the mixing time changing with the segregation index, and the relationship could be fitted as Equation 14.

(14)

According to Equation 14 and based on the results of Villermaux-Dushman experiments, the mixing time could be calculated. As showed in Figure 8c, the mixing time of T-type FOFM was shorter than that of Y-type FOFM at same Qtotal (viz. same Reynolds number), which was consistent with the result of segregation index. The mixing time of T-type FOFM decreased from 1×10-2 to 5×10-5 s as Qtotal increased from 7 to 80 mL/min. This is because the intensity of unique secondary flows (i.e., vortex, recirculation and oscillating flow) was enhanced with the increase of Qtotal; consequently, the mixing time decreased distinctly owing to the obvious decrease of molecular diffusion distance.

Direct precipitation through batch method

To demonstrate the unique outcome of using the designed microreactors, BaSO4 was also prepared by co-precipitation through batch method in a beaker. With respect to the batch mode, the concentrations of two reactants (aqueous BaCl2 and Na2SO4 solutions) were both 0.6 mol/L. BaCl2 solution was added into Na2SO4 solution dropwise under magnetic stirring (500 rpm), and after the addition, the mixture was magnetically stirred for another minute. The subsequent procedures for centrifugation, washing and drying of the products were consistent with those of flow mode. As indicated in Figure 9, the BaSO4 nanoparticles prepared by the batch method was relatively large (d = 248 nm) and uneven in terms of size distribution (σg = 1.92). This is because the process for the generation and precipitation of BaSO4 nanoparticles involves steps of nucleation, crystal growth and aggregation, and these steps are sensitive to fluid mixing and finish in an extremely short time. In a beaker, it is difficult to achieve homogeneous mixing of reactants down to molecular level before reaction, and hence the large size and wide PSD.

Microreactor method

First, both the T-type and Y-type FOFM were selected to study the effect of flow rates and inlet structure on the prepared BaSO4 nanoparticles with Qtotal ranging from 10 to 160 mL/min. The concentrations of BaCl2 and Na2SO4 solutions were both 0.1 mol/L, and the flux ratio for both reactants was 1. Figure 10 shows the XRD pattern of the BaSO4 nanoparticles produced in T-type FOFM at different total volumetric flow rates. The XRD peaks were consistent with those of the BaSO4 standard JCPDS card (No. 24-1035), confirming that pure BaSO4 nanoparticles were successfully obtained. The crystal size was calculated using the Scherrer formula (see Supporting Information), and the results indicate that the average size dXRD decreased from 72 to 26 nm as Qtotal increased from 10 to 160 mL/min (Figure 10b).

Figure 11 depicts the TEM images of the BaSO4 nanoparticles produced by T-type FOFM. All the nanoparticles were found to be small (26–109 nm) and had a narrow PSD with the geometric standard deviation σg in the range of 1.22–1.43. In addition, the crystal size became smaller and PSD narrower as Qtotal increased. This phenomenon can be explained as follows: Based on the above results of CFD simulation, three mixing mechanisms including vortex, recirculation and oscillation could be achieved in FOFM when Qtotal was larger than 5 mL/min. The three mixing mechanisms could distinctly enhance the lateral turbulence of liquids for efficient chaotic advection mixing. Therefore, the intensity of chaotic advection mixing increased with the increase of Qtotal. As such, smaller average particle size and narrower PSD could be achieved at flow rates higher than 5 mL/min. Noted that an average particle size of 26 nm with narrow PSD (σg = 1.22) could be achieved at Qtotal = 160 mL/min, and the actual particle production rate could reach 105.5 g/h. The production rate achieved in FOFM is higher than that in ordered lamination flow microreactor (9.32 g/h) 22 and much higher than that in segment flow microreactors (7×10-3 g/h) 10. In addition, compared with the crystal size calculated based on XRD information, the average size measured by TEM data was larger when Qtotal was in the range of 10–40 mL/min, whereas in the range of 80–160 mL/min, the two are rather similar (Figure 10b and Figure 11). These phenomena may be caused by system reasons. The particle sizes calculated based on the Scherrer formula are determined by the width at half-maximum peak intensity, but compositional and geometric inhomogeneity can introduce peak broadening 23. Therefore, owing to particle geometric inhomogeneity, the average particle sizes calculated based on TEM images were larger than those calculated using the Scherrer formula in the Qtotal range of 10–40 mL/min. In addition, the geometric shape of particles became more orderly with the increase of Qtotal, especially at large flow rates (i.e., Qtotal = 60–160 mL/min), which could significantly reduce the peak broadening effect, thereby the XRD calculation results are closer to those of TEM. A similar phenomenon was reported by Huang et al. 24.

Furthermore, the TEM results indicate that the nanoparticles prepared in T-type FOFM were smaller and had a narrower PSD than those prepared in Y-type FOFM (Figure S5 and Supporting Information). Accordingly, the T-type FOFM was adopted to investigate the effect of precursor concentration and precursor concentration ratio R (i.e., the concentration of BaCl2 divided by the concentration of Na2SO4) on the particle size and PSD of BaSO4 (Figure S6, Figure S7 and Supporting Information). The results indicate that the crystal size became smaller, and the PSD narrower with the increase of precursor concentration. In addition, compared with the batch method (Figure 9), smaller crystal size and narrower PSD could be achieved by T-type FOFM (Figure S6c and f) owing to chaotic advection mixing of high efficiency. Furthermore, as R < 3, the average size and non-uniformity of BaSO4 nanoparticles slightly reduced with the increase of R (Figure S7).

Comparison with other microreactors

Table 1 lists the size and total throughput of T-type FOFM and other microreactors. It can be found that the size range of the synthesized BaSO4 nanoparticles in this study is 23–109 nm, which is smaller than that reported in most literatures. In addition, the largest total throughput in this work (160 mL/min) is 4-fold that in laminar flow microreactors (40 mL/min) and is about 16-fold that in segment flow microreactors (9.946 mL/min). Therefore, it is demonstrated that FOFM may be ideal for producing high quality small-sized BaSO4 nanoparticles with high throughput.

Conclusions

Four-stage asymmetric oscillating feedback microreactor (FOFM) was designed based on the concept of chaotic advection mixing. For the first time, the flow characteristics and mixing mechanism of FOFM were studied by computational fluid dynamics. The results reveal that unique flow patterns including vortex, recirculation and oscillation could be induced as the total volumetric flow rate (Qtotal) is larger than 5 mL/min, leading to enhanced chaotic advection mixing. The mixing index increases with the increase of Qtotal, and near-complete mixing could be achieved at the outlet of FOFM when Qtotal is larger than 7.5 mL/min.

The micromixing efficiency was evaluated by Villermaux-Dushman experiments. The results show that the segregation index and micromixing time decrease with increase of Qtotal, implying better micromixing efficiency. In addition, the T-type FOFM has better micromixing efficiency than Y-type FOFM. On equal Qtotal basis, the BaSO4 nanoparticles produced by the former are smaller in size and narrower in particle size distribution (PSD) than those produced by the latter. In addition, the crystal size is smaller and PSD narrower with the increase of total volumetric flow rates, as well as the enlargement of precursor concentration. Overall, the acquired results deepen our understanding on the effects of chaotic mixing characteristics on the size and PSD of BaSO4 nanoparticles. Using the designed passive asymmetric oscillating feedback microreactor, large throughput synthesis of high quality BaSO4 nanoparticles can be achieved. The designed microreactors are apt for industrial production of BaSO4 as well as other nanoparticles for a wide range of targeted applications.

Acknowledgements

This project was financially supported by the National Natural Science Foundation of China (Grants 21725602 and 22108066), the Innovative Research Groups of Hunan Province (Grant 2019JJ10001), and the Science and Technology Planning Project of Hunan Province (Grant 2019RS3010). CT Au thanks HNU for an adjunct professorship.

References

1.	Leng HJ, Wang X, Niebur GL, Roeder RK. Synthesis of a barium sulfate nanoparticle contrast agent for micro-computed tomography of bone microstructure. Indiana: John Wiley & Sons, Inc., 2012.

2.	Petrova A, Hintz W, Tomas J. Investigation of the precipitation of barium sulfate nanoparticles. Chemical Engineering & Technology. 2008;31:604–608.

3.	Du L, Wang YJ, Lu YC, Luo GS. Process intensification of BaSO4 nanoparticle preparation with agitation of microbubbles. Powder Technology. 2013;247:60–68.

4.	Ying Y, Chen GW, Zhao YC, Li SL, Yuan Q. A high throughput methodology for continuous preparation of monodispersed nanocrystals in microfluidic reactors. Chemical Engineering Journal. 2008;135:209–215.

5.	Yang M, Luo LM, Chen GW. Microfluidic synthesis of ultrasmall Co nanoparticles over reduced graphene oxide and their catalytic properties. AIChE Journal. 2020;66: e16950.

6.	Li SW, Xu JH, Wang YJ, Luo GS. Liquid-liquid two-phase flow in pore array microstructured devices for scaling-up of nanoparticle preparation. AIChE Journal. 2009;55:3041–3051.

7.	Hessel V, Hardt S, Löwe H, Schönfeld F. Laminar mixing in different interdigital micromixers: I. Experimental characterization. AIChE Journal. 2003;49:566–577.

8.	Kockmann N, Kastner J, Woias P. Reactive particle precipitation in liquid microchannel flow. Chemical Engineering Journal. 2008;135:S110–S116.

9.	Li SW, Xu HH, Wang YJ, Luo GS. Controllable preparation of nanoparticles by drops and plugs flow in a microchannel device. Langmuir. 2008;24:4194–4199.

10.	Du L, Li Y, Gao RM, Yin JB, Shen C, Wang YJ, Luo G. Controllability and flexibility in particle manufacturing of a segmented microfluidic device with passive picoinjection. AIChE Journal. 2018;64:3817–3825.

11.	Su YH, Chen GW, Kenig EY. An experimental study on the numbering-up of microchannels for liquid mixing. Lab on a chip. 2015;15:179–187.

12.	Hossain S, Fuwad A, Kim KY, Jeon TJ, Kim SM. Investigation of mixing performance of two-dimensional micromixer using tesla structures with different shapes of obstacles. Industrial & Engineering Chemistry Research. 2020;59:3636–3643.

13.	Xie TL, Chen MX, Xu C, Chen J. High-throughput extraction and separation of Ce(III) and Pr(III) using a chaotic advection microextractor. Chemical Engineering Journal. 2019;356:382–392.

14.	Stroock AD, Dertinger SKW, Ajdari A, Mezic I, Stone HA, Whitesides GM. Chaotic mixer for microchannels. Science. 2002;295:647–651.

15.	Yang M, Yang L, Zheng J, Hondow N, Bourne RA, Bailey T, Irons G, Sutherland E, Lavric D, Wu KJ. Mixing performance and continuous production of nanomaterials in an advanced-flow reactor. Chemical Engineering Journal. 2021;412:128565.

16.	Xie TL, Xu C. Numerical and experimental investigations of chaotic mixing behavior in an oscillating feedback micromixer. Chemical Engineering Science. 2017;171:303–317.

17.	Xu C, Chu YF. Experimental study on oscillating feedback micromixer for miscible liquids using the Coanda Effect. AIChE Journal. 2015;61:1054–1063.

18.	Sun YL, Sun MH, Cheng WD, Ma CX, Liu F. The examination of water potentials by simulating viscosity. Computational Materials Science. 2007;38:737–740.

19.	Asano S, Maki T, Mae K. Evaluation of mixing profiles for a new micromixer design strategy. AIChE Journal. 2016;62:1154–1161.

20.	Ottino JM. The kinematics of mixing: stretching, chaos, and transport. Cambridge: Cambridge university press; 1989.

21.	Yang HJ, Chu GW, Zhang JW, Shen ZG, Chen JF. Micromixing efficiency in a rotating packed bed: Experiments and simulation. Industrial & Engineering Chemistry Research. 2005;44:7730–7737.

22.	McCarthy ED, Dunk WA, Boodhoo KV. Application of an intensified narrow channel reactor to the aqueous phase precipitation of barium sulphate. Journal of Colloid and Interface Science. 2007;305:72–87.

23.	Yao MH, Baird RJ, Kunz FW, Hoost TE. An XRD and TEM investigation of the structure of alumina-supported ceria–zirconia. Journal of Catalysis. 1997;166:67–74.

24.	Huang C, Wang YJ, Luo GS. Preparation of highly dispersed and small-sized ZnO nanoparticles in a membrane dispersion microreactor and their photocatalytic degradation. Industrial & Engineering Chemistry Research. 2013;52:5683–5690.

25.	Sen N, Koli V, Singh KK, Panicker L, Sirsam R, Mukhopadhyay S, Shenoy KT. Segmented microfluidics for synthesis of BaSO4 nanoparticles. Chemical Engineering and Processing-Process Intensification. 2018;125:197–206.

26.	Su YF, Kim H, Kovenklioglu S, Lee WY. Continuous nanoparticle production by microfluidic-based emulsion, mixing and crystallization. Journal of Solid State Chemistry. 2007;180:2625–2629.

27.	Jeevarathinam D, Gupta AK, Pitchumani B, Mohan R. Effect of gas and liquid flowrates on the size distribution of barium sulfate nanoparticles precipitated in a two phase flow capillary microreactor. Chemical Engineering Journal. 2011;173:607–611.