Supporting Information

Fig. S1 (a) Melting and (b) cooling curves of BBB/olive oil mixtures at 2, 4, 6, 8, 10, 20, 30, 40, 50, 60, 70, 80, 90, and 100 wt.% BBB from the bottom to the top of each figure

Fig. S2 Melting curves of oleofoams at (a) 60 min and (b) 120 min

Fig. S3 (a) Strain, (b) frequency, and (c) flow sweeps for oleofoams containing 6, 10, and 20 wt.% BBB

Fig. S4 Temperature sweep curves (a cycle between 0 C and 80 C) for oleofoams at BBB concentrations of (a) 6 wt.%, (b) 10 wt.%, and (c) 20 wt.%

Fig. S5 Photomicrographs of oleofoams with 10 wt.% BBB at (a) 20 C and (b) 40 C under polarized light (left, 20X) and bright field (right, 20X)

Table S1 Thermal parameters (Tm and Hm) for oleofoams with different BBB concentrations at 60 min and 120 min. Values are given as means ± SD from triplicate measurements.

| 60 min. |  |  |  |  |
| --- | --- | --- | --- | --- |
| Sample | Temperature (C) |  |  | H (mJ/mg) |
|  | onset | peak top | offset |  |
| BBB 4 wt.% | 43.2±1.86 | 51.01±0.19 | 54.93±0.15 | 5.79±0.26 |
| BBB 6 wt.% | 45.40±0.82 | 53.26±0.40 | 56.62±0.01 | 9.56±1.33 |
| BBB 8 wt.% | 46.55±1.23 | 54.48±0.41 | 57.75±0.17 | 14.84±1.14 |
| BBB 10 wt.% | 46.76±1.50 | 55.59±0.10 | 58.73±0.24 | 16.9±1.05 |
| BBB 20 wt.% | 52.22±1.75 | 59.06±0.09 | 61.72±0.19 | 40.08±2.05 |
| 120 min. |  |  |  |  |
| Sample | Temperature (C) |  |  | H (mJ/mg) |
|  | onset | peak top | offset |  |
| BBB 4 wt.% | 43.68±1.71 | 51.09±0.17 | 54.91±0.09 | 7.08±0.72 |
| BBB 6 wt.% | 45.04±0.74 | 52.96±0.06 | 56.37±0.18 | 9.52±0.95 |
| BBB 8 wt.% | 46.86±1.46 | 54.44±0.11 | 57.54±0.33 | 14.83±1.78 |
| BBB 10 wt.% | 47.31±0.69 | 55.54±0.05 | 58.29±0.38 | 22.93±0.98 |
| BBB 20 wt.% | 53.54±2.18 | 59.00±0.20 | 61.21±0.21 | 39.59±3.55 |