Synthesis and characterization of Oil Palm Empty Fruit Bunch Activated Carbon for Battery Electrodes

Yunita Trianaa,f, Sintya Efrianaa,f, Rahmat Pratamaa,f, Sukma Wina Anjania,f, Masato Tominagab, Fredy Kurniawanc, Widi Astutid, Andi Idhil Ismaile

aDepartment of Materials and MetallurgicaleEngineering, Institut Teknologi Kalimantan, Balikpapan, Indonesia

bDepartment of Chemistry and Applied Chemistry, Saga University, Saga, Japan

cDepartment of Chemistry, Institut Teknologi Sepuluh Nopember, Surabaya, Indonesia

dResearch Center for Mining Technology, National Research, and Innovation Agencye(BRIN), Lampung, Indonesia

eDepartment of Mechanical Engineering, Institut Teknologi Kalimantan, Balikpapan, Indonesia

fElectrochemistry ResearcheCenter, Institut Teknologi Kalimantan, Balikpapan, Indonesia

Corresponding author

Yunita Triana: nita@lecturer.itk.ac.id

Abstract

In this work, the synthesis and characterization of the oil palm empty fruit bunch (OPEFB) activated carbon were studied for battery electrodes application. First, chemical activation carried out by variation concentrations and immersion time of NaOH and KOH. Then, the physical activation was studied using variation of activation temperature. The characterization of OPEFB activated carbon investigated on the surface morphology, surface area and the capacitance specific. Moreover, we designed, assembled and measured the electricity potential of the battery prototype. The activator solution of KOH 2 M showed the highest surface area of 354.25 m2g-1, capacitance specific of 116.78 F.g-1, and potential of 1.17 V. Furthermore, the optimal immersion time was 18 hours with the highest surface area of 380.28 m2g-1, capacitance specific of 96.57 F g-1, and the potential of 1.05 V. Finally, the optimal activation temperature is 900oC which showed with the highest surface area 334.28 m2g-1, capacitance specific of 96.41 F.g-1, and the potential of 1.12 V. Based on this report, OPEFB activated carbon can be used as the battery electrodes due to the carbon properties.

Keywords: Activated Carbon; Battery; Palm bunch

- Introduction

Oil palm empty fruit bunch (OPEFB) waste reaches around 22.75 million tons per year in the palm oil industry [1]. In fact, it has been used in limited applications such as fertilizer, catalyst, water purifier, and metal removal [2]. However, it needs a longer time, procedure, and high cost. On the other hand, OPEFB contains high levels of phenolic compounds such as lignocellulose (46% cellulose, 16.49% hemicellulose, and 22.84% lignin) [3]. Recently, it attracted attention to produce OPEFB into activated carbon [4], [5], [6]. The activated carbon has been used widely for water purification [7], electronics field [8], catalyst [9] due to the adsorption properties [10].

The activated carbon has high adsorption performance compared to other adsorbents [11]. To increase the adsorption properties of activated carbon, an activation process can be carried out which is divided into three types including chemical activation, physical activation, and a combination of both [12]. Chemical activation is carried out using chemical substances such as H3PO4, KOH, and NaOH [13]. The process of chemical and physical for carbon activations are the important key to increase its porosity quality and quantity of the activated carbon. Previous works showed activated carbon from different biomass such as neem seed resulted in surface area at 246 m2g-1 [14], biomass from bamboo waste resulted in highest surface area at 408 m2g-1 [15]. In our previous study, oil palm frond activated carbon has been investigated by using an activator of NaOH 1 M with 30 hours of immersion time showed the highest surface area at 336 m2g-1 and the electrical potential of 0.902 V [16].

Therefore we continue our work by using NaOH and KOH as the activators to improve the OPEFB activated carbon in this study. The chemical activation of OPEFB carbon was activated through concentration and immersion time by using the activators. Furthermore, the physical activation was optimized by using the temperature variation. The characterization properties of OPEFB activated carbon was investigated on the surface morphology and surface area. Finally, we designed, assembled and measured the electric capacity of the battery prototype.

- Experimental

2.1 Materials

The materials are oil palm empty fruit bunch (OPEFB) which originated from East Kalimantan, Indonesia. NaOH and KOH, HCl, H2SO4, NaCl, pH indicator, PVA, K2CO3, demineralized water, copper plate, and polymethyl methacrylate (PMMA) were purchased from Merck.

2.2 Synthesis of OPEFB to carbon

Pre-activated of carbon OPEFB was prepared by following the previous report [17], [18]. OPEFB were cut into 1-2 cm and dried in a drying oven at 105oC for 2 hours to remove the moisture. Carbonization was completed after calcination in a muffle furnace at 400°C for 1 hour. Finally, the carbon was crushed and sieved with a 300-mesh screen.

2.3 Procedure of activated carbon

The chemical activation of OPEFB was influenced by a mixture of NaOH and KOH solutions with the variation of concentration were 0-2; 0.5-1.5; 1-1; 1,5-0.5; 2-0 M, and the immersion time of 12, 18, 24, 30, and 36 hours. The carbon that has been chemically activated, continued by physical activation with the variations of temperature of 700, 750, 800, 850, and 900oC. The activated carbon was washed with HCl and demineralized water to achieve a neutral pH. The activated carbon was then dried in an oven at 105°C for 24 hours to remove any remaining water.

2.4 Characterization of OPEFB activated carbon

The functional group of OPEFB carbon before activation was studied using Fourier Transform Infra-Red (FTIR) with Bruker Alpha II. The surface morphology and elemental composition of the activated carbon were analyzed using Scanning Electron Microscopy-Energy Dispersive X-Ray (SEM-EDX) with a Phenom Pro X instrument. The surface area and porosity were measured by nitrogen adsorption using the Quantachrome Surface Area Analyzer/Brunauer Emmett-Teller (SAA/BET) Nova Touch LX-4. The capacitance was measured using Autolab and Nova 2.1.6 software.

2.5 Development of battery prototype

The prototype component consists of a protective casing by using poly methyl methacrylate (PMMA) sheet, current collector of copper plate, electrodes of OPFEB activated carbon and electrolyte of PVA-K2CO3. The initial stage of preparing the electrode sheet involves the creation of an activated carbon slurry. The slurry is different in two parts for anode and cathode. The cathode is made by combining activated carbon with distilled water to form a homogeneous mixture. The anode carbon was mixed with NaCl solution to make a different potential from the cathode. Next, the polymer electrolyte is made by mixing K2CO3 with PVA by dissolving 0.7 g of PVA and 0.3 g of K2CO3 in 20 mL of distilled water, then stirring and heating the solution until it reaches 80°C, transforming the PVA- K2CO3 into a solid gel. Finally, all components are assembled according to the design shown in Fig. 1 and was tested for its voltage using DT830B Multimeter.

Fig. 1. Design of the battery prototype

- Results and discussion

3.1 Functional group of OPEFB carbon

The carbonized OPEFB exhibits a noticeably black and uniform size around 8 – 44 nm, primarily due to the release of volatile compounds from the particles. The pyrolysis process involves reactions that facilitate this transformation:

| CxHyOn (s) + O2 (g) → C (graphite) + CO (g) + H2O (g) | (1) |
| --- | --- |

The peaks as shown in Table 1, confirmed the presence of the hydroxyl group was the result of the reaction between NaOH and KOH with carbon on the surface [8], [19]. The C-O and C-H which was associated with the alkane bond [20], the form of alcohol, acid, phenolic, eter, and/or ester functional group [21], and the influence of temperature resulting alteration on the particle surface and impact on the release of oxygen functional group content.

Table 1. Functional groups of OPEFB carbon by FTIR

| Wavenumber (cm-1) | Functional group | Reference |
| --- | --- | --- |
| 1045 | C-O | (Ali et al., 2020) |
| 729 | C-H | (Ali et al., 2020) |
| 701 | C-H | (Ali et al., 2020) |
| 668 | C-H | (Harimu et al., 2022) |
| 628 | C-H | (Harimu et al., 2022) |

At a temperature of 240-360oC, cellulose degradation, hemicellulose at 200-260oC, and lignin at 280-500oC. During the initial reaction of lignin decomposition, the back color of the smoke, thin and white, is characterized by the gradual disappearance of the smoke [22]. Degradation at low temperatures produces temperatures low tar and char but more volatile. This caused the closed access to porosity [23].

3.2 Analysis of the surface morphology and area of OPEFB carbon

The morphology and EDXlspectrum of carbon before activation is illustrated in Fig. 2. Physically and chemically during the composition before activation Table 2, changes can be seen that physically significant differences in OPEFB carbon which were originally in the form of brownish fiber turned into black particles after being sieved using 300 mesh and visually observed using SEM. In Fig. 2, it can be seen that the pores are still covered with many substances causing the absorption quality of the particles to be low as a result closed access for ions to enter the carbon surface.

Fig. 2. Morphology of OPEFB carbon

Fig. 3. Isotherm graph of OPEFB carbonization

Fig. 3. showed the decreased nitrogen adsorption capacity, indicating the access of nitrogen being blocked to be adsorbed to the pores in carbon. This obstruction complicates the straightforward determination of pore size distribution based on the graph. [24].

Table 2. Composition of OPEFB carbon before activation

| Element | Elemental Content (%) |
| --- | --- |
| Carbon | 66.37 |
| Oxygen | 33.63 |

3.3 Comparison analysis of the surface morphology of OPEFB activated carbon

The composition of the activated carbon samples activated by variations of concentration are summarized in Table 3. From the table, the trend showed an increase of carbon content and a decrease of oxygen which influenced the morphology of pores after activation as shown in Fig. 4. Activator solution, immersion time, and temperature to activate the carbon forced the release of gas and impurities such as oxygen, nitrogen, carbon dioxide, and other elements from the carbon and produced more porosity.

Table 3. Composition of activated carbon sample concentration variations

| Sample | Carbon (%) | Oxygen (%) |
| --- | --- | --- |
| KA-0-2 | 84.47 | 15.53 |
| KA-0.5-1.5 | 78.62 | 20.91 |
| KA-1-1 | 82.16 | 17.84 |
| KA-1.5-0.5 | 79.09 | 21.38 |
| KA-2-0 | 77.56 | 22.44 |

As the porosity increased, the area for the nitrogen to be adsorbed relatively increased [25]. Table S1 compares the elemental compositions of activated carbon at different NaOH and KOH concentrations, revealing that the highest percentages were 84.47% carbon and 15.53% oxygen.

| (A) | (B) |
| --- | --- |
| (C) | (D) |
| (E) |  |

Fig. 4. Morphology of activated carbon concentration variation, (a) KA-2-0, (b) KA-1.5-0.5, (c) KA-1-1, (d) KA-0.5-1.5, (e) KA-0-2

From Table 4, the oxygen element contained in this activated carbon is the oxygen element that comes from raw materials left behind by the process of incomplete carbonization. When using a mixture of NaOH and activator KOH shows an increase in the amount of carbon when compared by only using the NaOH activator.

Table 4. Composition of activated carbon sample immersion time variations

| Sample | Carbon (%) | Oxygen (%) |
| --- | --- | --- |
| KA-12 | 85.97 | 14.03 |
| KA-18 | 88.33 | 11.67 |
| KA-24 | 86.61 | 13.39 |
| KA-30 | 86.15 | 13.85 |
| KA-36 | 86.11 | 13.89 |

The highest carbon content was found in the use of 2M KOH activator. KOH compound as an activator is considered better than other chemicals because it can enrich the formation of OH groups on the carbon surface, producing more micropores [26].

| (A) | (B) |
| --- | --- |
| (C) | (D) |
| (E) |  |

Fig. 5. Morphology of activated carbon concentration variation, (A) KA-12, (B) KA-18, (C) KA-24, (D) KA-30, (E) KA-36

The carbon that was activated by 18 hours of activation showed the highest result in containing carbon 88.33% shown in Fig. 5(B). This matter is caused by the longer immersion or activation time on carbon, The absorption capacity of carbon will be less than optimal due to the pores in the carbon. Where immersion for too long will expand the pores in the carbon continuously so that the small pores will unite into pores larger ones this will make the pores wider but it was damaged due to excessive erosion by the activator [27].

| (A) | (B) |
| --- | --- |
| (C) | (D) |
| (E) |  |

Fig. 6. Morphology of activated carbon concentration variation, (A) KA-700, (B) KA-750, (C) KA-800, (D) KA-850, (E) KA-900

According to [28], if it is related to the morphology shown in Fig. 6 of the pores formed, the activation process at high temperatures will create pores that can release impurities and re-form the carbon matrix which will later be applied as an electrode. This phenomenon has been studied by [29] which shows that temperatures of more than 700oC will evaporate non-carbon components from particles such as water, oxygen and nitrogen content as visualized by the test results, and 900oC is the most optimal temperature to evaporate the impurities as summarized in Table 5.

Table 5. Composition of activated carbon sample temperature variations

| Sample | Carbon (%) | Oxygen (%) |
| --- | --- | --- |
| KA-700 | 69.91 | 30.09 |
| KA-750 | 70.72 | 29.28 |
| KA-800 | 74.77 | 25.23 |
| KA-850 | 75.52 | 24.48 |
| KA-900 | 81.47 | 18.53 |

3.4 Surface area comparison analysis

According to Table 6, the greatest adsorption of nitrogen gas on activated carbon surfaces occurred when activated with a 2 M KOH concentration. Therefore, activated carbon produced using 2 M KOH demonstrated the highest pore surface area and absorption capacity. According to IUPAC standard, the isothermal curve type of the sample combines types IV and VI [30]. Although the diameter pore size is 3.02 - 2.54 nm, indicates that these samples possess mesoporous structure simultaneously. This result is very suitable because the mesopore can increase the electro absorption capacity, and the fast transport of electrons and ions results in an increased power density [31].

The smaller radius of the carbon pores causes an increase in surface area along with an increase in the amount of porosity that will form in one activated carbon particle [32]. Apart from that, the curve is also categorized as type VI where the adsorption/desorption pattern does not form a smooth line, which means the pore size in the sample is not uniform [33]. The ratio in the chemical activation process and the temperature used is considered to influence carbon absorption capacity [34].

Table 6. Activated carbon surface area variation concentration

| Sample | Surface area (m2g-1) |
| --- | --- |
| KA-2-0 | 118.25 |
| KA-1.5-0.5 | 149.75 |
| KA-1-1 | 301.50 |
| KA-0.5-1.5 | 281.52 |
| KA-0-2 | 354.25 |

So, the absorption capacity of activated carbon is higher. The highest surface area obtained at KA-0-2 concentration variations is 354.25 m2g-1 while the lowest surface area was obtained in the KA 2-0 variation, at 118.25 m2g-1. There is a mixture of concentration variations on the train 1.5 – 0.5 and KA-1-1 indicating an increase in the surface area of 149.75 m2g-1 increasing to 301.50 m2g-1. However, there was a decrease in surface area at varying KA concentrations from 0.5 - 1.5 to 281.52 m2g-1, this shows that the concentration of the NaOH and KOH activator mixture has reached the optimal point because a further increase in concentration can cause a decrease in surface area due to excessive erosion

Table 7. Activated carbon surface area variation immersion time

| Sample | Surface area (m2g-1) |
| --- | --- |
| KA-12 | 235.56 |
| KA-18 | 380.28 |
| KA-24 | 330.64 |
| KA-30 | 200.18 |
| KA-36 | 194.79 |

The lowest surface area was obtained in the KA-36-hour variation with a value of 194.79 m2g-1, followed by the KA-30 Hour variation of 200.18 m2g-1, the KA-12 Hour variation of 235.56 m2g-1, the KA-24 Hour variation of 330.64 m2g-1 and the KA-18 Hour variation of 380.28 m2g-1 which has the highest surface area. The duration of carbon immersion significantly impacts the surface area (Table 8)due to prolonged interaction between the carbon and the activating agent. As the contact time increases, a higher number of volatile substances is released. These substances have the tendency to cover and block the carbon pores. It ensures a balance between adequate activation and preventing pore blockage, which is essential for maintaining the desirable properties of the carbon material, such as high surface area and enhanced adsorption capacity [35]. This is supported by [36], that the more volatile substances released on carbon, the surface area of ​​the carbon will increase.

Table 8. Activated carbon surface area variation temperature

| Sample | Surface area (m2g-1) |
| --- | --- |
| KA-700 | 170.66 |
| KA-750 | 319.64 |
| KA-800 | 310.19 |
| KA-850 | 318.08 |
| KA-900 | 334.28 |

The surface area produced in the KA-700 sample is activated carbon with the lowest surface area, at 170.66 m2g-1, and the active carbon with the highest surface area is shown in the KA-900 sample of 334.28 m2g-1. The surface area value at temperatures of 700 and 900oC shows a significant increasing trend, then at temperatures of 750-850oC it shows an increasing and decreasing trend but is not too significant where this phenomenon is influenced by N2 absorption [37] that an increase in activation temperature indicates the formation of a porous structure and causes a diversity of pore sizes including micropores and mesopores, and the most N2 gas is absorbed by activated carbon at the highest temperature or 900oC.

| (A) | (B) |
| --- | --- |
| (C) |  |

Fig. 7. Isotherm graph of variation, (A) KA-0-2, (B) KA-18, (C) KA-900

3.5 Electrochemical behavior comparison analysis

Analyzing the electrochemical properties of activated carbon derived from EFB waste materials is essential for optimizing electrochemical applications. The CV test results are presented with a scan rate of 10 mV/s in the range of -0.4 to 0.4 V. The wider the current curve, the greater the specific capacitance value produced. The largest specific capacitance value is the battery with KA 1 - 1 concentration, at 116.78 F.g-1, and the lowest specific capacitance value shown in Table 9 for the battery is in the concentration with KA-2 - 0 concentration, resulting in 69.04 F.g-1. The KOH activator causes the breakdown of lignocellulose, resulting in several new pores on the surface of the activated carbon electrode [37] . The resulting pores will become a place to store charge on the surface of the activated carbon electrode, resulting in a large capacitance value [38].

Table 9. Specific capacitance of concentration variation

| Sample | Specific Capacitance (F.g-1) |
| --- | --- |
| KA-2-0 | 69.04 |
| KA-1.5–0.5 | 112.34 |
| KA-1-1 | 116.78 |
| KA-0.5–1.5 | 113.73 |
| KA-0-2 | 114.60 |

Based on the use of the CV equation, the highest capacitance produced on KA-18 Hours was 96.57 F.g-1, followed by an up and down trend in the resulting capacitance values ​​where on KA-12 hours it was 91.89 F.g-1, KA-24 hours is 94.82 F.g-1, KA-30 hours is 83.79 F.g-1 and KA-36 hours is 77.10 F.g-1 summarized in Table 10. This indicates that the soaking time is short and too long will reduce the capacitance value of the carbon.

Table 10. Specific capacitance of immersion time variation

| Sample | Specific Capacitance (F.g-1) |
| --- | --- |
| KA-12 | 91.89 |
| KA-18 | 96.57 |
| KA-24 | 94.82 |
| KA-30 | 83.79 |
| KA-36 | 77.10 |

An increase in the physical activation temperature changes the morphological condition of the carbon pores to become wider, giving a higher value along with an increase in the temperature used and is confirmed by the results of the specific capacitance of 77.11 F.g-1 to 96.41 F.g-1 even though the value of variables between them experience increases and decreases in capacitance value [39]. Table 7 showed that the relative physical activation temperature affects the electrochemical properties of the battery. Besides that, the hetero-atom reduction that occurs in KA-700 and KA-900 also plays a role in increasing the specific capacitance (Table 11) [40].

Table 11. Specific capacitance of activation temperature variation

| Sample | Specific Capacitance (F.g-1) |
| --- | --- |
| KA-700 | 77.11 |
| KA-750 | 65.41 |
| KA-800 | 66.16 |
| KA-850 | 59.64 |
| KA-900 | 96.41 |

Increasing the physical activation temperature of samples KA-700 to KA-900 significantly changes the porosity structure with a combination of micro and mesopores, where micro and mesopores contribute to providing short ion exchange or transfer pathways and better ion flow. This results in high electrochemical properties on the battery electrodes [41].

3.6 Battery voltage comparison analysis

The battery voltage test results showed that the highest voltage of 1.17 V was achieved with activation using 2 M KOH, while immersing carbon for 18 hours resulted in 1.05 V. Physical activation at 900°C produced a voltage of 1.12 V, the highest among other temperatures tested. The surface area of the carbon significantly influences battery voltage. Higher carbon surface area correlates with increased capacitance and higher battery voltage (Fig. 8). On the contrary, a lower surface area of activated carbon generates a lower capacitance and voltage [42].

| (A) | (B) |
| --- | --- |
| (C) |  |

Fig. 8. Prototype battery voltage test, (A) KA-2-0, (B) KA-18, (C) KA-900

3.7 Mechanism reaction in the battery system

Electron flow that generates electricity within the battery illustrated in Fig.9. The carbon electrodes in these batteries do not produce electricity nor do they react with other elements. Instead, these electrodes serve an inert role, primarily functioning to store the energy within the battery. This inertness is crucial for maintaining the stability and efficiency of the battery's energy storage capability [43]. Sodium chloride (NaCl) is introduced into the electrode to establish a potential difference, where the electrode serves as the cathode. This potential difference drives the movement of electrons from higher to lower potential. The reaction below describes how electric current is generated in the battery (Fig. 7).

The carbon electrode functions as the anode interacts with the cathode and the solid electrolyte PVA-K2CO3. In the battery, the electrolysis reaction involves the decomposition of the K2CO3 electrolyte, yielding 2K+ and CO32- ions. [44]. At the cathode, the reaction involves the ions present in the electrolyte, specifically K+ cations. However, the K+ ions do not directly participate in the reaction. Instead, water molecules (H2O) are the substances that react at the cathode. If this reaction continues, the anode will degrade completely in the electrolyte and the battery will run out of power [45] .

Electrolyte: K2CO3 → 2K+ + CO32-

Cathode: 2H2O + 2e- → H2 + 2OH-

Anode: 2H2O + 4H+ → O2 + 4e-

Reaction: 6H2O → 4OH- + 2H2 + 4H+ + O2

Electrodes from biomass that are processed into active carbon are inert materials or materials that cannot react [46]. So to create conditions with different potentials, one way is by adding an electrode such as sodium chloride (NaCl), so the reaction can occur as it should. Initially, the reaction that occurs is oxidation on the anode which results in the ionization of NaCl where ions dissolved on the electrode will produce electrons that move from the current collector to the cathode to be translated into electrical energy [47]. In the electrode it can be seen that there is migration of negative ions (anions) in the electrolyte, attracted to the anode side and vice versa to the cathode which corresponds to the electrode potential (Fig. 9). In the 2K+ half-reaction, carbon degradation will occur and capacity will decrease as the battery life increases, and this also results in the battery not being able to withstand the reaction for a long time [48].

Fig. 9. Mechanism reaction in the battery system

- Conclusions

Activated carbon from OPEFB waste was successfully prepared using the variations of NaOH and KOH solution, impregnation time, and physical activation. According to SEM analysis, OPEFB-activated carbon produced using 2 M KOH concentration, 18-hour immersion time, and 900°C activation temperature exhibits a porous structure and consists predominantly of carbon elements as high as 84.47%, 88.33%, and 81.47%. From BET examination, the variation in 2 M KOH, 18 hours of immersion time, and activated at 900oC resulted in a carbon surface area of 354.25 m2g-1, 380.28 m2g-1, and 334.28 m2g-1. OPEFB-activated carbon is categorized within the mesopore group based on its pore volume and adsorption capacity. Based on the electrochemical behavior of 2 M KOH, immersion time 18 hours, and temperature activation 900oC produces specific capacitance 116.78 F.g-1, 96.57 F.g-1, and 96.41 F.g-1. Electrical voltage test of battery prototype, it is known that the highest voltage produced is 1.17 V with a variation of 2 M KOH, 1.05 V with a variation of 18 hours immersion time, and 1.12 V of 900oC activation temperature. The use of biomass waste from OPEFB as electrodes in battery applications is an emerging development. This study has achieved promising results, demonstrating potential applications in electrochemistry and absorbance.

Declaration of Competing Interest

The authors declare no known competing financial interests or personal relationships that could have appeared to influence the work reported in this paper.

Acknowledgement

This work is supported by research funding of BIMA Kemendikbudristek 2024 by the Ministry of Education, Research and High Education, Indonesia. In addition, the research get support from Prof. Dr.Eng. Widi Astuti, M. Eng, Badan Riset Inovasi Nasional (BRIN) and Grand Riset Sawit (GRS) 2024 by Badan Pengelola Dana Perkebunan Kelapa Sawit (BPDPKS).

References

[1]	R. Dolah, R. Karnik, and H. Hamdan, “A Comprehensive Review on Biofuels from Oil Palm Empty Bunch (EFB): Current Status, Potential, Barriers and Way Forward,” Sustainability, vol. 13, no. 18, p. 10210, Sep. 2021, doi: 10.3390/su131810210.

[2]	N. A. Ramlee, J. Naveen, and M. Jawaid, “Potential of oil palm empty fruit bunch (OPEFB) and sugarcane bagasse fibers for thermal insulation application – A review,” Constr. Build. Mater., vol. 271, p. 121519, Feb. 2021, doi: 10.1016/j.conbuildmat.2020.121519.

[3]	V. Giorgi et al., “Enzymatic Production of Lauroyl and Stearoyl Monoesters of d-Xylose, l-Arabinose, and d-Glucose as Potential Lignocellulosic-Derived Products, and Their Evaluation as Antimicrobial Agents,” Catalysts, vol. 12, no. 6, p. 610, Jun. 2022, doi: 10.3390/catal12060610.

[4]	H. Rustamaji, T. Prakoso, H. Devianto, P. Widiatmoko, and W. H. Saputera, “Urea nitrogenated mesoporous activated carbon derived from oil palm empty fruit bunch for high-performance supercapacitor,” J. Energy Storage, vol. 52, p. 104724, Aug. 2022, doi: 10.1016/j.est.2022.104724.

[5]	J. M. L. Thoe, N. Surugau, and H. L. H. Chong, “Application of Oil Palm Empty Fruit Bunch as Adsorbent: A Review”.

[6]	N. N. Wulandari et al., “Production of activated carbon from palm empty fruit bunch as supercapacitor electrode material,” IOP Conf. Ser. Mater. Sci. Eng., vol. 1143, no. 1, p. 012004, Apr. 2021, doi: 10.1088/1757-899X/1143/1/012004.

[7]	A. T. Alves, D. J. Lasmar, I. P. De Andrade Miranda, J. Da Silva Chaar, and J. Dos Santos Reis, “The Potential of Activated Carbon in the Treatment of Water for Human Consumption, a Study of the State of the Art and Its Techniques Used for Its Development,” Adv. Biosci. Biotechnol., vol. 12, no. 06, pp. 143–153, 2021, doi: 10.4236/abb.2021.126010.

[8]	S. Rawal, B. Joshi, and Y. Kumar, “Synthesis and characterization of activated carbon from the biomass of Saccharum bengalense for electrochemical supercapacitors,” J. Energy Storage, vol. 20, pp. 418–426, Dec. 2018, doi: 10.1016/j.est.2018.10.009.

[9]	M. Iwanow, T. Gärtner, V. Sieber, and B. König, “Activated carbon as catalyst support: precursors, preparation, modification and characterization,” Beilstein J. Org. Chem., vol. 16, pp. 1188–1202, Jun. 2020, doi: 10.3762/bjoc.16.104.

[10]	S. Ha, S. G. Jeong, S. Myeong, C. Lim, and Y.-S. Lee, “High-performance CO2 adsorption of jellyfish-based activated carbon with many micropores and various heteroatoms,” J. CO2 Util., vol. 76, p. 102589, Oct. 2023, doi: 10.1016/j.jcou.2023.102589.

[11]	L. Harimu, S. Wahyuni, N. Nasrudin, M. J. Baari, and D. Permana, “Fabrication of Chitosan/Fe3O4 Nanocomposite as Adsorbent  for Reduction Methylene Blue Contents,” Indones. J. Chem., vol. 22, no. 3, p. 878, Mar. 2022, doi: 10.22146/ijc.65430.

[12]	I. C. Gómez, O. F. Cruz, J. Silvestre-Albero, C. R. Rambo, and M. M. Escandell, “Role of KCl in activation mechanisms of KOH-chemically activated high surface area carbons,” J. CO2 Util., vol. 66, p. 102258, Dec. 2022, doi: 10.1016/j.jcou.2022.102258.

[13]	W. Luo et al., “Critical thickness of phenolic resin-based carbon interfacial layer for improving long cycling stability of silicon nanoparticle anodes,” Nano Energy, vol. 27, pp. 255–264, Sep. 2016, doi: 10.1016/j.nanoen.2016.07.006.

[14]	M. K. Mahapatra and A. Kumar, “Taguchi Optimization Studies for Abatement of 2‐Chlorophenol Using Neem Seed Activated Carbon,” Chem. Eng. Technol., vol. 45, no. 4, pp. 641–648, Apr. 2022, doi: 10.1002/ceat.202100427.

[15]	N. A. Echeverry‐Montoya, J. J. Prías‐Barragán, L. Tirado‐Mejía, C. Agudelo, G. Fonthal, and H. Ariza‐Calderón, “Fabrication and electrical response of flexible supercapacitor based on activated carbon from bamboo,” Phys. Status Solidi C, vol. 14, no. 3–4, p. 1600258, Mar. 2017, doi: 10.1002/pssc.201600258.

[16]	M. I. Akbar et al., “Application of palm oil frond activated carbon for biobattery electrodes,” Energy Storage, p. e547, Dec. 2023, doi: 10.1002/est2.547.

[17]	J. M. González-Domínguez, M. Alexandre-Franco, C. Fernández-González, A. Ansón-Casaos, and V. Gómez-Serrano, “Activated carbon from cherry stones by chemical activation: Influence of the impregnation method on porous structure,” J. Wood Chem. Technol., vol. 37, no. 2, pp. 148–162, Mar. 2017, doi: 10.1080/02773813.2016.1253101.

[18]	H. Tran Thi Dieu, K. Charoensook, H.-C. Tai, Y.-T. Lin, and Y.-Y. Li, “Preparation of activated carbon derived from oil palm empty fruit bunches and its modification by nitrogen doping for supercapacitors,” J. Porous Mater., vol. 28, no. 1, pp. 9–18, Feb. 2021, doi: 10.1007/s10934-020-00957-2.

[19]	S. M. Waly, A. M. El-Wakil, W. M. A. El-Maaty, and F. S. Awad, “Efficient removal of Pb(II) and Hg(II) ions from aqueous solution by amine and thiol modified activated carbon,” J. Saudi Chem. Soc., vol. 25, no. 8, p. 101296, Aug. 2021, doi: 10.1016/j.jscs.2021.101296.

[20]	R. B. Suneetha, “Spectral, Thermal and Morphological Characterization of Biodegradable Graphene Oxide-Chitosan Nanocomposites,” J. Nanosci. Technol., vol. 04, no. 02, pp. 342–344, Apr. 2018, doi: 10.30799/jnst.sp208.18040201.

[21]	R. Ali, Z. Aslam, R. A. Shawabkeh, A. Asghar, and I. A. Hussein, “BET, FTIR, and RAMAN characterizations of activated carbon from wasteoil fly ash,” Turk. J. Chem., vol. 44, no. 2, pp. 279–295, Apr. 2020, doi: 10.3906/kim-1909-20.

[22]	A. Uke et al., “Effect of decomposing oil palm trunk fibers on plant growth and soil microbial community composition,” J. Environ. Manage., vol. 295, p. 113050, Oct. 2021, doi: 10.1016/j.jenvman.2021.113050.

[23]	F. P. Teixeira, O. D. F. M. Gomes, and F. D. A. Silva, “Degradation mechanisms of curaua, hemp, and sisal fibers exposed to elevated temperatures,” BioResources, vol. 14, no. 1, pp. 1494–1511, Jan. 2019, doi: 10.15376/biores.14.1.1494-1511.

[24]	Y. Wang, M. Qiao, and X. Mamat, “Nitrogen-doped macro-meso-micro hierarchical ordered porous carbon derived from ZIF-8 for boosting supercapacitor performance,” Appl. Surf. Sci., vol. 540, p. 148352, Feb. 2021, doi: 10.1016/j.apsusc.2020.148352.

[25]	E. Taer, A. Apriwandi, Y. S. Ningsih, R. Taslim, and Agustino, “Preparation of Activated Carbon Electrode from Pineapple Crown Waste for Supercapacitor Application,” Int. J. Electrochem. Sci., vol. 14, no. 3, pp. 2462–2475, Mar. 2019, doi: 10.20964/2019.03.17.

[26]	T. S. Hui and M. A. A. Zaini, “Potassium hydroxide activation of activated carbon: a commentary,” Carbon Lett., vol. 16, no. 4, pp. 275–280, Oct. 2015, doi: 10.5714/CL.2015.16.4.275.

[27]	R.-R. Han et al., “Efficient Preparation of Spongy-Like Porous-Activated Carbon from Waste Millfeed Towards High Performance Supercapacitors,” Nano, vol. 15, no. 08, p. 2050106, Aug. 2020, doi: 10.1142/S1793292020501064.

[28]	E. Barcaro, V. Marangon, M. Mutarelli, and J. Hassoun, “A lithium-ion battery with cycling stability promoted by the progressive activation of a silicon oxide anode in graphene-amorphous carbon matrix,” J. Power Sources, vol. 595, p. 234059, Mar. 2024, doi: 10.1016/j.jpowsour.2024.234059.

[29]	E. Taer, K. Natalia, A. Apriwandi, R. Taslim, A. Agustino, and R. Farma, “The synthesis of activated carbon nanofiber electrode made from acacia leaves ( Acacia mangium wild ) as supercapacitors,” Adv. Nat. Sci. Nanosci. Nanotechnol., vol. 11, no. 2, p. 025007, May 2020, doi: 10.1088/2043-6254/ab8b60.

[30]	M. Thommes et al., “Physisorption of gases, with special reference to the evaluation of surface area and pore size distribution (IUPAC Technical Report),” Pure Appl. Chem., vol. 87, no. 9–10, pp. 1051–1069, Oct. 2015, doi: 10.1515/pac-2014-1117.

[31]	C. Y. Jeong, S. K. Dodla, and J. J. Wang, “Fundamental and molecular composition characteristics of biochars produced from sugarcane and rice crop residues and by-products,” Chemosphere, vol. 142, pp. 4–13, Jan. 2016, doi: 10.1016/j.chemosphere.2015.05.084.

[32]	M. S. Yusoff, N. H. Adam, K. Watalinggam, H. Abdul Aziz, and M. Y. D. Alazaiza, “Effectiveness of Oil Palm Frond Activated Carbon for Removing COD, Color and Fe from Landfill Leachate,” J. Eng. Technol. Sci., vol. 53, no. 1, p. 210104, Jan. 2021, doi: 10.5614/j.eng.technol.sci.2021.53.1.4.

[33]	S.-H. Jung, S.-J. Oh, G.-G. Choi, and J.-S. Kim, “Production and characterization of microporous activated carbons and metallurgical bio-coke from waste shell biomass,” J. Anal. Appl. Pyrolysis, vol. 109, pp. 123–131, Sep. 2014, doi: 10.1016/j.jaap.2014.07.003.

[34]	M. Li, S. Ma, and X. Zhu, “Preparation of Activated Carbon from Pyrolyzed Rice Husk by Leaching out Ash Content after CO2 Activation,” BioResources, vol. 11, no. 2, pp. 3384–3396, Feb. 2016, doi: 10.15376/biores.11.2.3384-3396.

[35]	B. K. Saikia, S. M. Benoy, M. Bora, J. Tamuly, M. Pandey, and D. Bhattacharya, “A brief review on supercapacitor energy storage devices and utilization of natural carbon resources as their electrode materials,” Fuel, vol. 282, p. 118796, Dec. 2020, doi: 10.1016/j.fuel.2020.118796.

[36]	T. Sahlabji et al., “High surface area microporous activated carbon from Pisum sativum peels for hexavalent chromium removal from aquatic environment,” Toxin Rev., vol. 41, no. 2, pp. 639–649, Apr. 2022, doi: 10.1080/15569543.2021.1908361.

[37[	J. Sreńscek-Nazzal, A. Kamińska, J. Serafin, and B. Michalkiewicz, “Chemical Activation of Banana Peel Waste-Derived Biochar Using KOH and Urea for CO2 Capture,” Materials, vol. 17, no. 4, p. 872, Feb. 2024, doi: 10.3390/ma17040872.

[38]	L. J. Jönsson and C. Martín, “Pretreatment of lignocellulose: Formation of inhibitory by-products and strategies for minimizing their effects,” Bioresour. Technol., vol. 199, pp. 103–112, Jan. 2016, doi: 10.1016/j.biortech.2015.10.009.

[39]	M. Zhou, J. Gomez, B. Li, Y.-B. Jiang, and S. Deng, “Oil tea shell derived porous carbon with an extremely large specific surface area and modification with MnO2 for high-performance supercapacitor electrodes,” Appl. Mater. Today, vol. 7, pp. 47–54, Jun. 2017, doi: 10.1016/j.apmt.2017.01.008.

[40]	M. S. Guney and Y. Tepe, “Classification and assessment of energy storage systems,” Renew. Sustain. Energy Rev., vol. 75, pp. 1187–1197, Aug. 2017, doi: 10.1016/j.rser.2016.11.102.

[41]	A. Kozina, G. Radica, and S. Nižetić, “Analysis of methods towards reduction of harmful pollutants from diesel engines,” J. Clean. Prod., vol. 262, p. 121105, Jul. 2020, doi: 10.1016/j.jclepro.2020.121105.

[42]	X. Wang, G. Gaustad, C. W. Babbitt, C. Bailey, M. J. Ganter, and B. J. Landi, “Economic and environmental characterization of an evolving Li-ion battery waste stream,” J. Environ. Manage., vol. 135, pp. 126–134, Mar. 2014, doi: 10.1016/j.jenvman.2014.01.021.

[43]	E. Taer et al., “The synthesis of carbon electrode supercapacitor from durian shell based on variations in the activation time,” presented at the The 1st International Conference and Exhibition On Powder Technology Indonesia (ICePTi) 2017, Jatinangor, Indonesia, 2018, p. 030026. doi: 10.1063/1.5021219.

[44]	R. T. Ayinla, J. O. Dennis, H. M. Zaid, Y. K. Sanusi, F. Usman, and L. L. Adebayo, “A review of technical advances of recent palm bio-waste conversion to activated carbon for energy storage,” J. Clean. Prod., vol. 229, pp. 1427–1442, Aug. 2019, doi: 10.1016/j.jclepro.2019.04.116.

[45]	B. A. Abdulkadir et al., “Optimization of the Electrochemical Performance of a Composite Polymer Electrolyte Based on PVA-K2CO3-SiO2 Composite,” Polymers, vol. 13, no. 1, p. 92, Dec. 2020, doi: 10.3390/polym13010092.

[46]	S. Aziz, O. Abdullah, S. Hussein, and H. Ahmed, “Effect of PVA Blending on Structural and Ion Transport Properties of CS:AgNt-Based Polymer Electrolyte Membrane,” Polymers, vol. 9, no. 11, p. 622, Nov. 2017, doi: 10.3390/polym9110622.

[47]	M. Inayat, S. A. Sulaiman, and M. Y. Naz, “Thermochemical Characterization of Oil Palm Fronds, Coconut Shells, and Wood as A Fuel For Heat and Power Generation,” MATEC Web Conf., vol. 225, p. 01008, 2018, doi: 10.1051/matecconf/201822501008.

[48]	A. C. Martins et al., “Removal of tetracycline by NaOH-activated carbon produced from macadamia nut shells: Kinetic and equilibrium studies,” Chem. Eng. J., vol. 260, pp. 291–299, Jan. 2015, doi: 10.1016/j.cej.2014.09.017.

[49]	H. Wang et al., “Microscopic analysis of copper current collectors and mechanisms of fragmentation under compressive forces,” Mater. Today Energy, vol. 17, p. 100479, Sep. 2020, doi: 10.1016/j.mtener.2020.100479.