Qualitative fracture analysis of Si-C-N hard coatings: interfacial and triaxiality effect

A. S. Bhattacharyya1,2*, Kushal Bhattacharyya3

Department of Metallurgical and Materials Engineering, Central University of Jharkhand, Ranchi 835205 India1

Centre of Excellence in Green and Efficient Energy Technology (CoE GEET), Central University of Jharkhand, Brambe, Ranchi: 835205, India 2

Department of Mechanical Engineering, Netaji Subash Engineering College, Techno city Kolkata West Bengal 700152, India3

*Corresponding Author

2006asb@gmail.com;   arnab.bhattacharya@cuj.ac.in

Abstract

The mechanical properties of hard thin films need meticulous and precise inspection for their efficient applicability. SiCN hard coatings deposited on silicon substrates underwent Vickers indentation and fracture analysis was performed with the help of images of fractured regions under the microscope. The fractured regions were matched with geometrical patterns and the mechanism of the occurrence of delaminated and regions subject to brille failure was studied. Finite Element Analysis (FEA) were carried out to study the elastic-plastic as well as ductile to brittle transition in the indentation process. The novel features in the fracture process identified will add to the knowledge in the field of fractographic studies of hard coatings. The findings shall be helpful in fracture analysis of components subject to loading used in heavy-duty equipment as well as MEMS.

Keywords: Hard coatings, SiCN, Vickers indentation, Fracture, FEM

1. Introduction

In industrial tools and micro-electro-mechanical systems (MEMS), hard coatings made of Si3N4, SiC, TiN, cBN, Al2O3, ZrO2, and nano-composites like Si-C-N, Ti-Al-N, Ti-B-N, Ti-B-Si-C-N, etc. are used as protective coatings. The fabrication process involves the use of materials such as single- or polycrystalline silicon, Si3N4, SiC, and diamond-like tetrahedral amorphous carbon (ta-C). These materials have a high degree of rigidity, thermal stability, and environmental resistance. These materials are combined with polymeric compounds to add flexibility1-3. Si-C-N ceramics, a polymer-derived ceramic (PDC), are employed in MEMS as heat actuators, microgrippers, pressure transducers, and electrostatic actuators.4-6.

Fracture is an important mechanical property of protective metallurgical hard coatings. They should be tough enough to withstand external mechanical stimuli as observed in aerospace, automobiles, and other heavy-duty industries. Fracture-resisting ability is quantified by fracture toughness. In the case of coatings, interfacial fracture toughness is however more significant as it involves the adhesive strength of the coatings with the substrate as well.  Static and sliding (scratch) indentation of SiCN have previously been performed, and the various microstructures, internal and residual stress, and flaws in SiCN that affect the overall mechanical behavior have been evaluated.7-9.

The complexion of stress beneath the indent varies with the geometry of the indenter used10. The fracture nature therefore will vary at the different stages of the loading process. For sharper indenters like Berkovich may suffer from tip bluntness initially and the contact established at the primary phases turns out to be Hertzian in nature.  The situation however changes as the indents dig deeper making the conical sides get the major share of impact Determination of the fracture properties of thin films, unlike hardness determination, considers the substrate as well. The reason is that higher loads need to be applied to cause fracture in the coating/substrate system and hence the 10% rule loses its significance11. Fractographic analysis by inspecting the area where the fracture took place gives a whole lot of information about the coating substrate system and gives a qualitative prediction about its sustainability to fracture. Fracture analysis using Vickers Micro indentation showed the different fractural features resembling distorted geometrical shapes, which were analyzed meticulously to understand the nature of failure.

2. Materials and Methods

Magnetron sputtering (Hindhivac, Bangalore) was used to create Si-C-N coatings on Si, glass, and stainless steel (SS 304) substrates utilizing a sintered SiC target and nitrogen/Argon gas. Previously, the details of the experimental methodologies, as well as in-depth studies of structure-property correlations, were published12 – 14. Although nanoindentation is the preferred choice for the mechanical characterization of thin films, the hard operating conditions depend on the testing of the coatings under higher loads.  Micro indentation by Vickers indenter was therefore done and computational analysis using MATLAB showed the effect of substrate, thickness, and stress on the hardness.  The images of the failure region depicting the different types of failure were captured through an attached optical microscope (Leica, Germany). ImageJ software was used to obtain the line profile of specific regions in the images. Nanoindentation (MTS, USA) and Finite Element Modeling using ABAQUS were performed.

3. Results and discussions

3.1 Fracture morphology (some portions have been reproduced with permission15)

Fig 1 (a-f) depicts a variety of fracture morphologies of SiCN coatings placed on silicon substrates. Fig 2 shows the line profile of the highlighted segments (1–8) in the photos. Fig 3 (a-l) shows a schematic illustration of the mechanisms involved in the film failure process. The circular flow of shear stress that causes coating delamination can be shown in Fig 1(a), where the indentation was performed at 100gf force. Very little radial fissures were also discovered. Fig 1(b) shows enhanced radial cracking and chipping 5 seconds following the same indenter impression. The circular circumferential delaminated area morphed into a cardioid, as shown schematically in Fig 3(a, b).  This region corresponds to the residual compressive pulse enclave, which develops when the plastic zone near the crack tip, which has developed owing to overload, is unable to restore its shape after unloading, as opposed to the elastic zone in the case of fatigue failure. An increase in stress induces chipping, which impedes shear flow, resulting in delamination, and the enclave is pushed back towards the indented region, forming a cardioid shape. [Fig 3 (c) - (e)]. The cardioid shape is generated geometrically when a circle crosses a path along the perimeter of another lower area circle that resembles the Mohr circle [Fig 3(f)]. Tresca and Mises yield criteria for anelastic deformation at the fracture tip are used to calculate the plastic zones [Fig 3(h), (i)]. which have the shape of a cardioid and a compressive residual stress area. Because plastic deformation is induced by dislocation nucleation and motion, such cardioid forms are likewise obtained during the operation of a Franck-Read source during dislocation multiplication. The mechanism relates to the annihilation of two dislocation contact points at the cusp, resulting in the formation of a new dislocation inside the cardioid [Fig 3(j)]. The production of facture corresponds to the formation of a new dislocation, and the dislocation loop region corresponds to the delaminated area, implying a reverse parallel between the two situations. The J-integral can be defined by the cardioid around the indentation with its cusp at the crack tip [Fig 3(k)]15, 16. From geometry, any chord passing through a cusp has a length of 2a and the area of the cardioid is 3/2 πa2 [Fig 3(l)]17. Because the chord length was 40 m, the size of the plastically flown zone was 1884 m2. The applied force was 0.98N (100gf), hence the delamination shear flow stress, which is just load divided by area, was 520 MPa.

5

8

6

4

7

3

2

1

Fig 1. Optical micrographs showing fracture mechanisms of SiCN coatings deposited on silicon substrates having lower hardness and adhesion at indentation loads of (a)100gf, (b)100gf (delayed). (c) 200gf, (d) 300gf (e) 500gf and (f) 1000gf (reproduced with permission)15

The formations of lateral cracks and shear bands can be inside the delaminated area at higher loads of 200gf (Fig 1(c)). The enclave has not been drawn into the indented region as chipping (brittle failure) has not yet taken place. The chipping segments were observed on increasing the load to 300 gf where the radial and lateral cracks have joined. A phenomenon of chipped area bifurcation caused by the formation of secondary radial crack can be seen. These secondary radial cracks arise due to some preexisting flow along the indentation (indenter) sides which gets intensified at higher loads. The shear stress flow persisted outside the chipped region with shear bands as well as radial cracks, which can be called tertiary radial cracks. The enclave was found to slightly distort due to the chipping (shown by arrow) and gets transformed into a lateral crack [Fig 1(d)]. The brittle failure intensified on increasing the load further and consequently, the shear flow regions kept on reducing as observed for 500 and 1000 gf, and the radial cracks were interestingly seen to propagate further [Fig1(e), (f)]. This indicates the sources of radial and to some extent, lateral cracks keep on regenerating and are active post brittle failure as well.

The line profiles shown in Fig 2 have distance in terms of pixels on the x-axis and photo intensity represented as "Gray Value" on the y-axis. The bar length scale in the images was tallied with the pixel to estimate the distance or the depth. It provides a cross-sectional estimation of the fractural features. The initial delamination that occurred surrounding the indentation can be seen in Fig 2a. The sinusoidal nature of the plot thereafter indicates the shockwaves propagating from the center where the indentation was made. The load applied was 100 gf which was found to cause radial crack (Fig 2b). The shear bands although equally spaced were observed to be following damping intensity on moving close to the indentation region (Fig 2c).

Fig 2. Line profile of regions marked 1 to 8 in Fig 1. (The x-axis represents pixels and the Y-axis is the gray value)

The indentation made caused a central pile-up showing localized delamination. The discontinuities observed in the profile can have several causes viz, defects, strain hardening in the coating, and the interfacial crystalline (inter crystalline) crystalline morphology is different from the surface morphology. Having nano crystallites on the surface providing good hardness may not be a confirmation of having high toughness as well as often can generate cracks due to stress intensifiers (Fig 2d). The lateral cracks were found to be less sharp compared to radial cracks (Fig 2e). The bifurcation of the chipped segment by the two radial cracks can be seen in Fig 2f. In case of intense brittle failure on a higher load of 1 kgf being used, the delaminated segment along the indented side was smoother and higher in magnitude compared to those which occurred along the cracks (Fig 2 g, h). The stress distribution developing beneath a Vickers indentation has been found to be maximum at the fracture tip which gets separated at the film/substrate interface into an axial component and a lateral component, potentially leading to the production of lateral cracks 9, 18.

Chipping

Chipping

Fig 3. The schematic representation of chronological development of the indented failure zone taking the

shape of Cardioid and subsequent brittle failure in the form of chipping, its geometrical origin which resembles the Mohr circle and plastic zones based on Tresca and Mises yield criteria for an anelastic deformation at the crack tip (reproduced with permission) 15

Unloading

Unloading

Unloading

Loading

Loading

Loading

Loading

= Unloading

Fig 4. Simulated load-depth curves corresponding to a) 100 % elastic recovery with no residual depth and (b – d) elastic-plastic responses with increasing residual depth (open access) 19

3.2 Nanoindentation

Based on its depth-sensing capabilities, a nanoindentation is an effective instrument for determining material properties. The load-depth curve obtained during nanoindentation provides the load necessary to penetrate a specific depth in the material as well as the elastic and plastic work performed during the indentation process. Nanoindentation load depth curves were computationally created in our earlier article, and an attempt was made to shed light on some of the parameters during the loading and unloading process that gave rise to distinct shapes of the curves. (Fig 4). The hypothetical P-h plot with 100% elastic recovery is shown in Fig 4a, where the unloading curve coincides with the loading curve. The deviations between the unloading and unloading increases in Fig 4 b – d, getting manifested as residual depth which is a parameter to indicate the extent of plastic deformation that might have taken place during the indentation involving dislocation mechanics 19-22.

3.3 Finite Element Modeling

3-dimensional finite element analysis is performed on carbon-silicon nitride film on a silicon substrate. Berkovich indenter is modelled as a discrete rigid indenter. The film and substrate are modelled as 1/8th portions of the real cylindrical specimen to reduce the computational time as shown in Fig 5a. The element is meshed with C3D8R which is an 8-node linear brick element reduced integration, hourglass control. The film is meshed with a denser mesh containing 33720 elements and the substrate is meshed with 7798 elements as shown in Fig 5b. Elastoplastic analysis is performed taking the boundary condition as applied in the experiment. Hard contact is established between the Indenter and the film and the film and the substrate is as perfectly bonded because delamination is not observed in the experiment The boundary conditions and the Von misses stress distribution only for the loading phase are given in Fig 5 c & d respectively The load displacement of the finite element is compared with that of experimental results for the loading portion as shown in Fig.6a  The result shows a matching trend up to 100 nm then it deviates as the indentation progress. The FEA plot shows periodical discontinuities as indicated by arrows that correspond to film failure which get manifested in the form of minor thorough-thickness cracking. They also indicate ductile to brittle transitions as explained later. No major cracking phenomena were observed, unlike the experimental plot where a clear step formation takes place due to major crack formation. The deviation arises due to pre-existing flaws in the sample which act as stress intensifiers in the presence of load which were not taken into consideration in the FEA.  It compels us to incorporate some damage models for a more accurate study of the stress pattern near the indenter tip. A discontinuity is observed in the experimental from the Triaxiality (η) distribution (eq 1) and the maximum triaxiality is observed at 200 nm from the indenter tip as shown in Fig 6b.

Triaxiality(η)=σHydrostaticσ&equivalent&                                                                       (1a)

σHydrostatic=σxx+σYY+σZZ3                                                                      (1b)

σequivalent=12σxx-σyy2+σyy-σzz2+σzz-σxx2       (1c)

Triaxiality is an important parameter for damage control. The lower (<1) magnitude of η indicates ductile fracture. However, a lower value at deeper penetration indicates, brittle failure at shallow depths due to the presence of hard coating and less substrate influence. The high stain (~ 1.9 × 10 3) at shallow depth as found in Fig 5 d seems to be in concurrence with the phenomena. The sudden increase in η around 100 nm for both the cases indicated by arrow is the evidence of ductile to brittle transitions (DTB).

(a)

(b)

(c)

(d)

Fig 5 (a) 3D of 1/8th portion of thin film model with Berkovich indenter (b) Mesh distribution (c) boundary conditions and (d) the Von misses stress distribution for the loading phase

The residual stress changes as the indenter penetrates the surface influencing crack growth23. In the plastic zone formed in front of the propagating crack tip, new or emitted dislocations form24. As previously demonstrated, even brittle oxides (MgO, ZrO2, and ZnO) deform solely plastically with dislocations under strong indenter points. During tests with sharp indenters, dislocation-governed plasticity was discovered in a few cases, with a densification process accompanying dislocation activation. (LiF, CaF2, SiC, ZrB2, and ZnS). Cracks form as a result of high loads or indenters with a radius greater than the plastic zone, triggering the DTB transition. LiNbO3 and LiTaO3 are two examples of oxides.  The crack-related indentation size effect, also known as the indentation size-dependent brittle to ductile transition, states that at ever-decreasing small scales with decreasing fault density, shear strength is reached before fracture strength25.  The area of the step region as shown in Fig 6a was about 180 pJ which is the energy released due to fracture, which occurred at 300 nm corresponding to a triaxiality magnitude of 0.65 which showed a sudden steep increase. Interestingly, a somewhat opposite nature of the plot was observed for lower penetration where the η curve with a slight increase became parallel to the x-axis reflecting strain hardening due to ductile slips which can be matched with the formation of new dislocations in front of an advancing crack tip as mentioned above.  This phenomenon can be termed a brittle to ductile transition (BTD). The two opposite natures of the curves were seen at almost the same penetration depth of 250 nm. So, it's that critical penetration depth where the course of action of the penetrating indenter changes based upon factors like thickness, radius of the indenter tip, and hardness of the coating. Ductile slip causing strain hardening was also observed in the second case but at a higher penetration depth of 300 nm.

3.4 Stress distribution

The theoretical shear strength and cohesive strength (or tensile strength) are about μ/2π = 14 GPa and E/π = 70 GPa, respectively, where μ = E/2(1+ν) is the shear modulus and E is the Young's modulus., the shear strength is about 1/5 of the cohesive strength, as the Poisson's ratio ν is 0.25 and E = 220 GPa. ΓP is related to the size of plastic zone where energy is consumed and changed continuously before reaching a steady state limit. If the plastic zone is very small, the total work of fracture Γ is almost contributed from Γ 26- 29. The plastic zone near the crack tip is the dislocation distribution area with dimension rp=1πΓiH where Γi is the interfacial energy of the film-substrate and H is the film hardness (Fig 6f) 30, 31.

Fig 6a shows the Finite Element Modeling of nanoindentation of TiB2 coatings on Si substrates where the distribution of compressive and tensile stress can be seen33. A schematic representation of the cracks generated at indenter tip, along the indenter sides and at the coating-substrate interface is given in Fig 6b34. The two symmetric cracks proceeding perpendicular and at an angle of ~30 degrees towards the film-substrate interface for Ti-N films is given in Fig 6c35. The cracks which are subjected to branching and are represented by the linear profiles of the segments marked in the image. The branched cracks about 1/7 – 1/8 times deep than the main cracks formed. These branching which tells about the interfacial toughness and adhesion strength of the coatings arise due to the inter-crystalline make-up of the coatings as shown in Fig 6d. The histogram showing the closely packed crystallites is shown in the linear profiles. The profile was fitted with a polynomial as given in eq 2 with coefficients below. The positive coefficients indicate coalescence of the crystallites causing an increase in peak height, the negative value represent homogeneity of the interface. An optimization between the two is required for coatings giving best performance.

y = a+bx+cx2+dx3+ex4+fx5+gx6+hx7+ix8      (2)

a = 128.91763; b = 22.56806; c = -3.78988; d = 0.26929; e = -0.010379; f = 0.00023505; g = -3.13439E-6; h = 2.27967E-8, i = -6.97030E-11

This columnar crystalline morphology imparts high fracture toughness and adhesive strength to the coatings, However, there may be instances where localized crystallization may take place due to presence of impurities as marked by circle. These may be detrimental to the overall coating performance. Between the coating and the substrate, an intra facial region exists. This region gets smeared due to indentations as shown in Fig 7c. A significant amount of pile up can be observed by means of the image profile which gives a glimpse of brittle to ductile transitions (BDT). Stress induced crystallizations can also be observed to be occurring in the substrate as shown in Fig 7d. Similar studies involving FEM analysis have shown very high in-plane compressive stresses (~10 GPa) in the film near-surface region next to the indenter. The formation of in-plane tensile stresses under the indenter can also be observed (Fig 6e)32

Intraface

(e)

(d)

Stress induced crystallinity

Columnar growth

Surface

coating

branch

crack

Intercrystalline

Intra-face

-

(f)

Crystallization

substrate

Fig 6 (a)Finite Element Modeling of nanoindentation of TiB2 coatings on Si substrates (open access CC BY 4.0) 33 (b) cracks generated at indenter tip, along the indenter sides and at the coating-substrate interface (c) Two symmetric cracks proceeding perpendicular and at an angle of ~30 degrees towards the film-substrate interface for TiN films (open access CC BY 4.0) 35 with linear profiles of the marked regions  (d) cross-sectional SEM image of TiN films showing columnar growth (reproduced with permission)29 with  histogram showing the inter-crystallinity and the different zones from coating to  substrate  (e) FEM showing very high in-plane compressive stresses (~10 GPa) in the film near-surface region next to the indenter (Open Access CC BY 4.0) 32 (f) schematic of plastic zone surrounding crack tip of radius rp.

3.4 Crystallographic correlations

The crystalline growth affects the fractographical features of the sample surface caused by nanoindentation. Si-C-N has been considered as an upgradation of SiC. The N2 incorporation not only introduced conductivity into the material., but also took care of the fracture toughness which decreases in SiC due to being a valence crystal with high hardness6. In valence crystals, neighboring atoms share their valence electrons through the creation of strong homopolar or covalent bond36, A mixed phase of β-C3N4 and β-Si3N4 was observed for 1 Pa and 5 Pa   Ar/N2 pressures at a temperature close to 500 oC.  There was also evidence of nanocrystalline graphite and diamond forming a diamond-like nanocomposite (DLN) film having high hardness. Multicomponent components having a higher number of elements viz., quaternary (4), quinary (5), senary (6), and even septenary (7) nanocomposites like Ti-Al-N, Ti-B-N, Cr-Fe-Hf-Mn-Ti-Ta-V, etc have been reported 37-42. Some of them have shown much higher hardness than Si-C-N43. Still, Si-C-N has not lost its significance as having incomparable diversified properties. Being initially discovered as a polymer-derived ceramic (PDC) 44, 45.

200 nm

1 µm

(1)

defect

2.5 µm

(c)

β

BDT

DBT

a-Si-O-C-N

(d)

(b)

(a)

LN

(1)

QJ

(2)

BR

(3)

LN

BR

QJ

(3)

(2)

Fig.7 a) Comparison of Load Displacement with Experiment and Finite Element Analysis and (b) Triaxiality variation with indentation depth. FESEM of (c) interface and (d)surface of SiCN coating (reproduced with permission) 14 and profiles marked regions (1), (2) and (3).

The intercrystallite region and surface topography of Si-C-N coating are given in Fig 7 b, c respectively. Three different morphologies marked A, B, and C can be seen. The highly crystalline region with preexisting defects in the form of cracks (A) was followed by the amorphous region (B) and then the substrate (C). The horizontal profile depicted the highly intense crystalline growth. The substrate used in this case was Si (100). The interface regions are usually of high energy and defects and inhibit dislocation motion making ductile to brittle transitions and may lead to an extension of the pre-existing cracks. The amorphous region (B) is significant due to SiOx layer on the.  Si surface, the formation of Si-O-C-N takes place. The SiOx phase acts as the buffer layer between the coating and the substrate and enhances the mechanical strength of the coating/substrate by restraining any crack growth by absorbing the strain caused by it. 46-51 The columnar growth regions also have minute fractured regions as well as dislocations due to the plastic zone created by the strain field in front of the crack. This represents a brittle to ductile transition taking place at the interface. As there are multiple cracks, plastic zones overlap and so do the dislocations and the amorphous region inhibits their flow as mentioned previously.

The surface shows the formation of grains due to clustering and coalescence of the crystallites with features that can be called grain boundaries, voids, or surface cracks There were instances when the cracks were seen to form linear patterns (LN), triple and quadrupole junctions (QJ) and branching (BR) as well. Some places showed particles much less in size than the existing growth patterns to be present in the cracked regions. The profiles of the marked regions (1), (2), and (3) are given below the images to give an idea of how far these features might have gone into the interface. The plots were given in gray value vs. pixels and from the scale bar in the image, approximate estimations of the dimensions were determined. The features were on average 1 to 1.5 µm deep which is the region A at the interface indicating strong correlations between the two and requires further studies.

During indentation, the compressive stress beneath the indenter will cause strain hardening which matches with the observations made previously.  Apart from having protective applications 52, Si-C-N is being currently looked for the absorption of electromagnetic waves (shielding) 53, as thin film pressure and temperature sensors 54, 55, as a bonding layer for memory devices 56. MEMS magnetic devices 57 and even in endodontics 58 All these applications have a direct relation with the fracture stability of the Si-C-N coating and the points discussed so far shall add to the knowledge regarding its workability.

4. Conclusions

Hard coatings of Si-C-N that were indented (Vickers) for fracture investigations revealed mixed mode (ductile-brittle) features. Analysis was done on the observed altered geometrical shapes of the indentation regions. The shear flow causing delamination was found to take geometrical shapes as well and was found to get forfeited subject to brittle failure causing chipping on increasing the loads. The cross-sectional profiles of the different fractured regions provided a clear picture of the different cracking phenomena and showed interesting aspects that demand future in-depth studies The elastic plastic nature of contact and reversible ductile to brittle transitions have been found and analyzed with computational studies of nanoindentation and finite element modeling using triaxiality. An in-depth analysis of the crystallographic growth at the surface and more importantly interfaces revealed the possible mechanism which was in a nutshell ascribed to the brittle to ductile (BDT) and ductile to brittle transitions (DBT) taking place which matched with the FEM observations These finding shall be beneficial for coatings used for microelectronic components and as protective coatings for industrial tools and all other areas where the fracture stability has a major impact on the device performance.

Acknowledgments

The author acknowledges Dr. S.K. Mishra, CSIR-NML Jamshedpur for experimental facilities

DECLARATIONS

The authors declare no conflict of interest

The submitted work is original and has not been published elsewhere in any form or language

Reproduction of previously published material has been done with proper permissions

Data will be made available on request

No funding was received for conducting the research

REFERENCE

(1)	Fan, X.; Smith, A. D.; Forsberg, F.; Wagner, S.; Schröder, S.; Akbari, S. S. A.; Fischer, A. C.; Villanueva, L. G.; Östling, M.; Lemme, M. C.; Niklaus, F. Manufacture and Characterization of Graphene Membranes with Suspended Silicon Proof Masses for MEMS and NEMS Applications. Microsyst. Nanoeng. 2020, 6 (1), 17.

(2)	Chang, Y.; Wei, J.; Lee, C. Metamaterials – from Fundamentals and MEMS Tuning Mechanisms to Applications. Nanophotonics 2020, 9 (10), 3049–3070.

(3)	Zara, J. M.; Yazdanfar, S.; Rao, K. D.; Izatt, J. A.; Smith, S. W. Electrostatic Micromachine Scanning Mirror for Optical Coherence Tomography. Opt. Lett. 2003, 28 (8), 628–630.

(4)	Shah, S. R.; Raj, R. Mechanical Properties of a Fully Dense Polymer Derived Ceramic Made by a Novel Pressure Casting Process. Acta Mater. 2002, 50 (16), 4093–4103.

(5)	Riedel, R.; Kleebe, H.-J.; Schönfelder, H.; Aldinger, F. A Covalent Micro/Nano-Composite Resistant to High-Temperature Oxidation. Nature 1995, 374 (6522), 526–528.

(6)	Tomastik, J.; Ctvrtlik, R.; Ingr, T.; Manak, J.; Opletalova, A. Effect of Nitrogen Doping and Temperature on Mechanical Durability of Silicon Carbide Thin Films. Sci. Rep. 2018, 8 (1).

(7)	Dash, R.; Bhattacharyya, A. S. Crack Growth Based on Indentation along Substrate and Nanocrystallites in Titanium Diboride Thin Films. Fatigue Fract. Eng. Mater. Struct. 2023, 46 (7), 2714–2719

(8)	Dash, R.; Bhattacharyya, K.; Bhattacharyya, A. S. Fracture Associated with Static and Sliding Indentation of Multicomponent Hard Coatings on Silicon Substrates. Fatigue Fract. Eng. Mater. Struct. 2023, 46 (4), 1641–1645.

(9)	Dash, R.; Bhattacharyya, K.; Bhattacharyya, A. S. Film Failure at Earlier and Later Stages of Nanoindentation in Static and Sliding Modes. Eng. Fail. Anal. 2023, 150 (107353), 107353.

(10)	Dieter, G. E. Mechanical Metallurgy; McGraw-Hill,: New York, 1961.

(11)	Tsui, T. Y.; Pharr, G. M. Substrate Effects on Nanoindentation Mechanical Property Measurement of Soft Films on Hard Substrates. J. Mater. Res. 1999, 14 (1), 292–301.

(12)	Bhattacharyya, A. S.; Kumar, R. P.; Priyadarshi, S.; Sonu; Shivam, S.; Anshu, S. Nanoindentation Stress–Strain for Fracture Analysis and Computational Modeling for Hardness and Modulus. J. Mater. Eng. Perform. 2018, 27 (6), 2719–2726.

(13)	Bhattacharyya, A. S.; Mishra, S. K.; Mukherjee, S.; Das, G. C. A Comparative Study of Si–C–N Films on Different Substrates Grown by RF Magnetron Sputtering. J. Alloys Compd. 2009, 478 (1–2), 474–478.

(14)	Bhattacharyya, A. S.; Das, G. C.; Mukherjee, S.; Mishra, S. K. Effect of Radio Frequency and Direct Current Modes of Deposition on Protective Metallurgical Hard Silicon Carbon Nitride Coatings by Magnetron Sputtering. Vacuum 2009, 83 (12), 1464–1469.

(15)	Mishra, S.K., Bhattacharyya, A.S. (2013). Adhesion and Indentation Fracture Behavior of Silicon Carbonitride Nanocomposite Coatings Deposited by Magnetron Sputtering. In: Li, H., Wu, J., Wang, Z. (eds) Silicon-based Nanomaterials. Springer Series in Materials Science, vol 187. Springer, New York, NY.

(16)	Wei, R. P. Fracture Mechanics: Integration of Mechanics, Materials Science and Chemistry; Cambridge University Press: Cambridge, England, 2014.

(17)	Wolfram MathWorld: The web’s most extensive mathematics resource. Wolfram.com. https://mathworld.wolfram.com/ (accessed 2023-10-05).

(18)	Sun, L.; Ma, D.; Wang, L.; Shi, X.; Wang, J.; Chen, W. Determining Indentation Fracture Toughness of Ceramics by Finite Element Method Using Virtual Crack Closure Technique. Eng. Fract. Mech. 2018, 197, 151–159.

(19)	Bhattacharyya, A. S. Computational Studies of the Nanoindentation Load Depth Curves. J. Sci. Ind. Res. (India) 2015.

(20)	Bull, S. J. Nanoindentation of Coatings. J. Phys. D Appl. Phys. 2005, 38 (24), R393–R413.

(21) Bahr, D. F.; Wilson, D. E.; Crowson, D. A. Energy Considerations Regarding Yield Points during Indentation. J. Mater. Res. 1999, 14 (6), 2269–2275.

(22) Lemay, I. Principles of Mechanical Metallurgy; Hodder Arnold: London, England, 1981

(23)	Zeilinger, A.; Todt, J.; Krywka, C.; Müller, M.; Ecker, W.; Sartory, B.; Meindlhumer, M.; Stefenelli, M.; Daniel, R.; Mitterer, C.; Keckes, J. In-Situ Observation of Cross-Sectional Microstructural Changes and Stress Distributions in Fracturing TiN Thin Film during Nanoindentation. Sci. Rep. 2016, 6 (1), 22670.

(24)	Ly, T. H.; Zhao, J.; Cichocka, M. O.; Li, L.-J.; Lee, Y. H. Dynamical Observations on the Crack Tip Zone and Stress Corrosion of Two-Dimensional MoS2. Nat. Commun. 2017, 8 (1), 14116.

(25) Fang, X.; Bishara, H.; Ding, K.; Tsybenko, H.; Porz, L.; Höfling, M.; Bruder, E.; Li, Y.; Dehm, G.;     Durst, K. Nanoindentation Pop‐in in Oxides at Room Temperature: Dislocation Activation or Crack   Formation? J. Am. Ceram. Soc. 2021, 104 (9), 4728–4741.

(26) Kundu, T. Fundamentals of Fracture Mechanics; CRC Press: London, England, 2019.

(27) Frenkel, J. Zur Theorie der Elastizitätsgrenze und der Festigkeit kristallinischer Körper

Eur. Phys. J. A 1926, 37 (7–8), 572–609.

(28) Advances in Mechanical Metallurgy: Processes and Applications; Auris Reference: Birmingham, England, 2015

(29) Wang, A.-N.; Yu, G.-P.; Huang, J.-H. Fracture Toughness Measurement on TiN Hard Coatings Using Internal Energy Induced Cracking. Surf. Coat.

Technol. 2014, 239, 20–27.

(30) Li, J., Yang, B., Wang, S. et al. Modified Model of Crack Tip Stress Field Considering Dislocation Slip Accumulation and Crack Tip Blunting. Chin. J. Mech. Eng. 36, 47 (2023).

(31)	Pippan, R.; Hohenwarter, A. Fatigue Crack Closure: A Review of the Physical Phenomena. Fatigue Fract. Eng. Mater. Struct. 2017, 40 (4), 471–495.

(32)	Liu, H.; Dai, M.; Tian, X.; Chen, S.; Dong, F.; Lu, L. Modified Stoney Formula for Determining Stress within Thin Films on Large-Deformation Isotropic Circular Plates. AIP Adv. 2021, 11 (12).

(33)	Dash, R.; Bhattacharyya, K.; Bhattacharyya, A.S.; Stress distribution variations during nanoindentation failure of hard coatings on silicon substrates, Nanotech & Prec. Eng 2023, NPEE-2023-0013.R4 (Article in Press)

(34)	Bhattacharyya, A.S.; Bhattacharyya, K.; Effect of growth inhomogeneity in the chronological failure mechanism of nanocomposite Si-C-N Coatings, Next Materials 2023 Article 100037

(35)	Zeilinger, A., J. Todt, C. Krywka, M. Muller, W. Ecker, B. Sartory, M. Meindlhumer, M. Stefenelli, R. Daniel, C. Mitterer and J. Keckes (2016). "In-situ Observation of Cross-Sectional Microstructural Changes and Stress Distributions in Fracturing TiN Thin Film during Nanoindentation." Scientific Reports 6. DOI: ARTN 22670 10.1038/srep22670

(36)	Hall, G. G. Valence Crystals. In: Molecular Solid-State Physics; Springer: Berlin, Heidelberg, 1991.

(37)	Xing, Q.; Feltrin, A. C.; Akhtar, F. High-Temperature Wear Properties of CrFeHfMnTiTaV Septenary Complex Concentrated Alloy Film Produced by Magnetron Sputtering. Wear 2022, 510–511 (204497), 204497.

(38)	Singh, V.; Singla, A. K.; Bansal, A. Wetting and Erosive Behavior of VC-TiC + CuNi-Cr Based Coatings Developed by HVOF: Role of Laser Texturing. Eng. Fail. Anal. 2023, 152 (107479), 107479.

(39)	Farhadizadeh, A.; Vlček, J.; Houška, J.; Haviar, S.; Čerstvý, R.; Červená, M. Hard and Electrically Conductive Multicomponent Diboride-Based Films with High Thermal Stability. Ceram. Int. 2022, 48 (1), 540–547.

(40)	Bosi, E., Meghwal, A., Singh, S. et al. Empirical and Computational-Based Phase Predictions of Thermal Sprayed High-Entropy Alloys. J Therm Spray Tech 32, 1840–1855 (2023).

(41)	Yan, Y.; Pei, Z.; Gao, M. C.; Misture, S.; Wang, K. Data-Driven Discovery of a Formation Prediction Rule on High-Entropy Ceramics. Acta Mater. 2023, 253 (118955), 118955.

(42)	Vazquez, G., Chakravarty, S., Gurrola, R. et al. A deep neural network regressor for phase constitution estimation in the high entropy alloy system Al-Co-Cr-Fe-Mn-Nb-Ni. npj Comput Mater 9, 68 (2023).

(43)	Dash, R.; Bhattacharyya, K.; Bhattacharyya, A. S. Synergistic Fractural Features Observed in Ti-B-Si-C Hard Coatings on Enhancing the Sharpness of Nano Indenters. Int. J. Refract. Hard Met. 2023, 116 (106373), 106373.

(44)	Mera, G.; Navrotsky, A.; Sen, S.; Kleebe, H.-J.; Riedel, R. Polymer-Derived SiCN and SiOC Ceramics – Structure and Energetics at the Nanoscale. J. Mater. Chem. A Mater. Energy Sustain. 2013, 1 (12), 3826.

(45)	Ren, Z.; Mujib, S.B.; Singh, G. High-Temperature Properties and Applications of Si-Based Polymer-Derived Ceramics: A Review. Materials 2021, 14, 614.

(46)	Zhang, X.; Zhang, B.; Mu, Y.; Shao, S.; Wick, C. D.; Ramachandran, B. R.; Meng, W. J. Mechanical Failure of Metal/Ceramic Interfacial Regions under Shear Loading. Acta Mater. 2017, 138, 224–236.

(47)	Zhang, X.; Mu, Y.; Dodaran, M.; Shao, S.; Moldovan, D.; Meng, W. J. Mechanical Failure of CrN/Cu/CrN Interfacial Regions under Tensile Loading. Acta Mater. 2018, 160, 1–13.

(48)	Zhang, X.; Namakian, R.; Meng, A. C.; Moldovan, D.; Meng, W. J. Size-Dependent Tensile Failure of Epitaxial TiN/Cu/TiN Sandwich Pillar Structures: A Combined Experimentation – Atomistic Simulation Study. Mater. Sci. Eng. A Struct. Mater. 2022, 855 (143889), 143889.

(49)	Ritchie, R. O. Mechanisms of Fatigue Crack Propagation in Metals, Ceramics and Composites: Role of Crack Tip Shielding. Mater. Sci. Eng. A Struct. Mater. 1988, 103 (1), 15–28.

(50)	Tsui, T. Y.; Ross, C. A.; Pharr, G. M. A Method for Making Substrate-Independent Hardness Measurements of Soft Metallic Films on Hard Substrates by Nanoindentation. J. Mater. Res. 2003, 18 (6), 1383–1391.

(51)	Anderson, N. J.; Zhang, B.; Meng, A. C.; Zhang, X.; Lijesh, K. P.; Khonsari, M. M.; Meng, W. J. Cr-Containing Diamond-like Carbon Coatings Deposited on 316 Stainless Steel Substrates: Characterization and Interfacial Fracture Toughness Measurements. Surf. Coat. Technol. 2023, 462 (129462), 129462.

(52)	Barrios, E.; Zhai, L. A Review of the Evolution of the Nanostructure of SiCN and SiOC Polymer Derived Ceramics and the Impact on Mechanical Properties. Mol. Syst. Des. Eng. 2020, 5 (10), 1606–1641.

(53)	Geng, TB., Yu, GY., Shao, GF. et al. Enhanced electromagnetic wave absorption properties of ZIF-67 modified polymer-derived SiCN ceramics by in situ construction of multiple heterointerfaces. Rare Met. 42, 1635–1644 (2023).

(54)	Wu, C.; Fu, Y.; Zeng, Y.; Chen, G.; Pan, X.; Lin, F.; Xu, L.; Chen, Q.; Sun, D.; Hai, Z. Ultrafast High-Temperature Sintering of Polymer-Derived Ceramic Nanocomposites for High-Temperature Thin-Film Sensors. Chem. Eng. J. 2023, 463 (142518), 142518.

(55)	Cui, Z.; Chen, X.; Li, X.; Sui, G. Thin-Film Temperature Sensor Made from Polymer-Derived Ceramics Based on Laser Pyrolysis. Sens. Actuators A Phys. 2023, 350 (114144), 114144.

(56)	Ma, K., Bekiaris, N., Ramaswami, S., Ding, T., Probst, G., Burggraf, J., & Uhrmann, T. 2023 IEEE 73rd Electronic Components and Technology Conference (ECTC) (pp. 1110-1114). IEEE.

(57)	Stiharu, I.; Andronenko, S.; Zinnatullin, A.; Vagizov, F. SiCNFe Ceramics as Soft Magnetic Material for MEMS Magnetic Devices: A Mössbauer Study. Micromachines (Basel) 2023, 14 (5).

(58)	Xia, X.; Chiang, C.-C.; Gopalakrishnan, S.K.; Kulkarni, A.V.; Ren, F.; Ziegler, K.J.; Esquivel-Upshaw, J.F. Properties of SiCN Films Relevant to Dental Implant Applications. Materials 2023, 16, 5318.