Effect of Ni incorporation in KCoPO4 on the charge storage capacity of  KCo1-xNixPO4 (0≤x≤0.5) Electrodes for the Fabrication of High-Performing Hybrid Supercapacitors

Krishna Gopal Nigam1, Abhijeet Kumar Singh1, Soham Mukherjee1, Asha Gupta2 and Preetam Singh1*

- Department of Ceramic Engineering,

Indian Institute of Technology (Banaras Hindu University) Varanasi, India -221005.

- Department of Chemistry

Indian Institute of Technology (Banaras Hindu University) Varanasi, India -221005.

*: corresponding Author

Email: preetamsingh.cer@itbhu.ac.in

preetamchem@gmail.com

Phone: 91-8118873748

Abstract

To fulfill the increasing energy demands of the world through renewable energy sources requires the utilization of a highly efficient large-scale electrochemical energy storage device. A hybrid Supercapacitor (HSC) that consists of a battery-type electrode coupled with the counter capacitive electrode, while in principle offering supercapacitor-like power and cyclability values and higher energy density can be a potential device as a large-scale energy storage device to cater to the energy needs through renewable energy sources. The KCo0.5Ni0.5PO4 electrode demonstrated a notably enhanced electrochemical performance attributed to the synergistic interaction of Co2+ and Ni2+ ions in a phosphate framework. The incorporation of redox-mediated diffusive charge storage through the incorporation of Ni2+ on the Co2+ site resulted in a large-scale charge storage capacity coupled with capacitive-type surface charge storage on the KCo1-xNixPO4 electrodes. The KCo0.5Ni0.5PO4 delivers 173 mAh/g (capacitances: 1038 F/g) at a current density of 0.5A/g in an aqueous 2M KOH electrolyte accompanied by cyclic stability up to 5000 cycles. HSC mode consists of Activated Carbon as the negative electrode along with KNi0.5Co0.5PO4 as the positive electrode displaying high energy density and power density of 183.7 Wh/kg and 7952W/kg respectively, in 2M aqueous KOH electrolyte. The superior full performance in HSC mode makes KCo0.5Ni0.5PO4 a potential positive electrode for the development of high-performing HSCs.

Introduction

Increasing energy demand to continue the growth and development of the world is accomplished by the burning of fossil fuels, resulting in global warming. For meeting the global energy needs, harnessing energy from renewable energy sources such as solar, wind, tides, etc., can be a prominent solution.[1–3] However, power produced through renewable sources faces power fluctuations due to the dependency on weather conditions. To effectively overcome power fluctuations and to supply stable power through renewable sources such as solar, wind, or tidal large-scale electrochemical energy conversion and storage devices are required [3–8]. Batteries and Supercapacitors have recently gained more attention due to superior performance in terms of excellent efficiency, cyclic stability, energy density, and fast charging/discharging at high current rates. Batteries have high energy density as ion enables redox reactions in bulk electrode materials that are diffusion-controlled. On the contrary, supercapacitors store charge by adsorption of electrolyte ions onto the surface of electrode materials.[5] Notably, the low power density of the batteries due to the sluggish faradic charge storage mechanism and the low energy density of the supercapacitor due to the double-layer charge storage on the electrode surface have made researchers deliberately contemplate hybrid energy storage devices.[5-7] A hybrid Supercapacitor (HSC) is a relatively new device that consists of a battery-type electrode coupled with the counter capacitive electrode, while in principle offering supercapacitor-like power and cyclability values and higher energy density.[9]

The selection of electrode material is a crucial step towards creating effective and reliable HSCs. Carbon-based materials such as activated carbon can be used as negative electrodes for delivering high power density with long-lasting cycles without any constraints.[3-10] Moreover, the positive electrode must be a battery-type material, potentially able to deliver high energy density with minimal loss of capacity with the cycle. However, oxide-based electrodes show slow kinetics with low cyclic stability which ultimately limits to attainment of higher power density and stable life cycle.[11,12] Polyanion frameworks indicate the class of material that inculcates covalent bonded (XO4)n- tetrahedron ( where X= P, S, B, C, Si, etc.) with a subunit of M-O polyhedral (Where M Fe, Ni, Co, etc.).[13] Polyanion framework-type materials are structurally more stable than oxide as the oxygen atom is tightly bound to the central ion X in the tetrahedral coordination sphere. In addition to that, the presence inductive effect of the central metal-ion of the polyanionic subunit increases the ionic character of the M–O bond resulting in an increase in the redox potential by compelling co-active participation of Mn/n+1 redox couple.[14]–[16] Transition metals such as nickel and cobalt are frequently utilized due to their electrochemically active nature in alkaline solutions. Cobalt-based phosphates exhibit pseudocapacitive behavior with high-rate performance but a reasonable amount of specific capacitance.[11], [17]–[20] On the contrary, nickel-based phosphate shows battery-type characteristics with high specific capacitance/capacity as compared to cobalt, but limits in rate performance.[15], [21]–[23] As a result, the substitution of nickel into the compounds based on cobalt can improve their overall electrochemical performance. The incorporation of Ni atoms will be a suitable way to increase active sites in electrode material will lead to higher electrochemical performance.[24], [25]

The present study reports the synthesis, characterization, and electrochemical charge storage performance of Nickel substituted Potassium Cobalt phosphate KCo1-xNixPO4 (0≤x≤0.5) and a detailed investigation of KCo0.5Ni0.5PO4 as a potential robust positive electrode in a Full Cell in asymmetric supercapacitance (ASC) mode. The KCo0.5Ni0.5PO4 electrode demonstrated a notably enhanced electrochemical performance attributed to the synergistic effect of Cobalt and Nickel. The KCo0.5Ni0.5PO4 delivers 173 mAh/g (capacitances: 1038 F/g) at a current density of 0.5A/g in an aqueous 2M KOH electrolyte accompanied by cyclic stability up to 5000 cycles. HSC mode consists of Activated Carbon as a negative electrode coupled with KNi0.5Co0.5PO4 as a positive electrode displaying high energy density and power density of 183.7 Wh/kg and 7952W/kg respectively, in 2M aqueous KOH electrolyte. The superior full performance in HSC mode makes KCo0.5Ni0.5PO4 a potential positive electrode for the development of high-performing HSCs.

Experimental Procedure:

Synthesis of KCo0.5Ni0.5PO4

Synthesis of KCo0.5Ni0.5PO4 was done by sol-gel auto-combustion process followed by calcination of precipitate at elevated temperature to get the crystalline material shown in Figure 1 schematics. Precursors of analytical grade were used for synthesis without any further purification. Nickel Nitrate Hexahydrate (Merck 99.0%), 0.5 Cobalt Nitrate Hexahydrate (Merck 99.0%), 1mM of Potassium Carbonate (Merck 99.9%), Ammonium phosphate (Merck 99.0%) and Citric acid (Merck 99.9%) were taken in respective molar ratio for the synthesis of KCo1-xNixPO4. Citric acid was taken twice the total moles of Co, Ni, and K precursor in the synthesis. For the preparation of KCo.5Ni0.5PO4, first 0.5mM of Nickel Nitrate Hexahydrate (Merck 99.0%), 0.5mM Cobalt Nitrate Hexahydrate, and 1mM of Potassium Carbonate (Merck 99.0%), cation solution was prepared in 100 ml of DI water named as named solution A. Then, solution B was prepared with 1 mM of Ammonium phosphate (Merck 99.0%). Further solution B was slowly added in solution A. After that, 4 mM of Citric acid was added drop by drop in the cation solution to form a homogeneous metal citrate complex at 100. The solutions were mixed with continuous stirring for 4 hours at 80oC, creating a light pinkish gel. Eventually, the reaction temperature was raised to 200 °C for the combustion process. The combustion process took place for about ~3 to 5min yielding voluminous fluffy brown materials. The materials were ground and kept in a muffle furnace at 400oC for 6 hours. The resulting powder was transferred to a furnace and calcined at 600 °C for 8 h to get crystalline KCo0.5Ni0.5PO4.  The indigo blue-colored powder was collected from the crucible and ground adequately and utilized for further characterization and electrochemical performance study.

Materials characterization:

Powder XRD of all KCo1-xNixPO4 samples was performed to examine the crystallinity and purity of phase with monochromatized Cu Kα radiation (λ = 1.54056 Å) as an X-ray source in benchtop X-ray diffractometer (Rigaku miniﬂex 600) with the 10-60o 2 range with a step size equal to 0.02. The structure was matched with X'Pert High Score Plus (PANalytical); further crystal structure of the materials was refined by the Rietveld refinement method using FullProf Suite software.  The morphology of the as-prepared sample KCo0.5Ni0.5PO4 was characterized by EVO - Scanning Electron Microscope MA15 / 18 CARL ZEISS. FT-IR spectra were measured in the wavenumber range of 400–4000 cm-1 to understand the presence of functional groups in the prepared sample with FT-IR spectrometer (Nicolet 6700, Thermo Scientific. The elemental composition and their electronic states present in the sample were examined by X-ray photoelectron spectroscopy (XPS) spectra were measured by a Thermo Scientific using a monochromatic Al Kα X-ray source. Brunauer–Emmett–Teller (BET) analyzer was used to determine the specific surface areas of KCo0.5Ni0.5PO4 sample using (BELSORP-II, Microtrac BEL Japan) with the help of N2 adsorption/ desorption isotherms at 77 K.

To investigate the electrochemical properties of the synthesized KCo0.5Ni0.5PO4 sample cyclic voltammetry (CV), galvanostatic charge-discharge (GCD), and electrochemical impedance spectroscopy (EIS) were performed by the conventional three-electrode system and measured by Metrohm Autolab (PGSTAT204) coupled with a FRA32M module for impedance analysis. NOVA1.1 software was used to analyze the Electrochemical measurements.

Electrode preparation:

Electrochemical measurements were performed in a three-electrode electrochemical cell which involves KCo1-xNixPO4 (x = 0, 0.1, 0.3 and 0.5) as the working electrode, saturated calomel electrode (SCE) used as the reference electrode, and platinum plate as the counter electrode. The working electrode was prepared in a 70:20:10 weight % of the active material (KCo1-xNixPO4), Conducting carbon (Acetylene black, Alfa Aesar), and binder (PVDF, Merck) respectively in NMP: N-Methyl-2-pyrrolidone solvent. The homogenous slurry was made in an agate mortar pestle. This slurry mixture containing ~1 mg of active material was coated onto a 1 cm2 area of Toray carbon paper (Alfa Aesar). It was followed by drying at 80 °C for 12 h to obtain the working electrode. After that, the weight of the loaded electrode material was calculated by taking the difference between the weight of the material loaded electrode and the weight of the blank electrode (Shimadzu electronic weighing balance machine, error limit: 0.01 mg). As prepared, dried electrodes were used for further study of electrochemical measurement. In full cell (Hybrid supercapacitor Mode), electrochemical studies were performed using the Activated Carbon as the counter cum reference electrode in 2M KOH electrolyte.

Result and discussion:

The powder XRD pattern of KCo1-xNixPO4 (x = 0, 0.1, 0.3, and 0.5) samples calcined at 600 oC is presented in Figure 2. XRD peaks of all the samples match well with JSPDS no.: 82-0762 of hexagonal KCoPO4. Rietveld refined powder XRD profile of calcined KCo0.5Ni0.5PO4 shown in Figure 3(a), which matched the reference structure (JCPDS No.: 82-0762 of KCoPO4) without observing any impurity peaks. Refined cell parameters (a = 18.021660, b = 18.021660, c = 8.604042) and Rp= 17.5, Rwp= 11.4, Rexp = 8.78, χ2= 1.67 represent the Hexagonal Crystal structure formation with space group P63. The presence of Co-O and Ni-O polyhedral shared connected by corner sharing of oxygen of phosphate is confirmed by the VESTA image displayed in Figure 3(b).

The FTIR spectra of KCo0.5Ni0.5PO4 powder samples between the wavenumber ranges of 400-4000cm-1 are revealed in Figure 3(c). The broad peak at 3400cm–1 in KCo0.5Ni0.5PO4 spectra implies the stretching vibration of a hydroxyl group (ν (-OH)) signifies the presence of water in the compound. In the FTIR spectra, a strong band arose at 1054.83cm-1  due to asymmetric stretching(νas) of P-O bond vibration (990-1200cm-1), and symmetric stretching(νss) vibration of P-O results in strong transmittance peak at 944cm-1, 845.9cm-1of -PO4 group.[26] Peaks at 620cm-1 referred to O-P-O out-plane bending and 428 cm-1 referred to -δPO4 group. Thus the major vibrational spectra validate the presence of the -PO4 group in KCo0.5Ni0.5PO4. The asymmetric stretching modes of CoO6 octahedra have been observed at 587cm−1.[27] The peak around 549 cm−1 may be ascribed to the asymmetric stretching of Ni–O bonds in NiO6 octahedra[28]. The absorption peak at 479cm−1 is also attributed to both Ni−O and Co−O bonding present in the prepared sample KCo0.5Ni0.5PO4.[29]

Indeed, to analyze the surface area and pore volume of the sample, the N2 adsorption-desorption isotherm carried at 77k is shown in Figure 3(d) and it represents the type III isotherm with the hysteresis loop of H3 type implying the presence of mesoporous structures connected via macropores.[30], [31] The small hysteresis in the high relative pressure range in the N2 adsorption-desorption isotherm indicates the capillary condensation phenomenon indicating the mesoporous nature.[32] Moreover, the specific surface area of the prepared sample equivalent to 2.5875 m2/g with major pore size distribution in a range of 3 to 10 nm with some macropores ⁓220nm obtained by BJH (Brunauer, Joyner, and Halenda) plot (inset of Figure 3(d)). Mesopores are attributed to result in good electrochemical performance of the materials because of high porosity. The calculated average pore diameter of the KCo0.5Ni0.5PO4   sample was found to be ~20.79 nm.

The chemical composition and valance state of constituent elements of the KCo0.5Ni0.5PO4 sample were examined by the XPS (X-ray photoelectron spectroscopy). The wide range survey spectrum shown in Figure 4(a) confirms the presence of K, Co, Ni, P, and O in the sample. Moreover, Figure 4(b) shows the binding energies K 2p3/2 and K 2p1/2 state at 292.2 eV and 295.1 eV respectively confirming the K+ ion in the sample. The Co(2p) spectrum shown in Figure 4(c) splits into different peaks, corresponding to 2p3/2 of Co2+ at 780.63 eV and 2p1/2 of Co2+ at 796.41 eV ions, as well as satellite peaks at 784.17 and 801.96 eV that arise from Co2+ ions. The core level spectrum of Ni(2p) is shown in Figure 4(d) and is de-convoluted into Ni 2p3/2 and Ni 2p1/2 states at the binding energies of 855.6 eV and 873.4 eV respectively, with corresponding satellite peaks at 860.9eV and 879 eV. These binding energies confirm Ni as Ni2+ in the sample. O(1s)  state of the KCo0.5Ni0.5PO4 sample has two prominent peaks shown in Figure 4(e)  at 530.8eV for the metal-oxygen bond of (Ni-O, Co-O) and 532.2 for P-O bonding respectively.[33] P(2p) peak de-convoluted into 2p3/2 and P 2p1/2  in Figure 4(f) observed at binding energy at 132.41eV and 133.47eV, respectively, confirming P5+ ion of -PO4 unit.

Figure 5(a) represents the FE-SEM image of the sample displaying the particle morphology and surface structure of the KCo0.5Ni0.5PO4 power sample suggesting the average particle size of the 437nm having flakes-like arrangements. Elemental analysis of the KCo0.5Ni0.5PO4 sample is shown in Figure 5(b) in the form of an Energy Dispersive X-ray Analysis (EDX) image which shows the peaks of all elements such as K, Co, Ni, P, and O present in KCo0.5Ni0.5PO4. Further, FESEM mapping of the prepared sample is shown in Figure 5(c-g) and confirms K, Co, Ni, P, and O, distributed throughout the electrode material present in the purest form on the synthesized product. Similarly, Figures S1, S2, and S3 represent the FE-SEM image as well as EDX along with elemental mapping of KCo1-xNixPO4  for x = 0,0.1 and 0.3 to understand the composition of doping.

High-resolution transmission electron microscopy (HRTEM) images of the KCo0.5Ni0.5PO4 sample are shown in Figure 6(a) represents the lattice fringes of the sample and Figure 6(a) (i-ii) represents the FFT (fast Furrier transformation) and inverse FFT image. Figure 6(b) shows the thickness of lattice fringes as the calculated d spacing 0.252nm matches very well with the (600) plane of the prepared sample KCo0.5Ni0.5PO4.

Electrochemical Studies:

Cyclicvaltagram (CV plots) of all the KCo1-xNixPO4 (x = 0, 0.1, 0.3, and 0.5) samples in 2M KOH electrolyte is shown in Figure 7 for comparison at the scan rate of 5mV/s in the voltage range of 0-0.6V. CV plot of KCoPO4 shows capacitive charge storage of near rectangular type CV curve. Redox peaks start appearing in the CV plot after Ni doping in the samples. As Ni content increased in the sample, the redox peak intensity increased along with the increased area under the CV curve representing an increase in the charge storage capacity of Ni-doped KCoPO4  samples. The charge storage capacity of the electrode materials was calculated using Equation 1 to examine the electrochemical characteristics of the prepared sample.

Csp=i VdV2mVϑ                                                                                       (1)

The specific charge storage capacity in mAh/g can be calculated using eq.2.

CmAhg=Csp*∆V=i VdV2mϑ*3.6                                                                                     (2)

Where ‘m’ is the active mass of the electrode (g), ‘V’ is the operating voltage window (V), and ‘ϑ’ is the scan rate (mV/s). The charge storage capacity of KCo1-xNixPO4 (x = 0, 0.1, 0.3, and 0.5) samples were found to be 575F/g, 623F/g, 735F/g, and 845F/g respectively at the scan rate of 5mV/s in 2M KOH electrolyte. The highest charge storage performance along with a distinctive redox peak was observed for the KCo0.5Ni0.5PO4 sample. That is why the investigation of the electrochemical performance of KCo0.5Ni0.5PO4 as the working electrode was carried out by cyclic voltammetry (CV), galvanostatic charge-discharge study (GCD), and impedance spectroscopy (EIS) in three-electrode arrangement in 2M KOH as an electrolyte. In Figure 8(a), the CV curves at various scan rates exhibit redox peaks between the potential range of 0 V to 0.6 V. Figure 8(a) shows the CV curve of KCo0.5Ni0.5PO4; the nature of the curve presents the redox-mediated intercalating storage coupled with surface redox (electrosorption) behavior. The nature of the CV curve nature confirms the intercalative type of redox-mediated storage.  Redox peaks resulted due to the reversible interconversion of both Co2+/3+ and Ni2+/3+ through Electrosorption of OH- ion represented by equation 1.

KCo0.5((II))Ni((II))0.5PO4 + OH-solKCo((III))0.5Ni0.5((III)) (OH-)PO4  (redox-mediated diffusion controlled intercalation)          (3)

EDLC-type surface capacitance:

KCo0.5((II))Ni((II))0.5PO4 + xKOHK+x│ KCo0.5((II))Ni((II))0.5PO4 │xOH- (4)

Total charge storage capacity:

KCo0.5((II))Ni((II))0.5PO4  + KOH + OH-solK+x│ KCo0.5((II))Ni((II))0.5PO4 │OH-(1+x)        (5)

The charge storage capacity of  KCo0.5Ni0.5PO4 was calculated using eq. 1&2, and charge storage capacity was found close to 142.3mAh/g (capacitance: 854F/g) at 0.5mV/s scan rate. The shifting of an anodic peak and the cathodic peak was observed linearly with increasing scan rate confirming the dominance of diffusion-controlled intercalative type of redox-mediated charge storage in the materials.  Figure 8(b) shows the relation of anodic and cathodic peak current linearly with the square root of the scan rate, confirming that the KCo0.5Ni0.5PO4 electrode exhibits the semi-infinite diffusion-controlled redox reaction. The Kinetics of electrodes can be examined by determining the ion diffusion coefficient. The ion diffusion coefficient of the electrode was calculated using the Randles-Sevick equation presented below.[34], [35]

ip=2.686 ×105 ×n3/2 A D1/2 Cov1/2                                         (6)

Where ip is peak current density (A), n is the number of electrons that participated in the redox reaction (usually 1), A is the area of the electrode in cm2, D is diffusion coefficient in cm2/s, Co is OH- ion concentration in mol/cm3 and ν is scan rate in V/s. Using eq. 6, the diffusion coefficient of OH- in the KCo0.5Ni0.5PO4 electrode was found to be 1.47×10-8cm2/s for the oxidation reaction and 1.38×10-8 cm2/s for the reduction reaction.

To qualitatively understand the electrochemical kinetics, a power-law equation was used given below in eq.7.[34]

i=aνb                                                                       (7)

a and b are adjustable parameters, i is the current (A), and ν is the scan rate (V/s). The b values lie between 0.5 to 1, b equal to 0.5 for the intercalative semi-infinite diffusion control redox process or battery-type charge storage behavior, while b equal to 1 represents the surface controlled charge storage. Figure 8(c) shows the log(peak current (ip) vs log (v) plots and from the slope of the plot, b values are extracted. The b-value of current observed for oxidation and reduction was close to 0.623 and 0.651 respectively, suggesting the charge storage mechanism in KCo0.5Ni0.5PO4 is a semi-infinite diffusion-controlled intercalating process rather than capacitive.

Scan rate dependence on the current density plot which can quantitatively determine the contribution of the capacitive and intercalation of ions at low scan rates shown in Figure 8(d). Dunn's method quantitatively separates the capacitive and diffusion-controlled charge storage in the electrodes into two components using eq. (8).[15], [29], [36]

iυ=k1v+k2v12                                                          (8)

Eq. (8) was simplified into eq 9 to separate the total charge stored into the peculiar contributions.

iυ/v(1/2)=k1/v(1/2)+k2                                                               (9)

From eq. 9, k1 and k2 explain the contribution of current from the surface capacitance and the diffusion-controlled intercalation charge storage respectively. Consequently, the current response i(V) is from CVs for a range of scan rates, and the slope of a linear fit offers a constant k1 and y-axis intercept for the constant k2, when plotted i(V)/v1/2 versus ν1/2 as displayed in Figure 9(d). As shown in Figure 8(e), after the calculation of k1 and k2 values, the contribution of surface-controlled charge storage was close to 37.7 %) and the contribution for the diffusion-controlled interaction process was close to 62.3% at 0.31 V peak potential with 0.5 mV/s scan rate. The contribution of diffusion-controlled intercalative and surface-controlled charge storage at various scan rates is shown in Figure 8(f).

According to Trassati, the sum of the contributions from the electrode's inner and outer surfaces determines a material's overall charge storage capacitance and is represented by eq. 10. [11],[15][34]

Ctotal = Cin + Cout (F /g)                                                         (10)

The total charge storage capacitance contribution from the inner and outer surface of the electrode is dependent upon the square root of the scan rate. The total charge stored at the electrode or the total capacitance of the electrode is measured by the y-intercept of the linear fit of C-1 vs. ν1/2 at different scan rates as shown in Figure 9(a). Further, the y-intercept of the linear C vs. ν1/2 curve determines the outer surface contribution to charge storage or outer capacitance (Cout) of the electrode displayed in Figure 9(b). Using Trasatti plot, the total amount of charge stored in the electrode was found close to 142.3mAh/g (capacitance: 854F/g) at 0.5mV/s  in which inner surface contribution and outer surface contribution in total capacitance, Cin was found to be  91mAh/g or 546 F/g (64 % of total capacity), and Cout was found to be 51.3mAh/g (Capacitance: 308 F/g  (36 %of total capacity), respectively. Overall, it can be concluded that the electrode stores charge primarily by the semi-infinite diffusion-controlled mechanism.[37]

GCD analysis was performed within the potential window 0–0.6 V at constant and different current density values to analyze the charge storage performance further. GCD curves at numerous discharge currents, the electrode's charge storage capacity (total capacitance) can be calculated using eq. 11. [38], [39]

Csp=I∆tm∆V                                                                (11)

The specific capacity of the electrode in mAh/g is calculated by modifying (eq. 11) as represented below.

CmAhg=Csp*∆V=I∆tm*3.6                                                         (12)

Where I is the discharge current density (A), ∆t is the discharge time (s), m is the active mass of the electrode (g) and ∆V is the potential window of the discharge (V).

Figure 10(a) depicts the Galvanostatic capacity/ capacitances of KCo0.5Ni0.5PO4  and the values are found close to 173 mAh/g (capacitances: 1038 F/g), 144.3mAh/g (capacitances: 865.8 F/g), 115.5 mAh/g (capacitances: 693F/g), 85.8mAh/g (capacitances: 515F/g), 61.2mAh/g (capacitances: 367.6 F/g), and 37.4mAh/g (capacitances: 224.4F/g) at the current rates of 0.5, 1, 2, 3, 4 and 5A/g. The GCD curves of KCo0.5Ni0.5PO4 electrodes exhibit a stable and symmetric charging and discharging nature which indicates that the electrode shows a pseudocapacitive nature, which originates from redox-mediated intercalating storage. Higher capacity was observed in GCD experiments compared to cyclic voltammetry suggesting more diffusion-controlled bulk charge storage of the material confirming the redox-mediated battery-type intercalating charge storage in the material. The specific capacity of KCo0.5Ni0.5PO4   is measured at different current densities from 0.5A/g to 5A/g with cycle number as presented in Figure 10(b). With the increase in current rates, the charge storage capacity of the material decreased. It’s worth noting when the current density is reversed back to 1A/g after testing at different rates, it clearly shows that the specific capacity of KCo0.5Ni0.5PO4 is stable. Figure 10(c) presents the superior cycle stability of KCo0.5Ni0.5PO4   electrodes at 5A/g for 5000 cycles. It was observed that 88.93% of capacity retention after 5000 cycles. Simultaneously, Figure 10(c) also displays the coulombic efficiency (η=tdtc) of the electrode and it was found ~ 97.2 % after 5000 cycles of charge/discharge suggesting the superior reversibility and robust performance of the KCo0.5Ni0.5PO4 electrode. Further, Electrochemical impedance spectroscopy (EIS) was conducted to investigate the electrochemical performance of the KCo0.5Ni0.5PO4 electrode during long-term application. EIS spectra are shown as Nyquist plot in Figure 10(d) of the KCo0.5Ni0.5PO4 electrode before and after the cycling stability test within the frequency range from 100kHz to 0.1 Hz at 10mV of the applied potential. The solution resistance (Rs) has suffered a very minute change (from 1.23 Ω to 1.52 Ω). The charge transfer resistance (Rct), which describes the accumulation of electrolyte ions across the KOH/ KCo0.5Ni0.5PO4 interface, increased from 0.55Ω to 0.81 Ω. The total resistance (a summation of Rs and Rct) represents the equivalent series resistance (ESR), an important parameter for generally evaluating storage materials[36]. In this particular instance, the KCo0.5Ni0.5PO4 electrode's ESR increased little (from 1.78 Ω to only 2.35 Ω), demonstrating the KCo0.5Ni0.5PO4 material's superior performance.

Full cell measurements in Hybrid Supercapacitor (HSCs) Mode:

A hybrid supercapacitor (HSC) was fabricated to demonstrate the practical application, employing KCo0.5Ni0.5PO4 as the positive electrode and Activated Carbon (AC) as the negative electrode in a 2M KOH electrolyte. To obtain the highest charge storage capacity in the full cell test, the storage capacity of both electrodes was balanced using the equation presented below:

1Ctotal= 1Cpositive+ 1Cnegative                                                 (13)

In  a  two-electrode  system,  the  optimal mass ratio (m+/m-) of  the  positive  electrode  and  the  negative electrode can be calculated according to

Equation:

m-m+= C+×∆E+C-×∆E-                                                                           (14)

Where m+, m-, C+, C-, ∆E+,  ∆E- are both electrodes' active mass, specific capacitance, and potential window.

Figure 11(a) shows the independent CVs of AC (activated carbon) (the negative electrode) and KCo0.5Ni0.5PO4   (the positive electrode). The active mass ratio (m-m+) of electrodes was found to be 3.1: 1. Figure 11(b) demonstrates the CV curve of AC// KCo0.5Ni0.5PO4   full cell in two electrode HSCs mode in the potential window of 1.6V with different scan rates of 1mV/s to 100mV/s. Subsequently, Figure 11(c), shows the quantitative charge storage ability of the full cell using the galvanostatic charge/discharge plot. The capacity/capacitance value was calculated was eq. 10 and the charge storage capacity full hybrid supercapacitor was found to be 228.3 mAh/g (capacitance: 514 F/g), 174.8 mAh/g (capacitance: 394 F/g),  112.5mAh/g (capacitance: 254 F/g), 77.2 mAh/g (capacitance:173.7 F/g), and  45.57  mAh/g (capacitance: 102.5 F/g) at respective current rates of  0.5A/g, 1A/g, 2.5A/g, 5A/g, and 10A/g. Figure 11(d) depicts the EIS spectra (Nyquist plot) in the frequency range (1MHz - 0.1Hz) at 10mV/s of applied potential before and after cyclibility. According to the Nyquist plot, before and after cyclability the value of solution resistance Rs =1.44Ω and Rs =2.12Ω respectively, accompanied by the charge transfer resistances of the device to be Rct = 5.03 Ω (before) and Rct = 7.86 Ω (after life cycle test). However, the change in resistance from EIS spectra reveals that higher charge transfer resulted in the superior capacitive performance of the full cell (AC// KCo0.5Ni0.5PO4). HSCs-based AC// KCo0.5Ni0.5PO4 full cell delivered Coulombic efficiency nearly of ⁓96% Figure 11(e) with excellent stability owing to a capacitance retention of 87.2 % after 5000 cycles. The amount of specific energy density (E) and specific power density (P), of the HSCs can be calculated according to the equations presented below:

E(Wh/kg)=12CHSCs 3.6V2                                        (15)

P(W/kg)=E*3600tdis                                               (16)

Where CHSCs is specific capacitance, V is Potential window and tdis is discharge time.

Figure 11(f) presents Ragone plot an energy density vs power capacity at different constant current densities. Full cell  (AC// KCo0.5Ni0.5PO4) delivered a maximum energy density equal to 183.7 Wh/kg at 0.5 A/g current rates achieving power capacity close to 414W/kg. The maximum power density equal to 7952 W/kg was obtained at an energy density of 36 Wh/kg at a current density of  10 A/g for the full cell. These enhanced full-cell performances in the two-electrode HSCs mode of the KCo0.5Ni0.5PO4 electrode validate the suitability of the new KCo0.5Ni0.5PO4 electrodes for creating superior hybrid supercapacitors. In the Hybrid Supercapacitor (HSC) mode, we presented a comparison, of the performance of alternative phosphate base transition metal phosphate-containing electrodes in Table 1.[11, 15-18, 20-24, 40-42] The table confirms the superior performance of full in HSC mode confirming battery type intercalating KCo0.5Ni0.5PO4  electrode as a potential candidate to fabricate high-performing Hybrid supercapacitors.

Conclusions:

KCo1-xNixPO4 (x = 0, 0.1, 0.3, and 0.5) powder was synthesized through facile two-step synthesis utilizing a sol-gel auto-combustion process followed by calcination at elevated temperatures of 600oC. Due to the synergistic interaction of Co2+ and Ni2+ ions in a phosphate framework, the incorporation of redox-mediated diffusive charge storage through the incorporation of Ni2+ on the Co2+ site resulted in a large-scale charge storage capacity coupled with capacitive-type surface charge storage on the KCo1-xNixPO4 electrodes. The KCo0.5Ni0.5PO4 electrodes delivered a specific capacity of 173 mAh/g  ( Capacitance: 1038 F/g ) at 0.5 A/g current density with excellent cyclic stability. Involvement of ⁓1:1 Co: Ni composition has a significant impact on charge storage in HSCs mode. Intercalative (inner) and capacitive (outer) surface charge storage on the electrode was close to 58 and 42%, respectively, suggesting that the high capacitance of the electrode is due to the predominant intercalative pseudocapacitive charge storage behavior caused by the active involvement of Co2+/3+ and Ni2+/3+ redox couple mediate charge storage. The superior cycle stability of KCo0.5Ni0.5PO4   electrodes at 5A/g for 5000 cycles with 88.93% capacity retention and coulombic efficiency (η=tdtc). In the potential window of 1.6V in 2M KOH electrolyte, the AC//KCo0.5Ni0.5PO4 cell in HSCs mode achieved the highest energy density, nearly 183.7 Wh/kg, with a power capacity of 414 W/kg. Moreover, the full cell (AC//KCo0.5Ni0.5PO4) demonstrated an exceptionally high power capacity of about 7952 W/kg, which allowed it to store 36.4 Wh/kg of charge at a current rate of 10 A/g while maintaining excellent cycle stability. After 5000 cycles, AC//KCo0.5Ni0.5PO4 HSCs coulombic efficiency has lost just 4.7%, demonstrating good capacity retention (87.2%) of its initial value. Conclusively, the KCo0.5Ni0.5PO4 reported in this work showed promising application as an efficient, stable, and environmentally begin electrode for supercapacitors in grid-scale energy storage applications.

Acknowledgments:

Krishna Gopal Nigam thanks the Department of Ceramic Engineering, IIT (BHU) Varanasi for its facility and support. The authors also thank the financial support from Cellgrid Energy Pvt. Ltd. (Project no.: UID0991) for completing this work. The author also thanks the Central Instrument Facility IIT(BHU) for the characterization of the samples.

Conflicts of interest:

The authors declare that they don’t pose any known competing financial restrictions and regulations that can influence the work reported in this paper.

References.

[1]	R. Eisenberg, “Addressing the Challenge of Carbon-Free Energy,” ACS Energy Lett., 2018, 3, 1521–1522, DOI: 10.1021/acsenergylett.8b00889.

[2]	S. Chu and A. Majumdar, “Opportunities and challenges for a sustainable energy future,” Nature, 2012, 488,294–303, DOI: 10.1038/nature11475.

[3]	K. Subramanyan, M. L. Divya, and V. Aravindan, “Dual-carbon Na-ion capacitors: progress and future prospects,” J. Mater. Chem. A, 2021, 9, 9431–9450, DOI: 10.1039/d0ta12099e.

[4]	E. Capacitors, “What Are Batteries, Fuel Cells, and Supercapacitors ?,” 2004, 104,4245-4270, DOI: 10.1021/cr020730k.

[5]	 P. Simon, Y. Gogotsi and B. Dunn “Where Do Batteries End and Supercapacitors Begin ?,” 2014, 343 (6176), 1210–1212, DOI: 10.1126/science.1249625.

[6]	J. Liu, C. Xu, Z. Chen, S. Ni, and Z. X. Shen, “Progress in aqueous rechargeable batteries,” Green Energy Environ., 2018, 3, 20–41, DOI: 10.1016/j.gee.2017.10.001.

[7]	J. Cherusseri, D. Pandey, and J. Thomas, “Symmetric, Asymmetric, and Battery-Type Supercapacitors Using Two-Dimensional Nanomaterials and Composites,” Batter. Supercaps, 2020, 3, 860–875, DOI: 10.1002/batt.201900230.

[8]	J. B. Goodenough and P. Singh, “Review-Solid electrolytes in rechargeable electrochemical cells,” J. Electrochem. Soc., 2015, 162, A2387–A2392, 2015, DOI: 10.1149/2.0021514jes.

[9]	J. Ding, W. Hu, E. Paek, and D. Mitlin, “Review of Hybrid Ion Capacitors : From Aqueous to Lithium to Sodium,” 2018, 118, 6457–6498, DOI: 10.1021/acs.chemrev.8b00116.

[10]	G. Z. Chen, “Understanding supercapacitors based on nano-hybrid materials with interfacial conjugation,”Prog.Nat.Sci.Mater. Int.,2013,23,245–255,DOI: 10.1016/j.pnsc.2013.04.001.

[11]	N. Priyadharsini, S. Surendran, B. Senthilkumar, L. Vasylechko, and R. K. Selvan, “Synthesis and Electrochemical Performances of γ-KCoPO4 Nanocrystals as Promising Electrode for Aqueous Supercapatteries,” ChemElectroChem, 2019, 6, 369–377, DOI: 10.1002/celc.201801440.

[12]	Y. Jiang et al., “Transition metal oxides for high performance sodium ion battery anodes,” Nano Energy, 2014,5, 60–66, DOI: 10.1016/j.nanoen.2014.02.002.

[13]	P. Singh, K. Shiva, H. Celio, and J. B. Goodenough, “Eldfellite, NaFe(SO4)2: an intercalation cathode host for low-cost Na-ion batteries,” Energy Environ. Sci., 2015, 8, 3000–3005, DOI: 10.1039/c5ee02274f.

[14]	L. Sharma and A. Manthiram, “Polyanionic insertion hosts for aqueous rechargeable batteries,” J. Mater. Chem. A, 2022,10, 6376–6396, DOI: 10.1039/d1ta11080b.

[15]	M. Singh, S. Kumar, R. Mondal, P. Singh, R. Prakash, and N. Sharma, “Combustion-Synthesized KNiPO4: A Non-toxic, Robust, Intercalating Battery-Type Pseudocapacitive Electrode for Hybrid Supercapacitors as a Large-Scale Energy Storage Solution,” Energy and Fuels, 2023, 37, 4094–4105, DOI: 10.1021/acs.energyfuels.2c04092.

[16]	M. Minakshi,D. Meyrick, and D. Appadoo, “Maricite(NaMn1/3Ni1/3Co1/3PO4)/Activated Carbon: Hyrid Capacitor,” Energy Fuels 2013, 27, 6, 3516–3522, DOI: 10.1021/ef400333s.

[17]	A. Agarwal, S. Majumder, and B. R. Sankapal, “Carbon Nanotube-Functionalized Surface-Assisted Growth of Cobalt Phosphate Nanodots: A Highly Stable and Bendable All-Solid-State Symmetric Supercapacitor,” Energy and Fuels, 2022, 36, 5953–5964,DOI: 10.1021/acs.energyfuels.2c00600.

[18]	H. Li, H. Yu, J. Zhai, L. Sun, H. Yang, and S. Xie, “Self-assembled 3D cobalt phosphate octahydrate architecture for supercapacitor electrodes,” Mater. Lett., 2015, 152, 25–28, DOI: 10.1016/j.matlet.2015.03.053.

[19]	J. Seok, T. Hoai, T. Luu, and Y. H. Lee, “Author ’ s Accepted Manuscript,” Energy Storage Mater., 2017, DOI: 10.1016/j.ensm.2017.12.009.

[20]	P. K. Katkar, S. J. Marje, S. S. Pujari, S. A. Khalate, A. C. Lokhande, and U. M. Patil, “Enhanced Energy Density of All-Solid-State Asymmetric Supercapacitors Based on Morphologically Tuned Hydrous Cobalt Phosphate Electrode as Cathode Material,” ACS Sustain. Chem. Eng., 2019, 7, 11205–11218, DOI: 10.1021/acssuschemeng.9b00504.

[21]	B. Senthilkumar, Z. Khan, S. Park, K. Kim, H. Ko, and Y. Kim, “Highly porous graphitic carbon and Ni2P2O7 for a high performance aqueous hybrid supercapacitor,” J. Mater. Chem. A, 2015, 3, 21553–21561, DOI: 10.1039/c5ta04737d.

[22]	C. Chen et al., “Polypyrrole-Modified NH4NiPO4·H2O Nanoplate Arrays on Ni Foam for Efficient Electrode in Electrochemical Capacitors,” ACS Sustain. Chem. Eng., 2016, 4, 5578–5584, DOI: 10.1021/acssuschemeng.6b01347.

[23]	M. Minakshi Sundaram and D. R. G. Mitchell, “Dispersion of Ni2+ ions: Via acetate precursor in the preparation of NaNiPO4 nanoparticles: Effect of acetate vs. nitrate on the capacitive energy storage properties,” Dalt. Trans., 2017, 46, 13704–13713,DOI: 10.1039/c7dt02444d.

[24]	B. Liang et al., “Controllable Fabrication and Tuned Electrochemical Performance of Potassium Co-Ni Phosphate Microplates as Electrodes in Supercapacitors,” ACS Appl. Mater. Interfaces, 2018 10, 3506–3514, DOI: 10.1021/acsami.7b14552.

[25]	X. Liu et al., “Ni-Doped Cobalt-Cobalt Nitride Heterostructure Arrays for High-Power Supercapacitors,” ACS Energy Lett., 2018 3, 2462–2469, DOI: 10.1021/acsenergylett.8b01393.

[26]	Y. Liu, Z. Li, Y. You, X. Zheng, and J. Wen, “Synthesis of different structured FePO4 for the enhanced conversion of methyl cellulose to 5-hydroxymethylfurfural,” RSC Adv.,2017 7, 51281–51289, DOI: 10.1039/c7ra09186a.

[27]	S. Vivekanandhan, M. Venkateswarlu, and N. Satyanarayana, “Ammonium carboxylates assisted combustion process for the synthesis of nanocrystalline LiCoO2 powders,” Mater. Chem. Phys., 2008 109, 241–248, DOI: 10.1016/j.matchemphys.2007.11.027.

[28]	Gangulibabu, D. Bhuvaneswari, N. Kalaiselvi, N. Jayaprakash, and P. Periasamy, “CAM sol-gel synthesized LiMPO4 (M=Co, Ni) cathodes for rechargeable lithium batteries,” J. Sol-Gel Sci. Technol., 2009 49, 137–144, DOI: 10.1007/s10971-008-1870-5.

[29]	N. K. Mishra, R. Mondal, T. Maiyalagan, and P. Singh, “Synthesis, Characterizations, and Electrochemical Performances of Highly Porous, Anhydrous Co0.5Ni0.5C2O4for Pseudocapacitive Energy Storage Applications,” ACS Omega, 2022 7, 1975–1987, DOI: 10.1021/acsomega.1c05356.

[30]	C. Schlumberger and M. Thommes, “Characterization of Hierarchically Ordered Porous Materials by Physisorption and Mercury Porosimetry—A Tutorial Review,” Adv. Mater. Interfaces, 2021 8, 4, DOI: 10.1002/admi.202002181.

[31]	J. Wen et al., “Constructing Multifunctional Metallic Ni Interface Layers in the g-C3N4 Nanosheets/Amorphous NiS Heterojunctions for Efficient Photocatalytic H2 Generation,” ACS Appl. Mater. Interfaces, 2017 9, 14031–14042, DOI: 10.1021/acsami.7b02701.

[32]	A. Mukhtar, N. Mellon, S. Saqib, S. P. Lee, and M. A. Bustam, “Extension of BET theory to CO2 adsorption isotherms for ultra-microporosity of covalent organic polymers,” SN Appl. Sci., 2020 2, 1–4, DOI: 10.1007/s42452-020-2968-9.

[33]	G. Wang, Z. Yan, N. Wang, M. Xiang, and Z. Xu, “NiO/Ni Metal-Organic Framework Nanostructures for Asymmetric Supercapacitors,” ACS Appl. Nano Mater., 2021 4, 9034–9043, DOI: 10.1021/acsanm.1c01628.

[34]	N. K. Mishra, A. K. Singh, R. Mondal, and P. Singh, “NiC2O4 ⋅ 2H2O Nanoflakes: A Novel Redox-mediated Intercalative Pseudocapacitive Electrode for Supercapacitor Applications in Aqueous KOH and Neutral Na2SO4 electrolytes,” ChemistrySelect, 2022 7, 21, DOI: 10.1002/slct.202201134.

[35]	N. K. Mishra, R. Mondal, and P. Singh, “Synthesis, characterizations and electrochemical performances of anhydrous CoC2O4nanorods for pseudocapacitive energy storage applications,” RSC Adv., 2021 11, 33926–33937, DOI: 10.1039/d1ra05180f.

[36]	R. Sa hoo et al., “Redox-Driven Route for Widening Voltage Window in Asymmetric Supercapacitor,” 2018, DOI: 10.1021/acsnano.8b04040.

[37]	N. R. Chodankar et al., “True Meaning of Pseudocapacitors and Their Performance Metrics: Asymmetric versus Hybrid Supercapacitors,” Small, 2020 16, 1–35, DOI: 10.1002/smll.202002806.

[38]	N. B. Velhal et al., “Exploring the Effect of Ultrafast Intensive Pulsed Light (IPL) Annealing on the Structure and Performance of Cobalt Oxide Electrodes for Supercapacitors,” ACS Appl. Energy Mater., 2023 6, 7405–7418, DOI: 10.1021/acsaem.3c00656.

[39]	S. Rudra et al., “Redox-Guided Synthesis of Au-V2O5-MnO2 Nanoflower Composites with Enhanced Electrical Conductance for Supercapacitor Applications,” ACS Appl. Nano Mater., 2023 6, 1648–1659, DOI: 10.1021/acsanm.2c04584.

[40]	S. Sathishkumar et al., “Bimetal Pyrophosphate of CoNiP2O7@polypyrrole Nanocomposite- Based Electrode for Hybrid Supercapacitor Applications,” Energy Technol., 2024 2301589, 1–12, DOI: 10.1002/ente.202301589.

[41]	P. Matheswaran, P. Karuppiah, S. M. Chen, and P. Thangavelu, “A binder-free Ni2P2O7/Co2P2O7nanograss array as an efficient cathode for supercapacitors,” New J. Chem., 2020 44, 13131–13140, DOI: 10.1039/d0nj00890g.

[42]	M. Z. Iqbal et al., “Copper doped cobalt-manganese phosphate ternary composites for high-performance supercapattery devices,” J. Energy Storage, 2020 35, 102307, 2021, DOI: 10.1016/j.est.2021.102307.

Table 1 Comparative Study of Electrochemical Performances of Cobalt and Nickel-based Phosphate Electrode Materials in Full Cell.

| Electrode material (Negative Electrode//Positive Electrode) | Electrolyte | Specific Capacitance | Energy density /Power Density | Ref. |
| --- | --- | --- | --- | --- |
| AC//γ-KCoPO4 | 1M KOH | 100 C/g at 0.6 mA/cm2 | ED=28 Wh/kg at PD=1600W/kg | [11] |
| AC//KNiPO4 | 2MKOH | 168.5 mAh/g (Capacitance: 935 F/g ) at 1 A/g | ED=200 Wh/kg PD=819 W/kg | [15] |
| AC// NaMn1/3Ni1/3Co1/3PO4 | 2M NaOH | 45 F/g at 0.5A/g | ED=15 Wh/kg PD=400 W/kg | [16] |
| AC// Co2P2O7/MWCNT | 1M KOH | 114 mAh/g at 2.9A/g | ED=57.3 Wh/kg at PD=4100 W/kg | [17] |
| AC// Co3(PO4)2 | 1M NaOH | 111.2 F/g at 5mA/cm2 | ED=29.20 Wh/kg at PD= 4687 W/kg | [18] |
| AC// Co3(PO4)2·8H2O | 1M KOH | 163 F/g at 2mA/cm2 | ED=58.12 Wh/kg at PW=3520 W/kg | [20] |
| HPGC//Ni2P2O7 | 1M NaOH | 183F/g at 1A/g | ED= 65 Wh/kg at PD=800W/kg | [21] |
| AC//NH4NiPO4·H2O | 3M KOH | 1513 F/g at 5 A/g | ED= 41.6 Wh/ kg at PD= 375 W/kg | [22] |
| AC// NaNiPO4 | 2M NaOH | 90 F/g at 0.3A/g | ED= 32 Wh/kg at PD= 300 W/kg | [23] |
| AC// KCo0.33Ni0.67PO4·H2O | 1M KOH | 227F/g at 1.5A/g | ED=80.64 Wh/kg at PW=8000 W/kg | [24] |
| AC// CoNiP2O7/NF@PPy | 2M KOH | 390mAh/g at 2A/g | ED= 94.6Wh/kg at PD=2791W/kg | [40] |
| AC// Ni2P2O7/Co2P2O7 | 2M KOH | 2074F/g at 5A/g | ED= 33.3 Wh/kg at PD= 257 W/kg | [41] |
| AC//Co0.125Cu0.375Mn0.5(PO4)2 | 1M KOH | 158.5F/g @1A/g | ED=56Wh/kg at PD=6420W/kg | [42] |
| AC//KCoPO4 | 2M KOH | 387F/g at 1A/g | ED=121 Wh/kg at PD= 6947 W/kg | Previous work |
| AC//KCo0.5Ni0.5PO4 | 2MKOH | 173mAh/g @0.5A/g | ED=183.5Wh/kg at PD=7952W/kg | This work |

Figure 1 Schematic of synthesis of KCo0.5Ni0.5PO4 sample.

Figure 2. Powder XRD pattern of KaCo1-xNixPO4 ( x = 0, 0.1, 02, 0.3, 0.4, and 0.5)

Figure 3 (a) XRD Rietveld refinement pattern of KCo0.5Ni0.5PO4 powder sample (b) VESTA image of KCo0.5Ni0.5PO4 (blue, green, grey are tetrahedra of Co-O, Ni-O and P-O, respectively)(c) FTIR spectrum of KCo0.5Ni0.5PO4 (d) N2 adsorption/desorption isotherm of KCo0.5Ni0.5PO4 sample

Figure 4. XPS of KCo0.5Ni0.5PO4 of powder sample; (a) full survey, (b) K (1s), (c) Co(2p), (d) Ni(2p), (e) O (1s) and (f) P (2p)

Figure 5. (a) Particle distribution of KCo0.5Ni0.5PO4 in SEM   image, (b) elemental analysis of KCo0.5Ni0.5PO4 by EDX. (c)-(g) Colour mapping of the element present in KCo0.5Ni0.5PO4.

Figure 6 (a) visible lattice fringes containing 600 planes in HRTEM image, (i-ii): FFT and inverse FFT images of the selected region of the (600) plane. (b) shows d spacing of fringes that matches with the (600) plane of the KCo0.5Ni0.5PO4 lattice.

Figure 7. Comparative CV of KCo1-xNixPO4 (x = 0, 0.1, 0.3 and 0.5) in 2M KOH electrolyte solution and 5mV/s scan rate.

Figure 8  (a) cyclic voltammetry of KCo0.5Ni0.5PO4  electrode in 2 M KOH electrolyte, (b) peak current density vs square root of the scan rates plot, (c) plot of log (peak current) vs log (scan rate) presenting b Values, (d) capacitive and diffusion control process contribution in the current density at the scan rate of 0.5 mV/s, (e) presenting surface capacitance and diffusion-controlled interaction process contribution at a scan rate 0.5 mV/s on the charging peak potential equal to 0.31V and (f) capacitive and diffusion control process contribution at different scan rates.

Figure 9 (a) C−1vs. ν1/2 (b) C vs. ν−1/2 derived from Trasatti’s method.

Figure 10. (a) Charge/discharge plot (V vs time) of the KCo0.5Ni0.5PO4 electrode at various constant current rates (0.5, 1, 2, 3, 4 and 5A/g), (b) capacity/capacitance performance of the KCo0.5Ni0.5PO4    in 2 M KOH electrolyte at different current densities, (c) Capacity retention and Coulombic efficiency plot and (d) Nyquist plot before and after cycle at 10 mV applied voltage in the frequency range of 1 MHz to 0.1 Hz.

Figure 11. (a) CV curves AC and KCoPO4 electrode at 5 mV/s in a three-electrode system, (b) CV curves of AC//KCo0.5Ni0.5PO4   as HSCs in 2MKOH at different scan rates, (c) Specific capacity of AC// KCo0.5Ni0.5PO4  as HSCs in 2MKOH at different current density, (d) capacitive retention and coulombic efficiency of the HSCs device, (e) Nyquist at initial cycle and after 5000 cycles of the full cell in HSCs mode (f) Ragone plot of AC// KCo0.5Ni0.5PO4  as HSCs with another literature report.