Density Functional Theory Studies on Tuning TaXTi(1-X)S2 For Insoluble Li2S2-Li2S Conversion in Lithium-Sulfur Batteries

Jinyan Chena, Shuai Zhaoa, Yuhan Wanga, Ruiyu Haoa, Chao Gaoa, Jianhua Houa,b*

aSchool of Materials Science and Engineering, Changchun University of Science and Technology, Changchun 130022, PR China

bEngineering Research Center of Optoelectronic Functional Materials, Ministry of Education, Changchun 130022, PR China

Corresponding author: houjh163@163.com

Abstract

Due to the complexity of insoluble Li2S2-Li2S conversion, few descriptors exist to correlate the catalytic performance and the underlying electronic structures of a given catalyst, which inhibits the development of lithium−sulfur catalysts. In this article, we employ the cluster expansion method to select 17 optimal structures for TaXTi(1-X)S2 (0≤X≤1) and apply density functional theory calculations to probe the electronic structures and the conversion of Li2S2 to Li2S relationships across different doping concentrations. We found the simultaneous pathway is most possible in propose five possible reaction pathways. Notably, we identify Ta0.38Ti0.62S2 as a promising candidate for electrocatalytic applications in the conversion from Li2S2 to Li2S. Furthermore, our study analyzes the charge transfer of Li2S2(QLi2S2), the electronegative difference(ΔX), the adsorption energy of Li2S(EaLi2S), and work function(WF) significantly influence the conversion process from Li2S2 to Li2S by machine learning based on various descriptors. This research contributes to a deeper theoretical understanding of the complex mechanisms underlying the Li2S2-Li2S conversion and provides valuable insights into the rational design of sulfur redox catalysts.

Keywords: insoluble Li2S2-Li2S conversion, cluster expansion method, density functional theory, machine learning, descriptors

1. Introduction

Lithium-sulfur batteries(LSBs) are considered promising candidates for replacing traditional lithium-ion batteries due to their ultra-high energy density, as well as the low cost[1-3]. During the discharge cycle, the active S₈ molecules undergo a reduction process, transforming into various lithium polysulfides (LiPSs) and ultimately yielding Li₂S through a comprehensive 16-electron sulfur reduction reaction (SRR)[4]. The rate-determining step observed in most catalytic materials such as the conversion of Li₂S₂ to Li₂S plays a critical role in determining the theoretical capacity of LSBs[5-7]. Nevertheless, slow reaction kinetics often impeded this conversion process, which is primarily attributed to sluggish solid-phase diffusion and associated reaction dynamics[8-9]. Consequently, particular attention has been directed towards understanding the conversion of Li₂S₂ to Li₂S in LSBs research; However, the reaction mechanism remains inadequately defined at this time[10-11].

Theoretical investigations have been conducted trying to clarify the mechanism of the Li2S2 conversion reaction. Notably, Peng et al. demonstrated a conversion pathway for Li2S2 that incorporates electrolyte solvent, employing the Gibbs free energy (ΔG) of adsorbed LiS intermediates as an activity descriptor[4]. Their findings contribute valuable insights into the understanding of Li2S2 conversion mechanisms. Wang et al. proposed that the accelerated conversion kinetics of LiPSs can be attributed to a more negative Gibbs free energy (ΔG < 0) occurring during the formation of Li2S2 and Li2S at the edges of materials such as Cr3S4, MoS2, and WS2[12]. However, the inherent complexities of the two-electron transfer process (Li2S2 + 2Li+ + 2e- → 2Li2S)[13-14], particularly the breaking and recombination of Li−S bonds, pose significant challenges for experimental observation. Furthermore, their analysis did not sufficiently account for the impact of intermediates on the overall reactivity. Fang et al. introduced three plausible intermediates (LiS, Li3S2, and S) across three distinct reaction pathways. Nevertheless, their analytical approach primarily relied on the difference between the d-band center and p-band (Δd-p), as well as Pauli electronegativity, which may not comprehensively capture the intricacies of the reaction dynamics[15]. Further investigation into intermediate states, their interactions, and the underlying reasons for ΔG < 0 could yield deeper insights into examining the conversion process and enhancing the overall performance of LSBs.

The revealed research indicated that ΔG < 0 with the conversion from Li2S2 to Li2S has primarily been examined in the context of transition metal dichalcogenides (TMDs) and single atoms doped TMDs (SACs-TMDs), such as TiS2[16], NbS2[17], CoSe2[18], Be-TiS2, Mg-TiS2[16], and so on. However, the specific roles and influences of TMDs and SACs-TMDs on the dissociation of Li2S2 remain inadequately understood. In this study, we consider the remarkable properties of TiS2, which include a high metal ion adsorption capacity, low diffusion barriers, and intrinsic semi-metallic band gap-driven chemical and electronic properties[19]. Furthermore, experimental synthesis of TaXTi(1-X)S2 (0<x<0.14) has further confirmed its stability and feasibility for practical applications[20-21]. Therefore, TaXTi(1-X)S2 (0≤X≤1) was chosen as the subject of our study. We are dedicated to addressing the knowledge gap by machine learning to investigate the complex Li2S2 to Li2S and intermediate states interactions that are influenced by tuning doping concentrations in TaXTi(1-X)S2.

We focus on the relationship between the electronic structures of TaXTi(1-X)S2 and the conversion from Li2S2 to Li2S. It is found that the simultaneous pathway is easier to form than the other pathways on TaXTi(1-X)S2, and the Ta0.38Ti0.62S2 serves as the optimal electrocatalyst for the conversion from Li2S2 to Li2S. Moreover, Our analysis reveals that factors such as the charge transfer of Li2S2(QLi2S2), the electronegative difference(ΔX), the adsorption energy of Li2S(EaLi2S), and work function(WF) significantly influence the conversion process from Li2S2 to Li2S. Our findings offer valuable theoretical insights into the intricate sulfur redox reactions and pave the way for the rational design of electrocatalysts within the realm of Li−S chemistry.

2. Calculation method

The structures of TaXTi(1-X)S2(0≤X≤1) are obtained by exploring the configurations space with cluster expansion (CE) method implanted[22] combined with fist-principle calculations. Density functional theory(DFT) calculations were carried out using the Vienna ab initio simulation package (VASP)[23]. The projector augmented-wave method with a 520 eV energy cutoff for the plane-wave basis set was adopted to treat the core-valence electron interactions. The electron exchange-correlation interactions were calculated by the generalized gradient approximation (GGA) in the Perdew-Burke-Ernzerhof (PBE)[24]. The Brillouin-zone integration was sampled with an 11 × 11 × 1 Monkhorst-Pack k-grid mesh for geometry optimization. All the lattice parameters and atomic positions were fully optimized until the force tolerance was below 0.05 eV Å-1.

The reaction Gibbs free energy (ΔG) of each step is given by

∆G = ∆E+ ∆EZPE-T∆S                         (1)

the ∆E, ∆EZPE, and ∆S are the DFT calculated energy, the changes of zero-point energy, and entropy between products and reactants, respectively. T is the temperature[18].

To have a deep insight into the electronic properties of TaXTi(1-X)S2, we calculated the work function (Φ) of TaXTi(1-X)S2. The work function is the minimum amount of energy required to remove an electron from the Fermi level to infinity, which can be evaluated as:

Φ= V (∞) − EF                          (2)

Where Φ was the work function, V (∞) was electrostatic potential at the vacuum level, and EF was the Fermi energy of TaXTi(1-X)S2[25].

3 Results and discussion

3.1 Structures and stability of TaXTi(1-X)S2(0≤X≤1)

To explore the potential structures in TaXTi(1-X)S2(0≤X≤1) monolayer, the cluster expansion (CE) method combined with 4x4x1 supercell of TiS2 is adopted, atomic structure diagram of the original TiS2 is illustrated in Figure 1(a). CE can analyze all the structures with different concentrations x in configuration space, the structures at other concentrations are as indicated in Figure 1(a). The CE calculations were conducted on structures comprising 48 atoms, identifying 17 distinct ratio sets and 517 possible structures within the TaXTi(1-X)S2 monolayer framework. Based on these constructed atomic structures, first-principle calculations were performed on randomly selected 54 structures. To assess the stability of this TaXTi(1-X)S2(0≤X≤1), we initially examined its formation energy (EForm). In the calculations, the formation energy is defined by the formula.

EForm=ETaXTi(1-X)S2 — [xETaS2— (1—x)ETiS2]           (3)

where ETaXTi(1-X)S2, ETaS2, and ETiS2 are the total energies of ETaXTi(1-X)S2, TaS2, and TiS2, respectively. Figure 1(a) shows EForm obtained from PBE of first-principles calculations and the CE method. The EForm of all configurations is negative for the whole range of compositions, which indicates that it is easy for TaS2 and TiS2 to form TaXTi(1-X)S2. For TaXTi(1-X)S2, the cross-validation fraction of the CE simulations and PBE of first-principles calculations is 0.012 eV[26], which indicates that the CE method is sufficiently accurate in predicting the variation of the formation energy of TaXTi(1-X)S2 with Ta concentration.

The energy band structure calculations carried out at the GGA layer are shown in Fig. 1(b) and Fig. S1(a-n), the TiS2 monolayer has semi-metallicity has energy band overlap consistent with findings from other studies[16]. With the doping of Ta atoms, TaXTi(1-X)S2 shows typical metallic nature, whose electronic orbitals across the Fermi level. Projected density of states (PDOS) analysis presented in Figure 1(c) indicates that the valence band minimum (VBM) of TiS2 is primarily derived from Ti-3d states, while the conduction band minimum (CBM) is predominantly contributed by both Ti-3d and S-3p states, which are in agreement with previous studies[27]. Similarly, for TaS2, the VBM mainly comprises Ta-3d states, while the CBM arises primarily from the combination of Ta-3d and S-3p states[28]. For the TaXTi(1-X)S2, the VBM is predominantly contributed by both Ti-3d and Ta-3d states, while the CBM is primarily composed of Ti-3d and Ta-3d, and S-3p states.

The d orbital electron is affected by the doping concentration of Ta atoms and the position of the Fermi level, d band center and p band center changes accordingly. As shown in Table 1, the difference between the d band and p band of TaXTi(1-X)S2 (Δd-p) ranges from 1.43 to 2.32. The trend of work function (WF) decreases gradually from 6.01 to 5.55eV with increasing doping concentration, suggesting that doping concentration influences an upward shift in the Fermi level. Since electronegativity affects the ability of interatomic charge transfer and thus the strength of adsorption, we further calculated the electronegativity difference (ΔX) between the metal and S of TaXTi(1-X)S2. The trend of ΔX is similar, which descends gradually from -1.04 to -1.08 with increasing doping concentration.

Figure 1. (a) The formation energy of TaXTi(1-X)S2 (0≤X≤1) Predicted structures (blue crosses) obtained using the CE method. The yellow crosses represent structures calculated using DFT. The top and side views of the monolayer TiS2, Ta0.38Ti0.62S2, and TaS2 structures, respectively. The grey, green, and yellow atoms are Ti, Ta, and S, respectively. (b) Energy band structure and (c) PDOS of TiS2, Ta0.38Ti0.62S2, and TaS2 monolayer.

Table 1. The parameters include the difference between d band center and p band (Δd-p), work function (WF), and electronegativity difference between the metal and S (ΔX) of TaXTi(1-X)S2(0≤X≤1).

| System | Δd-p | WF(eV) | ΔX |
| --- | --- | --- | --- |
| TiS2 | 2.04 | 6.01 | -1.04 |
| Ta0.06Ti0.94S2 | 1.45 | 5.93 | -1.04 |
| Ta0.13Ti0.87S2 | 1.43 | 5.88 | -1.05 |
| Ta0.19Ti0.81S2 | 2.06 | 5.85 | -1.05 |
| Ta0.25Ti0.75S2 | 1.76 | 5.82 | -1.05 |
| Ta0.31Ti0.69S2 | 2.08 | 5.80 | -1.05 |
| Ta0.38Ti0.62S2 | 2.08 | 5.71 | -1.06 |
| Ta0.44Ti0.56S2 | 2.08 | 5.74 | -1.06 |
| Ta0.5Ti0.5S2 | 2.08 | 5.71 | -1.06 |
| Ta0.56Ti0.44S2 | 2.02 | 5.74 | -1.06 |
| Ta0.63Ti0.37S2 | 2.02 | 5.71 | -1.07 |
| Ta0.69Ti0.31S2 | 2.30 | 5.71 | -1.07 |
| Ta0.75Ti0.25S2 | 2.27 | 5.69 | -1.07 |
| Ta0.82Ti0.18S2 | 2.30 | 5.66 | -1.07 |
| Ta0.88Ti0.12S2 | 2.30 | 5.63 | -1.08 |
| Ta0.94Ti0.06S2 | 2.30 | 5.61 | -1.08 |
| TaS2 | 2.32 | 5.55 | -1.08 |

3.2 Determination of intermediates

In practical LSBs, the SRR process of Li2S2 + 2Li+ + 2e− → 2Li2S involves a complex electron conversion[4]. According to the Sabatier principle[29], the complexity of this conversion is influenced not only by the Gibbs free energy between the reactants and products but also by the energy barrier associated with specific reaction pathways and intermediates. Recently, researchers have proposed several possible chemical mechanisms and intermediates for the conversation step, and the Gibbs free energy change between the intermediates and both initial and final states has been utilized to predict catalyst performance, corroborated by empirical observations. We investigated the adsorption behaviors of Li2S2 and Li2S on TaXTi(1-X)S2 and determined that the conversion from Li2S2 to Li2S involves the breaking and recombination of Li-S bonds, as shown in Figure 2 and S2-17. Consequently, we propose two reasonable intermediates (LiS, and Li3S2)[30] in five possible reaction pathways (as depicted in Figure 3(a))[14]

Pathway 1(P1)

ΔG1:*Li2S2 + * + 2Li+ + e- → 2*Li2S               (4)

Pathway 2(P2)

ΔG1:*Li2S2 + * + Li+ + e- → *Li2S + *LiS             (5)

ΔG2:*LiS + Li+ + e- → *Li2S                    (6)

Pathway 3(P3)

ΔG1:*Li2S2 + * → 2*LiS                     (7)

ΔG2:*LiS + Li+ + e- → *Li2S                   (8)

Pathway 4(P4)

ΔG1:*Li2S2 + Li+ + e- → *Li3S2                 (9)

ΔG2:*Li3S2+* → *Li2S+*LiS                  (10)

ΔG3:*LiS + Li+ + e- → *Li2S                  (11)

Pathway 5(P5)

ΔG1:*Li2S2 + Li+ + e- → *Li3S2                 (12)

ΔG2:*Li3S2+*+ Li+ + e- → 2*Li2S                (13)

where symbol * represents a substrate with an active surface.

There is an associative pathway in which two Li+ interact with Li2S2 simultaneously, referred to as the simultaneous pathway(Eq.(4)). It is a pathway that skips the formation of intermediates, as is manifested in P1. In P2, adsorbed Li2S2 decomposes into Li2S product and LiS intermediate, which LiS bonds with Li atoms to form Li2S (as shown in Eq.(5 and 6)). When Li2S2 decomposes before its adsorption, because Li+ and electron is impossible to encounter each other in electrolyte, only LiS intermediates will form. Then the intermediates adsorb on the electrode surface. LiS intermediates, Li+ and electron encounter at this time to form Li2S. In other words, Li2S2 reduction reaction becomes the combination of two one-electron process. It can be described by P3(as shown in Eq.(7 and 8)). P4 describes that adsorbed Li2S2 combines with one Li atom to spontaneously form a Li3S2 cluster, which Li3S2 decomposes into one Li2S product and one LiS intermediate. The LiS intermediate then transforms into Li2S by bonding with another Li atom (as shown in Eq. (9-11)). Finally, in P5, adsorbed Li2S2 combines with one Li atom to spontaneously form a Li3S2 cluster, which transforms into two Li2S by bonding with another Li atom (Eq.(12 and 13)).

3.3 Adsorption energy on TaXTi(1-X)S2

Figure 2. (a)Calculated adsorption energies of LiS, Li2S, Li2S2, and Li3S2 on TaXTi(1-X)S2. Optimized geometrical configurations of (b)Li2S, (c)LiS, (d)Li2S2, and (e)Li3S2 on Ta0.38Ti0.62S2. The grey, green, yellow-brown, and purple atoms are Ti, Ta, STa0.38Ti0.62S2, SLiPSs, and Li respectively.

We selected 17 atomic configurations that exhibited the lowest formation energies as illustrated in Figure 1(a) at each scale ranging from 0 to 1, and adsorbed LiS, Li2S, Li2S2, and Li3S2. The anchoring behavior of TaXTi(1-X)S2 is investigated through the calculation of adsorption energies for LiPSs, employing the formula:

Ea = ELiPSs + ETaXTi(1-X)S2− ELiPSs+TaXTi(1-X)S2               (14)

where ELiPSs, ETaXTi(1-X)S2, and ELiPSs+TaXTi(1-X)S2 correspond to the DFT energies of the LiPSs, TaXTi(1-X)S2, and theLiPSs adsorbed TaXTi(1-X)S2, respectively. As demonstrated in Figure 2(a) and Table S1, the overall trend of adsorption energy(Ea) on TaXTi(1-X)S2 shows a consistent pattern: Li2S>Li3S2>LiS>Li2S2. Based on the optimized structures depicted in Figure 2(b-e) and Figure S2-17, it is observed that LiS, Li2S, Li2S2, and Li3S2 maintain their original conformation during adsorption. Moreover, for Li2S and LiS, both the S atoms and Li atoms of Li2S and LiS boned with the STaXTi(1-X)S2 atom of TaXTi(1-X)S2. For Li2S2 and Li3S2, however, only the Li atoms interact with the S atom of TaXTi(1-X)S2, as illustrated in Figures 2(b-e) and S2-17..

Table S2 shows that the bond lengths of Li-STaXTi(1-X)S2 (dLiS, dLi2S, dLi2S2 and dLi3S2) increase as the number of S atoms in Li2S, LiS, Li3S2, and Li2S2 grows, which accords with previous studies[31-32]. The strength of the Li-STaXTi(1-X)S2 bond can be quantified by the integral of the Crystal Orbital Hamilton Population (ICOHP) up to the Fermi level 34. The more negative value of ICOHP corresponds to the stronger bond strength. The variation trend of ICOHP follows the same pattern as the bond lengths of Li-STaXTi(1-X)S2. As displayed in Figure S18, the Li-STaXTi(1-X)S2 bond strength presents the most negative value of Li2S, indicating that the Li-STaXTi(1-X)S2 bond of Li2S is more steady and hard to break.

Electrons are primarily transferred between the Li-STaXTi(1-X)S2 bonds in the LiPSs and the TaXTi(1-X)S2 surface, leading to surface electron rearrangement[33]. Electrons are mainly transferred between Li-STaXTi(1-X)S2 bond and result in surface electron rearrangement. The positive value of the transfer charge for the Li2S, Li3S2, LiS, and Li2S2 (∆eLiPSs) and negative transfer value for TaXTi(1-X)S2 (ΔeTaXTi(1-X)S2) indicate that the charge migrates from the LiPSs to TaXTi(1-X)S2, as shown in Table S3. Among LiPSs, LiS exhibits the smallest amount of charge transfer. As shown in Table 1, LiS, which contains only one Li and one S atom, undergoes the least electron loss compared to Li3S2, Li2S2, and Li2S. Except LiS, other LiPSs follow the rule that the larger the adsorption energy, the more the charge transfer. This charge transfer results in electron rearrangement on the TaXTi(1-X)S2 surface[34], which in turn leads to an increase in the surface Fermi level, thereby decreasing ∆WF. A notable decrease in ΔWFLi3S2 (shown in Table S4) due to the rise in the Fermi level of the TaXTi(1-X)S2 surface after Li3S2 adsorption. The electron transfer from LiPSs to the TaXTi(1-X)S2 surface plays a crucial role in altering the electronic structure, with implications for catalytic properties of TaXTi(1-X)S2.

3.4 The Gibbs free energy of TaXTi(1-X)S2(0≤X≤1)

To investigate the reaction-path dependent activity, we calculated the Gibbs free energy (ΔG1, ΔG2, and ΔG3) for Pathway 1-5 by Eq.(2), and listed the values of all five possible pathways on TaXTi(1-X)S2 in Figure 3. The negative energy in the response is spontaneous in Figure 3(b and e). From a thermodynamic perspective, the most probable reaction pathways on TaXTi(1-X)S2 are based on the values of ΔG < 0, which could involve the reaction of Li−SLiPSs bond decomposition. The result in Figure 3 shows that Pathways 1 and 5 are possible due to their value of ΔG being mostly negative, implying that Li2S are easily generated in Pathways 1 and 5. But there are still ΔG1 and ΔG2 of TaS2, and ΔG2 of Ta0.56Ti0.44S2 are positive in path 5, which means the catalyst necessitates a greater energy input for the conversion process. At the same time, the ΔG value of path 1 is more negative than the ΔG value of path 5, which means ΔG is more likely to proceed spontaneously on path 1 than on path 5. Therefore, the most possible pathway is the simultaneous pathway which is an associative pathway in which two Li+ interact with Li2S2 simultaneously. In other words, this may be the reason why the ΔG < 0 when Li2S2 to Li2S are transformed on TaXTi(1-X)S2.

In addition, the Li3S2 intermediates are easier to form than LiS intermediates because the relevant value is negative, which means the step involving the conversion of Li2S2 to Li3S2 is exothermic on TaXTi(1-X)S2 (except TaS2). For Ta0.38Ti0.62S2, the smaller negative values of ΔG1 and ΔG2 in P1 or 5 than other TaXTi(1-X)S2. This suggests that Ta0.38Ti0.62S2 is an optimal electrocatalyst for the conversion from Li2S2 to Li2S.

Figure 3. (a)Schematic diagram for five possible reaction pathways in the conversion from Li2S2 to Li2S on TaXTi(1-X)S2. (b)The first step Gibbs free energy (ΔG1), (c)the second step Gibbs free energy (ΔG2), and (d)the third step Gibbs free energy (ΔG3) in five possible reaction pathways on TaXTi(1-X)S2.

3.5 Explore the key descriptors affecting the Gibbs free energy using machine learning

To reveal the intrinsic relationship between the simultaneous pathway(P1) and structure of TaXTi(1-X)S2 and to develop effective and rational principles for designing catalysts, we hope that some simple and feasible descriptors can be found to accurately predict ∆G. Related studies have analyzed the existence of a relationship between ΔX, Δd-p, ICOHP and ∆G. For example, Pei et al. introduce ΔX as a descriptor to describe ∆G, due to the magnitudes of charge transfer between atoms being closely related to the values of their electronegativities[35]. The energy of the electrons in the p and d orbitals will have a direct impact on the formation and breaking of the bonds, therefore, Liu et al. introduce Δd-p as a descriptor to describe ∆G[36]. Moreover, Wu et al. introduced that the integral value of crystal orbital Hamiltonian population (ICOHP) of the Li-S bond in the adsorbed Li2S can be an excellent descriptor for evaluating the overall catalytic ability of substrates[37]. Collectively, these studies highlight the potential of these descriptors, such as ΔX, Δd-p, and ICOHP, as tools for predicting ∆G and guiding the rational design of efficient catalysts.

For comprehensive and systematic evaluation of the descriptors, here we considered a total as follows descriptors including the adsorption energy (EaLiS, EaLi2S, EaLi2S2, and EaLi3S2), the integral of the Crystal Orbital Hamilton Population (ICOHPLiS, ICOHPLi2S, ICOHPLi2S2, and ICOHPLi3S2), the Li-STaXTi(1-X)S2 bond length (dLiS, dLi2S, dLi2S2, and dLi3S2)， the charge transfer of LiPSs (QLiS, QLi2S, QLi2S2 and QLi3S2), the electronegativity differences between the metal atoms and the sulfur atom (ΔX), the difference between d-band center and p-band of TaXTi(1-X)S2(0≤X≤1) (Δd-p), the work function (WF) and the difference of WF(ΔWFLiS, ΔWFLi2S, ΔWFLi2S2 and ΔWFLi3S2) before and after adsorption.

To enhance the efficiency of the machine learning algorithm and mitigate the risk of overfitting[38], we selected the descriptors that exhibit the strongest correlations with ∆G, based on their Pearson correlation coefficients. The Pearson correlation coefficients for each descriptor are presented in Figure 4(a), with the detailed values provided in Tables S5. Combining all the above-mentioned parameters, we further adopted a machine learning method, i.e., the sure independence screening and sparsifying operator (SISSO), to build a useful mathematical model with physical meaning[39].

To evaluate the validity of the model, the physical parameters of the TaXTi(1-X)S2 system were selected as the training dataset in P1. The form of the optimal SISSO model with the root-mean-square error (RMSE) of 0.14 eV, is expressed as:

ΔG=4.71*(2EaLi2S/QLi2S2+EaLi2S)-14.60*(WF*ΔX*QLi2S2/EaLi2S)-45.08     (15)

As shown in Figure 4(b), the predicted ΔG based on this mathematical model are extent consistent with the DFT calculated results. According to Eq. (15), for TaXTi(1-X)S2 with the complex coordination environment, charge transfer of Li2S2(QLi2S2), the electronegative difference(ΔX), the adsorption energy of Li2S(EaLi2S), and work function(WF) would work together to determine the ΔG for Li2S2 to Li2S.

In order to further obtain the key factors affecting ΔG in the existing descriptors to gain more insight into the constructive relationship between TaXTi(1-X)S2 structure and activity, we evaluate the importance of the descriptors. The outputs are shown in Figure 4(b). The adsorption energy of EaLi2S is the most important factor affecting the ΔG in P1, with its proportion at 37.9%. This observation is consistent with the findings of Zhao et al.[18], who noted that the difference between EZPE and TΔS is minimal (less than 0.05 and 0.1 eV, respectively), which simplifies the calculation of ΔG. These results suggest that ΔE plays a significant role in determining the ΔG, and an increase in ΔE leads to an elevated Ea. This indicates a fundamental relationship between Ea and ΔG, further highlighting the importance of adsorption energy and electron transfer in modulating the catalytic process. In addition, our analysis reveals the QLi2S2 be a significant contributor (accounting for 24%) to the catalytic activity within our model framework. These findings are consistent with prior studies emphasizing the critical role of electron transfer in catalytic processes[40].

Meanwhile, electronegativity difference between the substitutional metal atoms and sulfur atom (ΔX) and work function (WF) of the TaXTi(1-X)S2 were conducive to affecting the interaction between TaXTi(1-X)S2 and LiPSs[25]. In our model, ΔX contributes 18.8%, while WF contributes 19.3%. These variables collectively influence the electronic interactions that determine catalytic behavior. Although the model demonstrates strong predictive performance within the training set, it is important to acknowledge the potential limitations of the mathematical model, due to the relatively small size of the training data.

Figure 4. (a) The correlation (Pearson correlation coefficient) between a single parameter and the Gibbs free energy of pathway 1. (b) Fitting results between the DFT-calculated Gibbs free energy values of pathway 1 and the sure independence screening and sparsifying operator (SISSO) algorithm predicted ones based on the TaXTi(1-X)S2, and the importance of features affecting ΔG.

4. Conclusion

In summary, we have investigated Li2S2-Li2S conversion on TaXTi(1-X)S2(0≤X≤1) based on the adsorption of Li2S2, Li2S, and Li3S2, LiS, the Gibbs free energy(∆G), and electronic structure analysis. The DFT calculation identifies the most likely reaction pathways as Pathway 1, and Li3S2 being the possible intermediate product during the conversion from Li2S2 to Li2S on TaXTi(1-X)S2. Notably, the Ta0.38Ti0.62S2 can effectively decrease ΔG compared to other TaXTi(1-X)S2, significantly facilitating the conversion from Li2S2 to Li2S. In addition, we employed the sure independence screening and sparsifying operator (SISSO) based on machine learning to screen and construct simple and effective descriptors to predict ΔG and derive their corresponding analytical expressions. By analyzing the importance of the descriptors, we pointed out that the charge transfer of reactants(QLi2S2), the electronegative difference(ΔX), the high adsorption energy of Li2S(EaLi2S), and work function(WF) affect together ΔG. This analysis provides valuable insights into the relationship between doping concentration and the Li2S2-Li2S conversion process. Our findings demonstrate that the machine learning approach we used is instructive for theoretical studies of Li2S2-Li2S reactions, opening a new window for rapid screening of efficient Li2S2 to Li2S catalysts.

Acknowledgment

This work is financially supported by the Scientific and Technological Development Project of Jilin Province, China (Grant No. 20240101111JC).

References

[1]	H. J. Peng, J. Q. Huang, X. B. Cheng, Q. Zhang, Advanced Energy Materials 2017, 7, 1700260.

[2]	A. Manthiram, Y. Fu, S.-H. Chung, C. Zu, Y.-S. Su, Chem. Rev. (Washington, DC, U. S.) 2014, 114, 11751-11787.

[3]	M. A. Pope, I. A. Aksay, Advanced Energy Materials 2015, 5, 1500124.

[4]	L. Peng, Z. Wei, C. Wan, J. Li, Z. Chen, D. Zhu, D. Baumann, H. Liu, C. S. Allen, X. Xu, Nature Catalysis 2020, 3, 762-770.

[5]	Z. Wang, H. Ji, L. Zhou, X. Shen, L. Gao, J. Liu, T. Yang, T. Qian, C. Yan, ACS Nano 2021, 15, 13847-13856.

[6]	R. Yan, Z. Zhao, M. Cheng, Z. Yang, C. Cheng, X. Liu, B. Yin, S. Li, Angewandte Chemie International Edition 2022, 62.

[7]	L. Zhou, D. L. Danilov, F. Qiao, J. Wang, H. Li, R. A. Eichel, P. H. L. Notten, Advanced Energy Materials 2022, 12.

[8]	J. Xie, B. Q. Li, H. J. Peng, Y. W. Song, M. Zhao, X. Chen, Q. Zhang, J. Q. Huang, Adv. Mater. (Weinheim, Ger.) 2019, 31, 1903813.

[9]	X. Ji, L. F. Nazar, Journal of Materials Chemistry 2010, 20, 9821-9826.

[10]	X. Fang, H. Peng, Small 2015, 11, 1488-1511.

[11]	Z. Jin, T. Lin, H. Jia, B. Liu, Q. Zhang, L. Li, L. Zhang, Z.-m. Su, C. Wang, ACS Nano 2021, 15, 7318-7327.

[12]	C. Wang, L. Sun, K. Li, Z. Wu, F. Zhang, L. Wang, ACS Appl. Mater. Interfaces 2020, 12, 43560-43567.

[13]	S. Feng, Z. H. Fu, X. Chen, B. Q. Li, H. J. Peng, N. Yao, X. Shen, L. Yu, Y. C. Gao, R. Zhang, Angewandte Chemie 2022, 134, e202211448.

[14]	Z. Yi, F. Su, L. Dai, Z. Wang, L. Xie, Z. Zuo, X. Chen, Y. Liu, C.-m. Chen, Energy Storage Materials 2022, 47, 327-335.

[15]	M. Fang, J. Han, S. He, J.-C. Ren, S. Li, W. Liu, Journal of the American Chemical Society 2023, 145, 12601-12608.

[16]	J. Chen, J. Zhong, S. Liu, Y. Wang, J. Hou, Q. Duan, ACS Applied Nano Materials 2024, 7, 15344-15353.

[17]	X. Zhang, X. Zhou, Y. Wang, Y. Li, Physical Chemistry Chemical Physics 2023, 25, 10097-10102.

[18]	X. Liu, Y. Zheng, M. Zhang, S. Qi, M. Tan, R. Zhao, M. Zhao, Advanced Materials Interfaces 2023, 10, 2202205.

[19]	Y. Jiang, H. Xie, L. Han, Y. Zhang, Y. Ding, S. Shen, B. Chen, M. Ni, Progress in Natural Science: Materials International 2023, 33, 133-150.

[20]	Y. Nishio, N. Kobayashi, Y. Muto, Journal of the Physical Society of Japan 1984, 53, 270-278.

[21]	N. Kobayashi, T. Sasaki, Y. Muto, Journal of the Physical Society of Japan 1980, 48, 1870-1878.

[22]	Z. Zhang, Y. Yang, G. Gao, B. I. Yakobson, Angewandte Chemie 2015, 127, 13214-13218.

[23]	M. Conrad, B. Harbrecht, T. Weber, D. Y. Jung, W. Steurer, Acta Crystallographica Section B: Structural Science 2009, 65, 318-325.

[24]	J. P. Perdew, K. Burke, M. Ernzerhof, Physical review letters 1996, 77, 3865.

[25]	L. Wang, Z. Hu, X. Wan, W. Hua, H. Li, Q. H. Yang, W. Wang, Advanced Energy Materials 2022, 12, 2200340.

[26]	A. Van De Walle, M. Asta, G. Ceder, Calphad 2002, 26, 539-553.

[27]	W. Zhao, L.-C. Xu, R. Li, Y. Guo, Z. Yang, R. Liu, X. Li, Materials Today Communications 2022, 30, 103196.

[28]	S. Meziane, H. Feraoun, T. Ouahrani, C. Esling, Journal of Alloys and Compounds 2013, 581, 731-740.

[29]	S. Hu, W.-X. Li, Science 2021, 374, 1360-1365.

[30]	S. Feng, Z. H. Fu, X. Chen, B. Q. Li, H. J. Peng, N. Yao, X. Shen, L. Yu, Y. C. Gao, R. Zhang, Q. Zhang, Angewandte Chemie International Edition 2022, 61.

[31]	T.-T. Yu, P.-F. Gao, Y. Zhang, S.-L. Zhang, Applied Surface Science 2019, 486, 281-286.

[32]	I. Muhammad, U. Younis, H. Xie, Y. Kawazoe, Q. Sun, Advanced Theory and Simulations 2020, 3.

[33]	H. Lin, N. Lou, D. Yang, R. Jin, Y. Huang, Journal of Alloys and Compounds 2021, 854.

[34]	Y.-X. Yu, Journal of Materials Chemistry A 2014, 2, 8910-8917.

[35]	T. Duan, L. Wang, Z. Ma, Y. Pei, Small 2023, 19.

[36]	J. Shen, X. Xu, J. Liu, Z. Wang, S. Zuo, Z. Liu, D. Zhang, J. Liu, M. Zhu, Advanced Energy Materials 2021, 11.

[37]	J. Xia, R. Cao, W. Xu, Q. Wu, Journal of Colloid and Interface Science 2024, 658, 795-804.

[38]	B. Mahesh, International Journal of Science and Research (IJSR) 2020, 9, 381-386.

[39]	R. Ouyang, S. Curtarolo, E. Ahmetcik, M. Scheffler, L. M. Ghiringhelli, Physical Review Materials 2018, 2.

[40]	X.-Y. Xiao, Z.-Y. Song, C.-C. Zhang, Y.-H. Zhao, Z.-W. Gao, S.-H. Chen, P.-H. Li, Y.-F. Sun, M. Yang, X.-J. Huang, Chemical Science 2023, 14, 2960-2970.